MECH 191 — Top 5 Board Terms by Week

The five most critical vocabulary terms to emphasize each week

MECH 191 — Metallurgy

Leeward Community College · Math and Science Division · Mechatronics Program

For instructor use — board reference, not a student handout

How to use this list

One page per week — just the five vocabulary terms most worth writing on the board that day, picked as the anchor concepts students need to walk away with.

# Week 1 — Atomic Structure & Bonding

| Alloy | An intentional mixture of two or more elements engineered for desired properties. |
| --- | --- |
| Metallic bond | Electrons form a shared 'electron sea' — explains conductivity and ductility. |
| Grain / grain boundary | A single crystal domain; the boundary between differently oriented grains. |
| Body-centered cubic (BCC) | A crystal structure with atoms at the eight corners of a cube plus one atom in the center; moderately packed (~68%), found in ferrite (α-iron), chromium, and tungsten — generally more brittle at low temperature than FCC metals. |
| Face-centered cubic (FCC) | A crystal structure with atoms at the eight corners of a cube plus one atom centered on each of the six faces; densely packed (~74%), found in austenite (γ-iron), aluminum, copper, and nickel — generally the most ductile common structure. |

# Week 2 — Mechanical Properties & Behavior

| Strength | A material's ability to resist an applied load without yielding or fracturing; most commonly reported as yield strength (the stress at which permanent deformation first begins) or ultimate tensile strength (the maximum stress the material reaches before necking). |
| --- | --- |
| Hardness | A material's resistance to localized permanent (plastic) deformation at its surface, measured by pressing a standardized indenter into the material under a known load and reading the size or depth of the resulting impression (Rockwell, Brinell, Vickers). |
| Ductility | A material's ability to undergo large plastic deformation — especially stretching — before it fractures, reported from a tensile test as % elongation or % reduction in area; high-ductility metals can be drawn into wire or deep-drawn into sheet parts. |
| Toughness | A material's ability to absorb energy and deform plastically before fracturing, combining strength and ductility; measured as the area under a material's stress-strain curve, or directly with an impact test (Charpy/Izod). |
| Brittleness | A material's tendency to fracture with little or no plastic deformation once its strength is exceeded — the opposite of ductility and toughness; brittle fractures happen suddenly and leave a flat, crystalline surface rather than necking or dimpling. |

# Week 4 — Carbon & Alloy Steels

| Ferrite / austenite (BCC/FCC iron) | Low-temp BCC iron phase vs. high-temp FCC iron phase — the basis of steel allotropy. |
| --- | --- |
| Carbon equivalent (CE) | CE = %C + %Mn/6 + (%Cr+%Mo+%V)/5 + (%Ni+%Cu)/15 — determines weldability/preheat needs. |
| Martensite | A hard, brittle, supersaturated body-centered tetragonal microstructure that forms when austenite is cooled too fast for diffusion to occur, trapping carbon in the iron lattice; requires tempering to restore usable toughness. |
| Hardenability | How deeply a steel can be hardened through its cross-section (different from hardness). |
| Quenching | Rapid cool from austenite — maximizes hardness (forms martensite). |

# Week 5 — Stainless Steels & Cast Irons

| Passive chromium oxide layer (Cr₂O₃) | Self-repairing surface film that makes stainless steel corrosion-resistant; requires ≥10.5% Cr. |
| --- | --- |
| Austenitic stainless (300 series) | FCC, non-magnetic, not hardenable by heat treatment — e.g. 304, 316. |
| Sensitization | Chromium carbide precipitation at grain boundaries during welding — depletes nearby Cr, causing intergranular corrosion susceptibility. |
| Gray cast iron | Carbon as graphite flakes — good damping/machinability, low tensile strength. |
| Ductile (nodular) iron | Mg/Ce addition makes graphite form as spheroids — much tougher than gray iron. |

# Week 6 — Nonferrous Metals & Phase Diagrams

| Aluminum alloy series (1xxx–7xxx) | Designation system by principal alloying element; heat-treatable vs. work-hardened series. |
| --- | --- |
| T6 temper | Solution treat + age — most common heat-treated condition for 6061/7075 aluminum. |
| Iron-carbon phase diagram | Maps stable phases across carbon content and temperature — ferrite, austenite, cementite, pearlite. |
| Eutectoid point | 0.77% C at 727°C — austenite transforms simultaneously to ferrite + cementite. |
| Brass (Cu-Zn) vs. Bronze (Cu-Sn / Cu-Al) | The two major copper alloy families — know composition and typical uses. |

# Week 7 — Mechanical Testing Methods

| Rockwell hardness test | Presses a diamond cone or hardened ball indenter into the surface under a minor then major load and reads hardness directly off the depth of penetration; fast and simple, the standard shop-floor check for finished, heat-treated steel parts. |
| --- | --- |
| Tensile test | A mechanical test in which a specimen is pulled along its axis at a controlled rate until it necks and fractures, while load and elongation are continuously recorded to determine yield strength, ultimate tensile strength, elastic modulus, and ductility. |
| S-N curve (Wöhler curve) | Plots stress amplitude vs. cycles to failure — used to find the fatigue limit. |
| Charpy impact test | An impact toughness test in which a notched specimen is supported horizontally at both ends and struck from behind the notch by a swinging pendulum, measuring the energy absorbed in fracture. |
| Ductile-brittle transition temperature (DBTT) | Temperature below which a material's fracture behavior shifts from tough to brittle. |

# Week 8 — Non-Destructive Testing (NDT) Methods

| Visual testing (VT) | The foundational inspection method — naked eye, lighting, magnification, borescopes. |
| --- | --- |
| Liquid/dye penetrant testing (PT) | Capillary action draws penetrant into surface-breaking defects; color contrast vs. fluorescent. |
| Magnetic particle testing (MT) | Detects surface/near-surface defects in ferromagnetic materials via flux leakage; yoke vs. prod methods. |
| Ultrasonic testing (UT) | Sound waves detect internal defects; A-scan, phased array (PAUT), straight vs. angle beam. |
| Radiographic testing (RT) | X-ray/gamma imaging of volumetric defects; film vs. digital radiography. |

# Week 9 — Quality Standards & Inspection

| Indication → Discontinuity → Defect → Reject | The precise evaluation sequence — memorize the distinct legal meaning of each term. |
| --- | --- |
| Porosity | A weld, casting, or PM defect consisting of small gas pockets (voids) trapped in the solidified or sintered metal, usually caused by dissolved or entrapped gas that could not escape before solidification finished. |
| Lack of fusion (LOF) | A weld defect in which the weld metal fails to bond completely with the base metal or with a previously deposited pass, leaving an unfused interface, usually caused by insufficient heat input, poor technique, or surface contamination. |
| Non-Conformance Report (NCR) | Formal documentation raised when a component is rejected. |
| Traceability | Linking an inspection record to the physical component via unique identifiers. |

# Week 10 — Casting Processes & Defect Recognition

| Sand casting | Pattern, mold, cores, gating system — flexible, low tooling cost, rough finish. |
| --- | --- |
| Die casting (hot chamber vs. cold chamber) | High-pressure injection into a reusable die — limited to lower-melting alloys. |
| Investment (lost-wax) casting | Ceramic shell over a wax pattern — best surface finish and accuracy of any casting process. |
| Gating system | The complete network of channels in a sand-casting mold that carries molten metal from the pouring cup into the mold cavity. |
| Shrinkage porosity / gas porosity | Two major casting defect types — irregular voids vs. smooth spherical voids. |

# Week 11 — Metal Forming Processes

| Hot working vs. cold working | No work hardening vs. work hardening — know the trade-offs of each. |
| --- | --- |
| Rolling | Reducing a metal's thickness (or forming its cross-section) by passing it between rotating rolls; performed hot or cold and used to produce plate, sheet, and structural shapes. |
| Forging | A compressive shaping process that hammers or presses metal into shape, producing the highest-integrity wrought parts; performed with open or closed dies. |
| Extrusion (direct vs. indirect) | Forcing metal through a die to produce constant-cross-section profiles. |
| Drawing | Pulling metal through a die (or forming it with a punch) under tension to reduce its cross-section or reshape it — as in wire drawing, tube drawing, and deep drawing. |

# Week 12 — Machining

| Turning | A machining process in which a cutting tool removes material from a rotating workpiece on a lathe to produce cylindrical or conical external and internal surfaces. |
| --- | --- |
| Milling | A machining process in which a rotating multi-tooth cutter removes material from a stationary or moving workpiece to produce flat surfaces, slots, pockets, and contoured features. |
| Cutting speed (Vc) | The speed at which the cutting edge moves relative to the workpiece surface, usually in meters per minute (m/min); set primarily by the tool material and the workpiece being cut. |
| Feed (f) | The distance the cutting tool advances relative to the workpiece per revolution (turning) or per tooth (milling), which — together with the tool's nose radius — largely determines the resulting surface finish. |
| Surface roughness: Ra and Rz | Arithmetic mean roughness vs. peak-to-valley height — the two key surface finish parameters. |

# Week 13 — Powder Metallurgy

| Sintering | Densification by solid-state atomic diffusion below the melting point — not melting. |
| --- | --- |
| Green compact / green strength | The fragile, pressed-but-unsintered powder part before sintering. |
| Hot isostatic pressing (HIP) | Simultaneous heat + isostatic gas pressure — eliminates porosity, approaches wrought properties. |
| Additive manufacturing | A family of layer-by-layer metal powder or wire fusion processes that build a part directly from a 3D model, with no tooling required. |
| Water atomization vs. gas atomization | Powder production methods producing irregular vs. spherical particle shapes. |

# Week 14 — Welding Processes

| SMAW (Shielded Metal Arc Welding / Stick) | Coated consumable electrode; flux forms shielding gas and slag. |
| --- | --- |
| GMAW (Gas Metal Arc Welding / MIG) | Continuous bare wire with shielding gas; transfer modes: short circuit, spray, pulsed. |
| GTAW (Gas Tungsten Arc Welding / TIG) | Non-consumable tungsten electrode; highest quality; AC for aluminum, DCEN for steel. |
| Heat input formula | HI = (V × A × 60) / (1000 × travel speed) → kJ/mm — controls cooling rate and grain size. |
| Preheat / interpass temperature | Minimum temperature before/during welding to slow cooling and prevent HAZ cracking. |

# Week 15 — Weld Metallurgy & Failure

| Heat-affected zone (HAZ) | Base metal heated above ~730°C but not melted — the most failure-prone weld region. |
| --- | --- |
| Dilution | The proportion of melted base metal mixed into the deposited weld metal. |
| Hydrogen-induced cracking (HIC) / cold cracking | Delayed cracking requiring three simultaneous conditions: susceptible microstructure, hydrogen, tensile stress. |
| Ductile fracture (microvoid coalescence, cup-and-cone) | Fracture with plastic deformation, dimpled surface. |
| Brittle fracture (cleavage, chevron marks, river marks) | Sudden fracture with no plastic deformation; flat, crystalline surface. |

# Week 16 — Corrosion

| Four-element corrosion cell (anode, cathode, electrolyte, metallic path) | All four must be present for electrochemical corrosion — remove one to stop it. |
| --- | --- |
| Galvanic series | Ranking of metals by electrochemical potential — determines which metal corrodes when dissimilar metals contact. |
| Passivation | Formation of a stable, adherent oxide layer that slows corrosion (stainless, aluminum, titanium). |
| Pitting corrosion / PREN | Localized passive-film breakdown; Pitting Resistance Equivalent Number quantifies alloy resistance. |
| Cathodic protection (sacrificial anode vs. impressed current) | Makes the structure the cathode so corrosion occurs only at a sacrificial anode. |

# Course Wrap-Up — Semester Synthesis

| Metallic bond | Electrons form a shared 'electron sea' — explains conductivity and ductility. |
| --- | --- |
| Carbon equivalent (CE) | CE = %C + %Mn/6 + (%Cr+%Mo+%V)/5 + (%Ni+%Cu)/15 — determines weldability/preheat needs. |
| Ultrasonic testing (UT) | Sound waves detect internal defects; A-scan, phased array (PAUT), straight vs. angle beam. |
| Forging | A compressive shaping process that hammers or presses metal into shape, producing the highest-integrity wrought parts; performed with open or closed dies. |
| Heat-affected zone (HAZ) | Base metal heated above ~730°C but not melted — the most failure-prone weld region. |