## Slide 1
M E C H 1 9 1 — M e t a l l u r g y
Week 13
Powder Metallurgy
November 16, 2026 · 5:00 – 7:30 PM · Kai Santos

## Slide 2
Class Agenda
01
Powder Production & Compaction
Atomisation methods, particle characteristics, die compaction, density gradients, and the green compact
02
Sintering & Advanced PM Processes
Sintering stages, atmosphere control, liquid phase sintering, MIM, HIP, and additive manufacturing
03
PM Defects & Process Selection
Density gradients, lamination cracks, blistering — and the Unit 4 process selection framework

## Slide 3
Alloy Research Portfolio — Module 12
No Microscope Required
Module 12 · Week 13
Copper Alloys
What to do this week:
Research 110 copper vs. 182 chromium copper: composition, conductivity,
and published HV for your Hardness Log. Powder metallurgy is covered
in today's lecture, not in this research module.
Steps:
1 Research — record data & sources
2 Answer — short-answer questions
3 Apply — critical-thinking & equations
Alloys of Record
· Alloys N, O — 110 copper & 182 chromium copper
How to Complete This Module:
1 Research the alloy(s) using credible sources
2 Record data with a source citation
3 Answer the short-answer questions
4 Answer the critical-thinking questions
5 Keep the module with your portfolio
Portfolio Handout — Module 12

## Slide 4
MECH 191 — Course & Unit Roadmap
Unit 1
Materials Fundamentals
Unit 2
Steel & Alloys
Unit 3
Testing & Quality
Unit 4
Manufacturing
Unit 5
Joining & Failure
Wk 1
Aug 24
Atomic Structure
& Bonding
Wk 4
Sep 14
Carbon &
Alloy Steels
Wk 7
Oct 5
Mechanical
Testing
Wk 10
Oct 26
Casting
Wk 14
Nov 23
Welding
Processes
Wk 2
Aug 31
Mechanical
Properties
Wk 5
Sep 21
Stainless &
Cast Irons
Wk 8
Oct 12
NDT Methods
Wk 11
Nov 2
Forming
Wk 15
Nov 30
Weld Metallurgy
& Failure
Wk 6
Sep 28
Nonferrous &
Phase Diagrams
Wk 9
Oct 19
Quality
Standards
Wk 12
Nov 9
Machining
Wk 16
Dec 7
Corrosion
& Wrap-up
Wk 13 ← here
Nov 16
Powder
Metallurgy
Week 17 · FINAL EXAM

## Slide 5
Week 13 — At a Glance
Topics
Powder production — water atomisation, gas atomisation, oxide reduction,
electrolytic, and carbonyl processes; particle characterization
Compaction — blending with lubricants, die compaction, density gradients,
green compact strength, and isostatic pressing (CIP/HIP)
Sintering — atmosphere control, three stages (burn-off, neck formation,
densification), and liquid phase sintering
Advanced PM — metal injection molding (MIM), hot isostatic pressing, and
additive manufacturing with metal powder feedstock
PM defects — density gradients, lamination cracks, blistering, and
dimensional variation from sintering shrinkage
Process selection — matching alloy, geometry, tolerance, volume, and cost
requirements across all Unit 4 processes
Resources
Reference Material
Kalpakjian Ch. 17
Powder Metallurgy — production, compaction,
sintering, and applications
Visualizers
MPIF Process Overview · Sintering Animation
Atomisation & Powder Production
Manufacturing Process Selection
Key Fact
Conventional PM: 85–95% theoretical density ·
Sintering shrinkage: 1–3%
Next: Week 14 — Welding Processes

## Slide 6
Core Questions
Try to answer these before we dive in — we'll revisit them with answers at the end of class.
1
What is powder metallurgy and what advantages does it offer over casting and machining?
2
How are metal powders produced, compacted, and sintered?
3
What are the limitations of powder metallurgy and what defects should a technician look for?
4
How do you select the right manufacturing process for a given application?

## Slide 7
Powder Production — How Metal Powders Are Made
Production Methods
Water Atomisation
Molten metal stream broken by high-pressure water jets — irregular, oxidized
particles, 50–200 μm. Most widely used for iron and steel; low cost; requires
reducing atmosphere sintering to remove surface oxides.
Gas Atomisation
Inert gas (argon or nitrogen) jets produce spherical, clean particles. Higher
cost; preferred for stainless steel, nickel superalloy, titanium, and tool steel.
Better flowability and packing density than water atomised powder.
Oxide Reduction
Iron oxide reduced by hydrogen or CO at elevated temperature — sponge iron
with irregular, porous morphology. Excellent green strength from mechanical
particle interlocking. Widely used for structural iron PM parts.
Electrolytic & Carbonyl
Electrolytic deposition produces high-purity dendritic copper and iron.
Carbonyl process decomposes metal carbonyls to yield extremely fine (1–10
μm) spherical iron or nickel powder — used in MIM and speciality
applications.
Powder Characterization
Powder characteristics directly control compaction behavior, green density,
and sintered properties — they are controlled specifications, not incidental
measurements.
Particle size distribution
Controls green density and flow — finer particles pack better but flow poorly;
measured by sieve analysis or laser diffraction.
Particle shape
Irregular particles interlock for higher green strength; spherical particles flow
better. Shape is set by the production method.
Apparent & tap density
Apparent density: freely poured; tap density: after vibration. Hausner ratio =
tap/apparent — indicates flow and compressibility.
Flow rate
Measured by Hall flowmeter — critical for automatic die filling; poor flow
causes density variations across the compact.

## Slide 8
Compaction — Die Filling, Pressing & the Green Compact
Die Compaction Process
1
Blending
Powder blended with lubricant (zinc stearate) to reduce die wall
friction and aid ejection; alloying additions (graphite for carbon
content, copper for strengthening) are mixed in uniformly.
2
Die Filling
Powder gravity- or force-fed into a closed die. Uniform filling is critical
— inconsistent fill causes green density variation and dimensional
scatter in sintered parts.
3
Pressing — 150 to 700 MPa
Upper and lower punches press simultaneously — pressing from both
ends reduces the density gradient through the part height. Pressure
proportional to final density.
4
Ejection — Green Compact
Compact ejected from the die. Green strength 5–15 MPa from
mechanical particle interlocking — fragile; handled carefully before
sintering. Predictable 1–3% shrinkage on sintering.
Density Gradient & Isostatic Pressing
The Density Gradient Problem
Compaction pressure attenuates with distance from the punch faces due to
inter-particle and die-wall friction — tall parts have lower density in the center.
Controlled by using multiple independently moving punch segments and limiting
the height-to-diameter ratio. Low-density zones have lower strength and
become failure initiation sites in service.
Isostatic Pressing — Eliminating Gradients
Powder sealed in a flexible membrane compressed by fluid pressure from all
directions simultaneously — no density gradient by design.
CIP — Cold Isostatic Pressing
Room temperature; used for large or complex shapes where die compaction
cannot reach uniform density.
HIP — Hot Isostatic Pressing
Simultaneous heat and pressure (100–200 MPa argon) — 99%+ theoretical
density; properties approach wrought. Used for aerospace superalloy discs,
titanium components, and tool steel dies.

## Slide 9
Sintering — Densification Without Melting
Three Stages of Sintering
1
Burn-off — 300 to 500°C
Lubricant is volatilised and removed from the compact before the
sintering temperature is reached. This stage cannot be rushed —
trapped lubricant vapour expands and causes surface blistering.
2
Neck Formation — 70 to 90% of Tm
At sintering temperature, atoms diffuse across particle contact
points forming necks. Porosity is reduced rapidly and strength
increases. For iron PM: approximately 1100–1150°C.
3
Densification & Grain Growth
Continued sintering reduces porosity further and grains coarsen.
Densification is desirable; grain growth reduces mechanical
properties — time and temperature must be optimised for the
alloy.
Atmosphere & Liquid Phase Sintering
Sintering Atmosphere
Atmosphere must prevent oxidation throughout the furnace cycle.
Hydrogen / Dissociated ammonia
Iron, copper, and their alloys — reducing atmosphere removes surface oxides
from the powder particles.
Nitrogen-hydrogen mixtures
Most structural PM steels — good reducing power at lower cost than pure
hydrogen.
Vacuum
Stainless steel, titanium, and reactive metals — prevents any oxidation at
sintering temperature.
Liquid Phase Sintering
A small amount of a lower-melting additive (cobalt in WC-Co; copper in iron PM)
melts during sintering and fills pores by capillary action — dramatically
accelerates densification. This is the key to tungsten carbide-cobalt cutting tool
manufacture: WC particles bonded by liquid cobalt that re-solidifies on cooling.

## Slide 10
Secondary Operations & PM Applications
Secondary Operations
Coining (Re-pressing)
Sintered parts re-pressed in a die to close surface porosity and improve
dimensional accuracy — increases density by 2–5% in surface layers.
Sizing
Re-pressing to correct dimensional variation from sintering shrinkage —
achieves tolerances of ±0.025 mm on critical dimensions.
Infiltration
Liquid copper or bronze drawn into pores by capillary action — fills porosity,
increases density and strength, improves machinability.
Oil Impregnation
Vacuum-impregnated porous bronze or iron bearings — oil stored in
interconnected pores and released to the bearing surface during operation.
Heat Treatment
PM parts through-hardened, case-carburised, or induction hardened —
porosity slightly reduces hardenability; thin sections monitored carefully.
Major PM Applications
Automotive
Connecting rod bearings, valve seat inserts, cam lobes, transmission
synchroniser hubs — largest PM market by volume.
Cutting Tools
Tungsten carbide-cobalt (WC-Co) inserts and drill blanks — PM via liquid phase
sintering is the only practical route to WC-Co.
Self-Lubricating Bearings
Oil-impregnated porous bronze and iron bearings in appliances, office
equipment, and automotive accessories.
Magnetic Components
Soft magnetic cores for motors and transformers; permanent magnets (NdFeB,
SmCo) for electric motors and sensors.
Medical & Dental
Implant components and dental crowns produced by MIM or DMLS — complex
geometry, high dimensional precision required.

## Slide 11
Advanced PM Processes — MIM, HIP & Additive Manufacturing
Metal Injection
Molding (MIM)
Complex small parts · Near full density
Very fine powder (1–20 μm) mixed with a
polymer binder to form a feedstock that is
injection molded like a plastic part. Binder
removed by solvent and thermal debinding; part
then sintered to 96–99% density. Produces
complex small parts under 100 g with good
surface finish and tight tolerances — used for
firearms components, medical instruments,
orthodontic brackets, and electronic hardware.
No die-compaction geometry limits.
Hot Isostatic
Pressing (HIP)
Highest density · Aerospace & medical
Powder or pre-sintered part sealed in a metal can
subjected to simultaneous high temperature and
high isostatic gas pressure (100–200 MPa argon).
Eliminates virtually all porosity — achieves 99%+
of theoretical density with isotropic properties
approaching wrought material. Used for
aerospace superalloy turbine discs, titanium
structural components, and tool steel dies where
100% density is a design requirement.
Additive
Manufacturing
Layer-by-layer · No tooling required
SLM (selective laser melting), EBM (electron
beam melting), and DED (directed energy
deposition) use gas atomised metal powder as
feedstock — fused layer by layer to build near-
net-shape parts. No tooling required; complex
internal channels and lattice structures
impossible by conventional methods. Fastest
growing area of PM technology — used for
aerospace brackets, medical implants with porous
ingrowth surfaces, and tooling inserts with
conformal cooling.

## Slide 12
PM Defects — Recognition and Detection
Defect
Cause
Appearance
Location
Detection
Action
Density
Gradients
Uneven compaction — pressure
attenuates from punch faces due to
inter-particle and die-wall friction;
most severe in tall or complex parts
No surface indication; lower
hardness on Vickers traverse
across the compact section;
lower density zones visible on
cross-section
Interior of compact,
away from punch
contact faces; typically
mid-height of tall parts
Hardness traverse;
density measurement;
UT velocity mapping
Multiple punch segments; limit height-
to-diameter ratio; optimise lubricant
content
Lamination
Cracks
Spring-back of compact on die
ejection — elastic recovery of the
powder mass causes horizontal
fracture planes perpendicular to
the pressing direction
Thin planar separations
perpendicular to pressing
direction — may not be visible on
the surface; crack plane parallel
to the compact base
Through compact cross-
section, perpendicular
to pressing axis; often
near the ends of the
compact
UT — planar crack
reflects beam clearly;
visual on fracture
surface if crack opens
during handling
Reduce ejection speed; increase die wall
taper; optimise lubricant level and
compaction pressure
Surface
Blistering
Trapped lubricant vapour expands
during sintering — caused by
rushing the burn-off stage (300–
500°C) or by contamination with
low-vapour-pressure material in the
powder blend
Raised blisters or bubbles on the
sintered surface; 1–10 mm
diameter depending on
contamination severity
Surface of sintered
compact; most
common where
lubricant burn-off is
slowest in the furnace
load
VT; surface
profilometry; cross-
section metallography
to reveal subsurface
void
Extend burn-off stage; reduce heating
rate through 300–500°C; verify lubricant
content and blend uniformity
Dimensional
Variation
Batch-to-batch changes in powder
characteristics (particle size,
apparent density) shift green
density and sintering shrinkage (1–
3%) — final part dimensions change
between batches
Parts outside dimensional
tolerance — not detectable by
visual inspection; found only by
measurement
All PM parts; most
critical on precision
bores, mating faces,
and any feature with
tight tolerance
CMM or gauge
measurement; 100%
dimensional inspection
is standard for critical
PM components
Tighten powder characterization
specification; coining or sizing after
sintering to correct critical dimensions

## Slide 13
Manufacturing Process Selection — Unit 4 Summary
5-Step Decision Framework
1
Alloy compatibility
Does the alloy constrain the process? Die casting cannot process steel; PM
cannot easily process reactive alloys without vacuum sintering; investment
casting handles almost any alloy.
2
Part geometry
Very large parts eliminate die casting and PM; complex internal geometry
favours casting with cores; parts with tight bores and flat surfaces require
machining.
3
Tolerance & surface finish
Sand casting for loose tolerances; grinding for very tight (Ra 0.025–0.8 μm);
PM for moderate; machining bridges the gap between casting and grinding.
4
Production volume
High volume favours die casting, PM, and cold forming with high tooling
investment; low volume favours sand casting and machining from bar stock.
5
Cost target
PM and die casting amortise high tooling cost over many parts; sand casting
and machining have low tooling cost but higher per-part cost.
Unit 4 Process Comparison
Casting
Alloy: excellent flexibility. Geometry: complex external and internal (cores).
Volume: sand = low; die = high. Finish: rough to moderate. Key defect:
porosity.
Forming (Forging & Rolling)
Alloy: wrought metals only. Geometry: limited — no internal features. Volume:
medium to high. Finish: moderate. Key advantage: superior grain flow and
fatigue life.
Machining
Alloy: almost any. Geometry: any external and internal features. Volume: any.
Finish: finest (Ra 0.025–0.8 μm). Limitation: material waste 50–90%; cost is
high per part.
Powder Metallurgy
Alloy: limited (no reactive without vacuum). Geometry: moderate — vertical
ejection only. Volume: medium to high. Key niche: WC-Co tools, self-lubricating
bearings, near-net-shape.

## Slide 14
Core Question Answers
What is powder metallurgy and what advantages does it offer over casting and machining?
PM starts with metal powder pressed into a die at 150–700 MPa then sintered at 70–90% of the melting point — solid-state diffusion bonds particles
without melting. Advantages: near-net-shape with minimal material waste; enables materials impossible by other routes (WC-Co cutting tools, self-
lubricating porous bearings, controlled-porosity filters); eliminates many secondary operations. Limitation: 85–95% theoretical density; economical only at
moderate to high volumes due to tooling cost.
How are metal powders produced, compacted, and sintered?
Production: water atomisation (irregular, iron/steel), gas atomisation (spherical, stainless/superalloys), reduction (sponge iron), electrolytic/carbonyl (high
purity). Compaction: blended with lubricant, die-filled, pressed from both ends at 150–700 MPa — green compact has 5–15 MPa strength. Sintering: burn-
off lubricant at 300–500°C, neck formation at 70–90% Tm (~1100–1150°C for iron), densification with controlled atmosphere (H₂, N₂, or vacuum) and
predictable 1–3% shrinkage.
What are the limitations of PM and what defects should a technician look for?
Limitations: density 85–95% theoretical; geometry limited to vertical die ejection; tooling cost high; part size limited by press capacity. Key defects: density
gradients (uneven compaction — detect by hardness traverse or UT); lamination cracks (spring-back on ejection — planar crack perpendicular to pressing
axis, detect by UT); blistering (rushed burn-off stage — VT); dimensional variation (powder batch changes — 100% measurement inspection).
How do you select the right manufacturing process for a given application?
Work through five factors in sequence: (1) alloy compatibility — does it constrain the process? (2) geometry — does part complexity eliminate options? (3)
tolerance and surface finish required; (4) production volume — high volume justifies high tooling investment; (5) cost target. Most finished parts involve
multiple processes in sequence — a casting that is then machined, or a forging that is then ground. Understanding the full manufacturing chain, not just the
individual operation, is the mark of a quality technician.

## Slide 15
Key Takeaways — Week 13: Powder Metallurgy
1
Powder metallurgy occupies a unique manufacturing niche — it is the only practical route to certain materials (WC-Co cutting tools,
self-lubricating bearings, controlled-porosity filters) and offers exceptional material efficiency; its limitations in density and
geometry constrain where it can be used but do not diminish its importance in the manufacturing landscape.
2
Sintering is a thermally activated diffusion process, not melting — controlling atmosphere, temperature, and time determines the
final density, microstructure, and mechanical properties of the PM part; deviations from the qualified sintering cycle are a quality
concern just as critical as incorrect heat treatment in steel.
3
Process selection across all Unit 4 processes requires simultaneously satisfying alloy, geometry, tolerance, volume, and cost
requirements — no single process is universally best, and most finished components involve multiple processes in sequence; a
technician who understands the capabilities and limitations of each process can reason about the entire manufacturing chain, not
just the individual step they are inspecting.

## Slide 16
Resources & What's Next
Week 13 Resources
Kalpakjian Ch. 17
Powder Metallurgy — production, compaction, sintering, and applications —
primary reading
MPIF Process Overview
Metal Powder Industries Federation interactive PM process visualizer
Sintering — Neck Formation
Animated sintering stages: burn-off, neck formation, and densification
Atomisation & Powder Production
Water vs. gas vs. reduction methods — particle shape and characteristics
Manufacturing Process Selection
Unit 4 summary tool — casting vs. forming vs. machining vs. PM
Week 14 — Welding Processes
November 23, 2026 · Unit 5: Joining & Failure begins
•
Fusion welding processes — SMAW, MIG, TIG, and their
applications
•
Heat input and the weld thermal cycle — heat-affected
zone formation
•
Weld joint design — groove, fillet, plug, and slot welds
•
Solidification of the weld pool — columnar grain
growth and cracking
•
Weld inspection and qualification — VT, RT, UT, MT, and
PT