## Slide 1
M E C H 1 9 1 — M e t a l l u r g y
Week 14
Welding Processes
November 23, 2026 · 5:00 – 7:30 PM · Kai Santos

## Slide 2
Class Agenda
01
Arc Welding Processes
SMAW, GMAW, GTAW, and FCAW — how each works, what it's used for, and its quality risks
02
Filler Metals & Thermal Control
AWS filler classification, matching vs. overmatching, preheat, interpass temperature, and carbon equivalent
03
Weld Symbols & Technician Responsibilities
Reading the reference line, identifying weld type and size, and applying the symbol to inspection

## Slide 3
Alloy Research Portfolio — Module 13
No Microscope Required
Module 13 · Week 14
Brass Alloys
What to do this week:
Research 260, 360, and 464 brass: zinc content, phase structure, and
published HV for your Hardness Log. Welding fundamentals are covered
in today's lecture, not in this research module.
Steps:
1 Research — record data & sources
2 Answer — short-answer questions
3 Apply — critical-thinking & equations
Alloys of Record
· Alloys K, L, M — 260, 360 & 464 brass
How to Complete This Module:
1 Research the alloy(s) using credible sources
2 Record data with a source citation
3 Answer the short-answer questions
4 Answer the critical-thinking questions
5 Keep the module with your portfolio
Portfolio Handout — Module 13

## Slide 4
MECH 191 — Course & Unit Roadmap
Unit 1
Materials Fundamentals
Unit 2
Steel & Alloys
Unit 3
Testing & Quality
Unit 4
Manufacturing
Unit 5
Joining & Failure
Wk 1
Aug 24
Atomic Structure
& Bonding
Wk 4
Sep 14
Carbon &
Alloy Steels
Wk 7
Oct 5
Mechanical
Testing
Wk 10
Oct 26
Casting
Wk 14 ← here
Nov 23
Welding
Processes
Wk 2
Aug 31
Mechanical
Properties
Wk 5
Sep 21
Stainless &
Cast Irons
Wk 8
Oct 12
NDT Methods
Wk 11
Nov 2
Forming
Wk 15
Nov 30
Weld Metallurgy
& Failure
Wk 6
Sep 28
Nonferrous &
Phase Diagrams
Wk 9
Oct 19
Quality
Standards
Wk 12
Nov 9
Machining
Wk 16
Dec 7
Corrosion
& Wrap-up
Wk 13
Nov 16
Powder
Metallurgy
Week 17 · FINAL EXAM

## Slide 5
Week 14 — At a Glance
Topics
Welding fundamentals — heat sources, joint types, groove preparations, weld
positions, and heat input formula
SMAW — stick welding, coated electrodes, E7018 classification, slag protection,
and low-hydrogen storage
GMAW — MIG welding, continuous wire, shielding gases, transfer modes (short
circuit, spray, pulsed)
GTAW — TIG welding, non-consumable tungsten, AC for aluminum, DCEN for
steel, highest quality
FCAW — flux-cored wire, self-shielded vs. gas-shielded, high deposition rate,
structural steel
Preheat & interpass — carbon equivalent, cooling rate control, HIC prevention,
verification methods
Weld symbols — reference line anatomy, arrow side vs. other side, weld type, size,
length, and tail
Resources
Reference Material
Kalpakjian Ch. 30 · Moniz Ch. 27
Fusion Welding Processes & Welding Metallurgy
Visualizers
SMAW — Arc & AWS Classification
GMAW — Transfer Modes & Shielding Gas
FCAW — Self-Shielded vs Gas-Shielded
GTAW — Tungsten & Filler Classification
Key Reference
AWS D1.1 Structural Welding Code
Weld Symbols — AWS A2.4
Preheat Calculator — Lincoln Electric
Next: Week 15 — Weld Metallurgy & Failure

## Slide 6
Core Questions
Try to answer these before we dive in — we'll revisit them with answers at the end of class.
1
What is welding and how does it create a metallurgical bond?
2
What are the main arc welding processes and when is each used?
3
How do filler metals work and how are they selected?
4
What are preheat and interpass temperature and why are they quality-critical?
5
How do you read a basic weld symbol?

## Slide 7
Welding Fundamentals — Joint Design & Heat Input
Joint Types & Groove Preparations
Five basic joint types:
Butt — two pieces edge to edge (most common in pipe and plate)
T-joint — one piece perpendicular to another (fillet or groove weld)
Lap — two pieces overlapping (fillet each side)
Corner — two pieces at right angles at their edges
Edge — two pieces parallel, welded along their edges
Groove preparations:
Square groove
Thin material; full penetration without bevel; simple and fast.
V-groove
Most common; single or double; bevel angle controls penetration and
weld volume.
U-groove
Thick material; reduced weld volume vs. V-groove; more prep cost but
less filler.
Bevel groove
Single-sided access only; one plate bevelled, the other left square.
Positions, Heat Input & Bond Formation
How welding creates a metallurgical bond:
A heat source melts the base metal and filler to form a weld pool — as it
solidifies, a continuous metallic connection forms across the joint. The joint
is not glued; it is a continuation of the metal itself. Microstructure and
mechanical properties are determined by the thermal cycle experienced.
Weld positions:
Flat (1G/1F) · Horizontal (2G/2F) · Vertical (3G/3F) · Overhead (4G/4F)
Position affects heat input control, weld pool behavior, and the skill required.
Procedure and welder qualifications are position-specific.
Heat Input
HI = (V × A × 60) / (1000 × travel speed mm/min) → kJ/mm
Higher heat input → slower cooling → coarser grain structure, wider HAZ, more
distortion
Lower heat input → faster cooling → finer grain structure, greater risk of
hydrogen cracking in hardenable steels
Heat input specified in the WPS and must be controlled within limits.

## Slide 8
SMAW & GMAW — Stick and MIG Welding
SMAW — Shielded Metal Arc Welding
How it works
Consumable coated electrode; the arc melts both the core wire and the flux
coating. Molten flux forms a shielding gas and a slag layer that floats on the
pool and slows cooling — slag removed between passes.
Equipment
AC or DC power source, electrode holder, work clamp, cables — minimal
equipment, highly portable. Can be used anywhere with a power supply.
E7018 — AWS Classification
E = electrode · 70 = 70 ksi (480 MPa) minimum tensile · 1 = all positions · 8
= low-hydrogen flux, DC or AC. Must be stored in a heated oven; use within 4
hours of removal.
Advantages / Limitations
Versatile, portable, all-position, tolerant of surface contamination and wind.
Lower deposition rate than GMAW/FCAW; frequent electrode changes; slag
removal required; skill-dependent.
GMAW — Gas Metal Arc Welding (MIG)
How it works
Continuous bare wire fed from a spool through the gun — no electrode
changes. Shielding gas protects the arc. Arc length is self-regulating with a
constant-voltage (CV) power source.
Shielding gases
Pure argon: non-ferrous metals (Al, Cu, Ti) — stable arc, good wetting.
Pure CO₂: carbon steel — deep penetration, more spatter, low cost.
75Ar/25CO₂: most common for structural steel — best balance of stability,
penetration, and spatter.
Transfer modes
Short circuit: low V/A — thin material and out-of-position; risk of lack of fusion.
Spray: high V/A — flat/horizontal only; high deposition, excellent fusion.
Pulsed spray: combines high rate with out-of-position capability.
Advantages / Limitations
High deposition rate, no slag removal, suitable for automation, good for thin to
medium material. Sensitive to drafts (outdoor use needs windshields); requires
clean base metal; less portable than SMAW.

## Slide 9
GTAW & FCAW — TIG and Flux-Cored Welding
GTAW — Gas Tungsten Arc Welding (TIG)
How it works
Non-consumable tungsten electrode — only the base metal and separately
fed filler rod melt. Complete independent control of heat input and filler
addition. No spatter; no slag.
AC vs. DCEN
AC for aluminum: positive half-cycle cleans the oxide layer (Al₂O₃ melts at
2050°C, base metal at 660°C); negative half-cycle provides penetration.
DCEN for steel and stainless: maximum heat into the workpiece, narrow deep
penetration profile.
Applications
Root passes in pipe and pressure vessel welds; thin sheet; stainless steel,
aluminum, titanium; any application where quality takes precedence over
productivity.
Advantages / Limitations
Highest quality welds; precise heat control; all materials and positions.
Slowest arc process; highest skill required; filler by hand limits deposition rate;
not economical for thick material.
FCAW — Flux-Cored Arc Welding
How it works
Tubular wire filled with flux fed continuously — same equipment as GMAW but
combines continuous wire feeding with slag protection. Higher current density
than solid wire gives higher deposition rate.
FCAW-S vs. FCAW-G
Self-shielded (FCAW-S): flux core generates its own shielding — no external
gas; highly portable and tolerant of wind; AWS D1.1 approved for structural
steel site welding.
Gas-shielded (FCAW-G): external CO₂/mixed gas added — better mechanical
properties and lower fumes; preferred for shop fabrication.
Applications
Heavy structural fabrication, shipbuilding, heavy equipment manufacture —
wherever high deposition rate and tolerance to mill scale are required. Out-of-
position with appropriate wire.
Advantages / Limitations
High deposition rate; all-position capability; tolerant of mill scale and
contamination. Slag removal required between passes; higher fume
generation; FCAW-S generally lower toughness weld metal.

## Slide 10
Filler Metals — Classification and Selection
How Filler Metals Work
Filler metal melts into the weld pool and becomes part of the deposited
weld metal — its composition determines the as-welded
microstructure, mechanical properties, and corrosion resistance.
Match or overmatch
Filler selected to meet or exceed base metal minimum tensile strength — an
undermatching weld is the weakest point of the joint and will fail first.
Chemical compatibility
Filler must be chemically compatible with the base metal and process —
different processes use different filler forms (coated electrode, bare wire, flux-
cored wire, rod).
Dilution
Deposited weld metal is a mix of filler and melted base metal. SMAW: 20–30%
dilution. GMAW: 25–35%. SAW: 50–70%. The WPS specifies the filler to
account for dilution.
AWS Classification System
Prefix letter identifies the form: E = electrode; ER = electrode or rod; R = rod
only.
E7018 — SMAW low-hydrogen electrode
E = electrode (SMAW consumable coated rod)
70 = 70 ksi (480 MPa) minimum tensile strength
1 = all-position capability (1G, 2G, 3G, 4G)
8 = low-hydrogen potassium flux; DC or AC; bake before use
ER308L — GTAW/GMAW stainless steel wire
ER = electrode or rod
308 = austenitic stainless filler for 304/308 base metal
L = low carbon (≤ 0.03% C) — prevents sensitization
ER4043 — GTAW/GMAW aluminum wire
ER = electrode or rod
4043 = aluminum-silicon filler for 6xxx series alloys
Lower cracking risk than 5xxx fillers for heat-treatable alloys

## Slide 11
Preheat & Interpass Temperature — Controlling the HAZ
Carbon Equivalent & Preheat
Preheat is the minimum temperature the base metal must reach before
welding begins. It slows the cooling rate of the weld and HAZ —
preventing brittle martensite formation and allowing hydrogen to
diffuse out before it can cause cracking.
Carbon Equivalent (CE) Formula:
CE = C + Mn/6 + (Cr+Mo+V)/5 + (Ni+Cu)/15
Higher CE = higher hardenability = higher preheat required.
CE < 0.40
Generally no preheat required for thin sections.
CE 0.40–0.60
Preheat typically 100–200°C; required for thicker
sections.
CE > 0.60
Preheat 200–300°C or higher; mandatory for most
applications.
Interpass Temperature, Verification & PWHT
Interpass temperature minimum
Must not cool below the preheat temperature between passes — critical for
multi-pass welds on thick sections where the joint can cool rapidly.
Interpass temperature maximum
Carbon steel typically 250–300°C. Austenitic stainless typically 150°C maximum
— excessive heat causes sensitization (Cr₂₃C₆ precipitation at grain boundaries,
reducing corrosion resistance).
Verification
Tempilstik (temperature-indicating crayons), contact thermometers, or infrared
pyrometers. Per AWS D1.1: verify at 75 mm from the joint each side,
immediately before welding.
Post-Weld Heat Treatment (PWHT)
Stress relief PWHT reduces residual stress and tempers HAZ martensite —
mandatory in many pressure vessel and piping codes above certain thickness
and CE thresholds. Temperature, heating/cooling rate, and hold time are
specified in the applicable code and WPS.

## Slide 12
Weld Symbols — Reading the Drawing Standard
Anatomy of a Weld Symbol
OTHER SIDE (above line)
ARROW SIDE (below line)
Size →6
△
50-200
← Length-Pitch
WPS-01
← Tail
↙ Arrow
1
Reference line
Horizontal baseline — all weld information
attaches to this line.
2
Arrow
Points to the joint; arrow side = below the
reference line; other side = above.
3
Weld type symbol
Sits on the reference line — below = arrow side;
above = other side.
4
Size
Left of symbol — leg size for fillets; depth of prep
for groove welds.
5
Length / Pitch
Right of symbol — length of each weld; pitch =
center-to-center spacing.
6
Tail
Fork at the opposite end — WPS number, process
designation, or notes.
Weld Type Symbols & Special Modifiers
△/ ▽
Fillet
T-joints and lap joints; most common weld type in structural fabrication.
∨
V-groove
Full-penetration butt weld; single V most common for plate; double V for
thick sections.
| |
Square groove
Full penetration in thin material without bevel preparation.
⌐∨
Bevel groove
One-sided access; one plate bevelled, the other left square.
∪
U-groove
Thick material — less weld volume than V-groove; more expensive prep.
○ / □
Plug / Slot
Weld through a hole or slot in the top piece into the piece beneath.
○ Weld all around ·
Field weld · G / M / C
⚑
Finish (grind/machine/chip) ·
Contour: flat / convex / concave

## Slide 13
Technician's Perspective
Welding is a quality-critical operation — the process, consumables, parameters, and thermal control are all specified for a
reason.
Red Flag: E7018 electrodes left out overnight — low-hydrogen status lost
A welder removes a fresh can of E7018 electrodes from the rod oven at end of shift and leaves them on the bench. Next morning they are used without
reconditioning. E7018 flux absorbs atmospheric moisture within hours — the 'low-hydrogen' designation is meaningless; hydrogen content in the deposited
weld metal is now equivalent to a standard electrode. On a high-CE structural steel this is a recipe for hydrogen-induced cold cracking in the HAZ, possibly
hours after the weld passes visual inspection. Reject the weld lot, recondition or discard the exposed electrodes, and document the non-conformance.
Caution: Preheat verified 30 minutes before welding — joint has since cooled
A welder preheats a thick plate joint to 150°C, confirmed by Tempilstik. Welding is delayed by 30 minutes while other work is completed. The joint has
cooled to ambient. The technician must require re-preheat and re-verification immediately before the arc is struck — per AWS D1.1 the temperature must
be present at the joint at the time of welding. A preheat reading taken earlier is not valid.
Good Practice: Using the weld symbol to verify the completed weld
A drawing calls for a 6 mm fillet weld, 50 mm long at 200 mm pitch, both sides of a T-joint. The technician locates the symbol on the reference line —
triangle below (arrow side) and above (other side), 6 to the left, 50-200 to the right. After welding, they measure the fillet leg with a weld gauge — finds 5
mm on the arrow side. This is undersize; an NCR is raised. Reading the symbol correctly is the foundation of all weld inspection.

## Slide 14
Core Question Answers
What is welding and how does it create a metallurgical bond?
A heat source melts the base metal edges and filler metal to form a weld pool — as it solidifies it creates a continuous metallic connection. The joint is a
continuation of the metal itself, not glued. Microstructure and mechanical properties are determined by the temperatures reached and the heating and cooling
rates — which is why controlling the thermal cycle is the foundation of welding quality.
What are the main arc welding processes and when is each used?
SMAW (stick): coated electrode, slag protection, portable and tolerant of wind/contamination — site work and maintenance. GMAW (MIG): continuous wire,
shielding gas, high deposition rate, automatable — manufacturing and fabrication. GTAW (TIG): non-consumable tungsten, highest quality, all materials — root
passes, stainless, aluminum, titanium. FCAW: flux-cored tubular wire, highest deposition rate, tolerant of mill scale — heavy structural fabrication.
How do filler metals work and how are they selected?
Filler melts into the weld pool and determines the as-welded composition, microstructure, and properties. Selected to match or overmatch base metal tensile
strength. AWS classification: prefix (E/ER) + tensile strength + position + flux/gas type. E7018 = low-hydrogen SMAW electrode, 70 ksi, all positions. ER308L = low-
carbon austenitic stainless GTAW/GMAW wire for 304L/316L. ER4043 = Al-Si filler for 6xxx aluminum.
What are preheat and interpass temperature and why are they quality-critical?
Preheat is the minimum base metal temperature before welding — slows cooling to prevent martensite formation and allow hydrogen to diffuse out, preventing
HIC. Required preheat determined by CE = C + Mn/6 + (Cr+Mo+V)/5 + (Ni+Cu)/15. Interpass minimum maintains preheat benefit between passes; interpass
maximum (250–300°C carbon steel, 150°C stainless) prevents grain coarsening and sensitization. Verified by Tempilstik or pyrometer immediately before welding.
How do you read a basic weld symbol?
Reference line is the horizontal baseline. Arrow points to the joint — symbols below the line apply to the arrow side, symbols above apply to the other side. Weld
type symbol sits on the reference line. Number left of symbol = weld size (leg for fillets, depth for grooves). Number right = length and pitch. Circle at arrow junction
= weld all around; flag = field weld. Tail specifies WPS number or process. Reading a symbol correctly is a non-negotiable inspection skill.

## Slide 15
Key Takeaways — Week 14: Welding Processes
1
The four main arc welding processes — SMAW, GMAW, GTAW, and FCAW — each occupy a distinct niche defined by portability,
productivity, quality, and base metal suitability; a technician must know not just what each process is but why it was specified for a
given application and what quality risks are associated with it.
2
Preheat and interpass temperature are not optional comfort measures — they are mathematically derived quality requirements
based on the carbon equivalent of the steel and the hydrogen level of the process; failing to achieve or maintain the specified
temperature is a non-conformance that must be documented and addressed before welding continues.
3
Reading weld symbols is a non-negotiable literacy skill for any technician working in fabrication or inspection — a symbol that is
misread means the wrong weld is made, and a wrong weld that passes inspection because the inspector did not check against the
symbol is a latent defect waiting to cause a failure.

## Slide 16
Resources & What's Next
Week 14 Resources
Kalpakjian Ch. 30 · Moniz Ch. 27
Fusion Welding Processes and Welding Metallurgy — primary reading
SMAW / GMAW / GTAW / FCAW Visualizers
Arc establishment, transfer modes, shielding gas selection — interactive
AWS D1.1 Structural Welding Code
Pre-qualified joints, filler metals, preheat, and inspection requirements
Weld Symbols — AWS A2.4
Complete standard for welding and NDT symbols — quick reference card
Preheat Calculator — Lincoln Electric
CE-based preheat recommendation by steel grade and section thickness
Week 15 — Weld Metallurgy & Failure
November 30, 2026 · Unit 5 continues
•
Weld microstructure — weld metal, CGHAZ, FGHAZ,
and their properties
•
Hydrogen-induced cracking — the three preconditions
and why it is delayed
•
Hot cracking — solidification cracking and crater cracks
•
Fracture types — ductile, brittle, and fatigue surface
features
•
Failure analysis methodology — preservation,
documentation, root cause