## Slide 1
M E C H 1 9 1 — M e t a l l u r g y
Week 15
Weld Metallurgy & Failure
November 30, 2026 · 5:00 – 7:30 PM · Kai Santos

## Slide 2
Class Agenda
01
Weld Metallurgy
Weld metal microstructure, HAZ sub-zones, and what the thermal cycle does to each region
02
Weld Cracking
Hot cracking, hydrogen-induced cold cracking, and lamellar tearing — mechanisms, conditions, and prevention
03
Fracture & Failure Analysis
Ductile, brittle, and fatigue fracture surfaces — and how a technician investigates a failed component

## Slide 3
Alloy Research Portfolio — Module 14
No Microscope Required
Module 14 · Week 15
Precipitation Hardening Comparison
What to do this week:
Research HV for 17-4PH stainless, then pull your logged 2024-T3 and
chromium-copper values to compare precipitation hardening across
three base metals — steel, aluminum, and copper.
Steps:
1 Research — record data & sources
2 Answer — short-answer questions
3 Apply — critical-thinking & equations
Alloys of Record
· Alloy F — 17-4PH stainless (revisit)
· Alloys J, O — 2024-T3 Al & chromium copper (revisit)
How to Complete This Module:
1 Research the alloy(s) using credible sources
2 Record data with a source citation
3 Answer the short-answer questions
4 Answer the critical-thinking questions
5 Keep the module with your portfolio
Portfolio Handout — Module 14

## Slide 4
MECH 191 — Course & Unit Roadmap
Unit 1
Materials Fundamentals
Unit 2
Steel & Alloys
Unit 3
Testing & Quality
Unit 4
Manufacturing
Unit 5
Joining & Failure
Wk 1
Aug 24
Atomic Structure
& Bonding
Wk 4
Sep 14
Carbon &
Alloy Steels
Wk 7
Oct 5
Mechanical
Testing
Wk 10
Oct 26
Casting
Wk 14
Nov 23
Welding
Processes
Wk 2
Aug 31
Mechanical
Properties
Wk 5
Sep 21
Stainless &
Cast Irons
Wk 8
Oct 12
NDT Methods
Wk 11
Nov 2
Forming
Wk 15 ← here
Nov 30
Weld Metallurgy
& Failure
Wk 6
Sep 28
Nonferrous &
Phase Diagrams
Wk 9
Oct 19
Quality
Standards
Wk 12
Nov 9
Machining
Wk 16
Dec 7
Corrosion
& Wrap-up
Wk 13
Nov 16
Powder
Metallurgy
Week 17 · FINAL EXAM

## Slide 5
Week 15 — At a Glance
Topics
Weld metal microstructure — columnar solidification, acicular ferrite,
allotriomorphic ferrite, bainite, and martensite
HAZ sub-zones — CGHAZ, FGHAZ, ICHAZ, SCHAZ: peak temperatures,
microstructures, and property implications
Hot cracking — solidification cracking and crater cracks: low-melting films, Mn:S
ratio, prevention
Hydrogen-induced cracking — three conditions, delayed nature, preheat, low-
hydrogen consumables, inspection timing
Lamellar tearing — through-thickness failure, MnS inclusions, Z-quality steel, UT
detection
Fracture types — ductile (dimples, cup-cone), brittle (chevrons, river marks),
fatigue (beach marks, striations)
Failure analysis — preserve, document, examine: the technician's role in root
cause investigation
Resources
Reference Material
Moniz Ch. 27 & Ch. 8 · Kalpakjian Ch. 32
Weld Metallurgy & Failure Analysis
Visualizers
Weld Microstructure & HAZ (Interactive)
Fracture Types & Surface Reading
Weld Cracking — Hot, Cold & Lamellar
SEM Fractography (Interactive)
Key Reference
ESAB Welding Metallurgy Handbook
ASM Vol. 11 — Failure Analysis
Lincoln Electric HIC & Preheat Guide
Next: Week 16 — Corrosion & Wrap-up

## Slide 6
Core Questions
Try to answer these before we dive in — we'll revisit them with answers at the end of class.
1
What are the metallurgical zones in a weld and what microstructure does each contain?
2
What is hydrogen-induced cracking and why is it the most dangerous welding defect?
3
What are the main fracture types and how do you identify them from the fracture surface?
4
How does a technician approach a failure analysis investigation?

## Slide 7
Weld Zones & Microstructure
Metallurgical Zones in Every Fusion Weld
Weld Metal
Fully molten region — solidifies as cast metal with columnar grains growing
from the fusion boundary toward the weld centerline. Composition = filler
metal + diluted base metal. Target microstructure in low-alloy steel: acicular
ferrite, for its combination of strength and toughness.
Heat-Affected Zone (HAZ)
Base metal heated above ~730°C but not melted — enough to alter its
microstructure. Subdivided into sub-zones by peak temperature. The most
metallurgically complex and most failure-prone region of any welded joint.
Unaffected Base Metal
Beyond the HAZ — original microstructure fully preserved. Properties match
the mill certificate. Serves as the reference baseline against which HAZ and
weld metal properties are compared.
Weld Metal Microstructure — Low-Alloy Steel
Solidification is epitaxial — grains nucleate at the fusion boundary and
continue the crystal orientation of the partially melted base metal grains.
Columnar grains grow perpendicular to the fusion boundary toward the weld
centerline, producing anisotropic properties.
Acicular ferrite
Fine, interlocking ferrite plates nucleating on non-metallic inclusions — the most
desirable microstructure. Deflects crack propagation and provides excellent
strength-toughness balance. Promoted by controlled oxygen content and inclusion
chemistry.
Allotriomorphic ferrite
Forms at prior austenite grain boundaries on cooling. Provides easy crack
propagation paths along boundaries — reduces toughness. Minimized by
composition and cooling rate control.
Bainite / Martensite
Form at higher cooling rates or in higher CE weld metals. Increase strength but
reduce toughness. Martensite in weld metal is generally undesirable and requires
tempering via PWHT.
Dilution by process: SMAW 20–30% · GMAW 25–35% · SAW 50–70%
The WPS specifies filler metal to account for dilution and achieve required weld
metal properties.

## Slide 8
Heat-Affected Zone — Sub-Zones & Critical Properties
HAZ Sub-Zones by Peak Temperature
CGHAZ >1100°C
Coarse-Grained HAZ — extensive austenite grain growth (5–10× base metal).
Cools to coarse upper bainite or martensite. Lowest toughness of any weld
zone. Primary site for hydrogen-induced cracking.
FGHAZ 900–1100°C
Fine-Grained HAZ — fully austenitised but insufficient time for grain growth.
Cools to a fine-grained microstructure. Typically the toughest region in the
entire weld.
ICHAZ 730–900°C
Intercritical HAZ — partially austenitised (between Ac1 and Ac3). Mixed
microstructure of transformed and untransformed regions. Can be a site for
localized softening in HSLA steels.
SCHAZ <730°C
Subcritical HAZ — no phase transformation. Tempering and stress relief only.
Properties approach base metal. Typically no toughness concern.
HAZ Width, Multi-Pass Welds & CGHAZ Risk
HAZ width
Determined by heat input and base metal thermal conductivity. Higher heat input
→ wider HAZ. Aluminum has higher thermal conductivity than steel → produces a
proportionally wider HAZ for the same heat input.
Multi-pass welds
Each subsequent pass reheats the HAZ of previous passes. The reheated CGHAZ
(now an ICHAZ of the prior pass) can be partially retransformed, refining the
coarse grain structure. Well-designed multi-pass procedures exploit this to
improve HAZ toughness.
Why CGHAZ is critical
The CGHAZ combines the worst of all factors: coarse grains reduce toughness;
martensite/bainite raise hardness; weld toe is a stress concentration; and this is
where hydrogen concentrates during cooling. All three HIC preconditions converge
here.

## Slide 9
Weld Cracking — Hot Cracking & Lamellar Tearing
Hot Cracking — Solidification Cracking
Mechanism
Liquid films at austenite grain boundaries cannot withstand tensile stress from
weld shrinkage during solidification. Most common in alloys with wide
solidification temperature ranges and high S or P content — these elements
concentrate in the last liquid to solidify and form low-melting films.
Appearance
Centerline cracks along the weld bead (solidification cracking) or open craters
at run ends (crater cracks). Crack surfaces are oxidized from exposure to the
arc environment at high temperature — a key distinction from cold cracking.
Prevention
Control S and P in base metal and filler; maintain Mn:S ratio >25:1 (Mn ties up
S as MnS with a higher melting point); use low crack-susceptibility filler
metals; fill craters properly at run ends; reduce restraint.
Detection
VT and PT for surface-breaking cracks; RT or UT for internal centerline cracks
that do not break the surface.
Lamellar Tearing
What it is
A base metal failure unique to welded joints — occurs in the through-thickness
direction of rolled plate under the transverse shrinkage stress of a fillet or T-joint
weld. It is not a weld defect — the weld itself may be perfectly sound.
Cause
Elongated MnS and silicate inclusions aligned parallel to the plate rolling surface
provide easy fracture paths under through-thickness tensile stress. Rolled plate
has much lower ductility in the through-thickness direction than in the rolling
plane.
Appearance
A stepped, terraced crack below and parallel to the fusion line, in the base metal
rather than the HAZ. The characteristic stepped morphology (tread-and-riser
pattern) is diagnostic — cracks run along inclusion planes and connect via short
through-thickness steps.
Prevention & Detection
Use low-sulfur steel (S <0.005%) with good through-thickness ductility (Z-quality
plate, tested by through-thickness tensile test — Z25 or Z35 grade). Redesign
joints to reduce through-thickness stress; use buttering passes. Detection: UT is
primary — characteristic subsurface location and morphology.

## Slide 10
Hydrogen-Induced Cracking (HIC) — Cold Cracking
HIC is uniquely dangerous because it is delayed — a weld that looks and tests sound immediately after completion can develop cracks hours to days
later.
1
Susceptible Microstructure
Hard martensite or coarse bainite in the CGHAZ —
formed when hardenable steel (high CE) cools
rapidly. The harder the microstructure, the more
susceptible to HIC. Controlled by preheat (slows
cooling) and keeping CE below critical thresholds.
2
Hydrogen Source
Atomic hydrogen generated in the welding arc
dissolves into the weld pool. Sources: moisture in
consumable flux/coating, base metal surface
contamination, humid atmosphere. E7018 low-
hydrogen electrodes must be stored in a heated
oven; use within 4 hours of removal.
3
Tensile Stress
Weld shrinkage stress and external restraint drive
hydrogen toward areas of high stress
concentration — typically the weld toe in the
CGHAZ. Higher restraint = greater risk. Minimize
by joint design, welding sequence, and
intermediate stress relief.
Mechanism: H diffuses to hard microstructure at high-stress sites → reduces cohesive strength → HIC initiates and grows. Prevention: Preheat + low-H
consumables + minimize restraint — all three must be controlled simultaneously. Detection timing: Inspect ≥24–48 h after welding on hardenable steels per AWS
D1.1.

## Slide 11
Fracture Types — Ductile & Brittle
Ductile Fracture
Mechanism
Microvoid coalescence (MVC) — voids nucleate at inclusions and second-
phase particles, grow under applied stress, and coalesce to form the fracture
surface.
Fracture surface
Dull, fibrous, gray appearance. Dimpled texture under SEM — each dimple
represents one coalesced void. Rough to the touch.
Macroscopic signs
Significant plastic deformation — necking in round specimens, distortion of
flat sections. Cup-and-cone profile in round bars (flat central zone + 45° shear
lip). The two halves do not fit back together cleanly.
Conditions that promote
High temperature, low strain rate, low strength, high toughness, small section
size (lower triaxiality). Most common failure mode in ductile metals at
ambient temperature under static overload.
Brittle Fracture
Mechanism
Cleavage — atoms separate along specific crystallographic planes with minimal
energy absorption. Grain boundaries may arrest cleavage cracks, causing short
intergranular segments between cleavage facets.
Fracture surface
Flat, bright, granular, crystalline appearance. Chevron marks (V-shaped ridges)
point back toward the fracture origin. River marks (fine lines on cleavage facets)
show crack propagation direction within each grain.
Macroscopic signs
No visible plastic deformation — the two fracture halves fit back together.
Fracture surface is perpendicular to the maximum tensile stress. Failure is sudden
and catastrophic with no warning.
Conditions that promote
Low temperature (below DBTT — ductile-to-brittle transition temperature), high
strain rate (impact loading), triaxial stress state (thick sections, notches), high-
strength/low-toughness microstructure.

## Slide 12
Fatigue Fracture — Reading the Fracture Surface
Initiation & Slow Crack Growth Zone
Initiation requires a stress concentration at or near the surface. Common
sites in welded components: weld toe, undercut, machining marks,
corrosion pits, or near-surface inclusions.
Beach marks (arrest marks)
Curved lines showing successive positions of the crack front — visible to the
naked eye. Form during crack arrest periods (rest, low load). Spacing increases
as the crack grows and stress intensity rises. The beach mark zone is the entire
slow crack growth region.
Striations
Microscopic ridges — one formed per load cycle, visible only under SEM.
Spacing equals crack growth per cycle and can be used to calculate how long
cracking was occurring. Parallel striations on a flat zone are the SEM signature
of fatigue.
Ratchet marks
Steps between multiple initiation sites — indicate high stress or multiple stress
concentrations. Each step is where two independent crack fronts have joined.
More ratchet marks = more severe stress concentration.
Overload Zone & Reading the Fracture
Final overload zone
Rough fast fracture at the opposite edge from initiation. Its proportion of the total
fracture area indicates applied stress: small fast zone = low stress, many cycles;
large fast zone = high stress, few cycles.
Reading the full story
Start at the initiation site (apex of the beach mark arc at the surface). Follow
beach marks outward as spacing increases. Locate the overload zone — its size
indicates stress level. Count ratchet marks for concentration severity.
Fatigue in weld toes
The weld toe is the most common initiation site — it combines geometric stress
concentration with tensile residual stress. Post-weld toe grinding, TIG dressing, or
peening remove the concentration and introduce compressive residual stress to
extend fatigue life.
Distinguishing from other modes
Fatigue: beach marks, smooth, surface-initiated. Brittle: chevrons, flat, crystalline,
no deformation. Ductile: dimpled, gray, plastic deformation. Fracture mode
identification is the first and most time-critical step of any investigation.

## Slide 13
Technician's Perspective
Weld metallurgy and fracture mechanics only matter when someone has to act on them — here is what that looks like in practice.
Red Flag: HIC found 72 hours after SMAW on high-CE structural steel — weld passed VT at completion
A welder completes a highly restrained structural connection on A514 steel (CE ≈ 0.55). Preheat was applied and verified at the start of the joint, but was not
maintained throughout a long multi-run sequence — the joint cooled between runs on a cool morning. VT immediately after welding shows no defects. 72 hours
later, MT reveals tight transverse cracks at the weld toes in the CGHAZ. Action: for high-CE steels, preheat is an interpass requirement, not just a starting condition;
maintain throughout the entire joint. Per AWS D1.1, final MT inspection must not be performed until at least 48 hours after completion of welding on any joint in a
high-CE steel.
Caution: Fatigue fracture at a crane boom weld toe — the weld meets the drawing, but the joint still fails
A crane boom fails in service after 3 years. The fracture surface shows clear beach marks initiating at a weld toe with a sharp profile and visible undercut. The weld
meets all dimensional requirements on the drawing. Root cause: the weld toe is a stress concentration — even a code-compliant weld toe creates a fatigue initiation
site under cyclic loading. No post-weld toe treatment was specified. Action: fatigue-critical welds require more than dimensional conformance; specify toe angle,
post-weld toe grinding or TIG dressing, and verify surface condition. Raise an NCR and an engineering review for the remaining joints.
Good Practice: Preserving the fracture surface — the difference between a defensible investigation and a dead end
A technician receives a failed shaft removed from service. Before doing anything else, they photograph the component in its as-found condition, bag each fracture
half separately in clean plastic, label with part number, date, and location found, and store in a dry environment. The fracture surface later reveals fatigue striations
under SEM with an initiation site at a machining mark. Preservation allowed the fractographic evidence to survive for definitive laboratory analysis. Action: never
clean, separate without care, or allow corrosion to develop on a fracture surface. The fracture is the primary evidence — treat it accordingly from the moment of
recovery.

## Slide 14
Core Question Answers
What are the metallurgical zones in a weld and what microstructure does each contain?
Three zones: Weld Metal (fully molten, solidifies to columnar grains; acicular ferrite is the target microstructure for toughness). HAZ (not melted but heat-altered,
subdivided into CGHAZ >1100°C with coarse grains/martensite/lowest toughness; FGHAZ 900-1100°C with fine grains/best toughness; ICHAZ partially transformed; SCHAZ
tempered only). Unaffected base metal beyond the HAZ retains original microstructure.
What is hydrogen-induced cracking and why is it the most dangerous welding defect?
HIC requires three simultaneous conditions: susceptible microstructure (martensite/bainite in CGHAZ), hydrogen (from consumables/moisture/atmosphere), and tensile
stress (weld shrinkage/restraint). Hydrogen dissolves in the arc and diffuses to high-stress hard microstructure regions, reducing cohesion. It is uniquely dangerous
because it is delayed — cracks develop hours to days after a weld passes VT. Prevention: preheat + low-hydrogen consumables + minimize restraint. Inspection timing: ≥48
h after welding on hardenable steels.
What are the main fracture types and how do you identify them from the fracture surface?
Ductile: dull, fibrous, gray, dimpled (SEM); cup-and-cone in round bars; significant deformation; halves don't fit back. Brittle: flat, bright, granular, crystalline; chevron
marks pointing to origin; river marks; no deformation; halves fit back; sudden failure. Fatigue: smooth beach mark zone (slow growth, visible to naked eye) + rough fast
fracture zone; striations under SEM; initiation at a surface stress concentration; ratchet marks if multiple initiation sites.
How does a technician approach a failure analysis investigation?
(1) Preserve — secure immediately; do not clean, separate carelessly, or allow further damage. (2) Document — photograph in as-found condition; record service history,
loading, environment, maintenance. (3) Visual examination — identify fracture type, locate initiation site, note crack path direction. (4) Non-destructive examination —
MT/PT for additional cracks; UT for subsurface; dimensional check. (5) Mechanical and metallographic testing — hardness survey, cross-section metallography, SEM
fractography. (6) Root cause and report — classify failure mode; identify root cause; recommend corrective action.

## Slide 15
Key Takeaways — Week 15: Weld Metallurgy & Failure
1
The HAZ is the most metallurgically complex and vulnerable region of any welded joint — understanding what happens to each sub-
zone during the thermal cycle explains why preheat, heat input control, and PWHT are specified, and why hydrogen cracking almost
always initiates in the coarse-grained HAZ rather than in the weld metal or the base metal.
2
Hydrogen-induced cracking is uniquely dangerous because it is delayed — a weld that looks and tests sound immediately after
completion can develop cracks hours or days later; for hardenable steels, inspection timing is a code requirement, not a convenience,
and a VT performed immediately after welding does not satisfy the requirement for a 48-hour hold.
3
The fracture surface is a record of how a component failed — ductile dimples, cleavage facets, beach marks, and striations each tell a
specific story; a technician who can read a fracture surface can identify the failure mode, locate the initiation site, and direct the
investigation toward the root cause before any laboratory testing is done.

## Slide 16
Resources & What's Next
Week 15 Resources
Moniz Ch. 27 & Ch. 8 · Kalpakjian Ch. 32
Welding Metallurgy and Failure Analysis — primary reading
Weld Microstructure & HAZ Visualizer
Interactive — zone boundaries, sub-zone microstructures, multi-pass effects
Fracture Types & Surface Reading
Interactive — ductile, brittle, and fatigue surface feature identification
Weld Cracking Types (Hot, Cold & Lamellar)
Interactive — mechanism, morphology, and prevention for each type
ESAB Welding Metallurgy Handbook
Primary reference for weld metal and HAZ microstructure
ASM Vol. 11 — Failure Analysis & Prevention
Standard reference for failure investigation methodology
Week 16 — Corrosion & Wrap-up
December 7, 2026 · Unit 5 concludes
Electrochemical corrosion — the four-element cell and how
to break it
Uniform, galvanic, pitting, crevice corrosion, and SCC
Protection methods — coatings, cathodic protection,
inhibitors
Material selection and design for corrosion resistance
Course wrap-up — key themes across all 5 units