## Slide 1
M E C H 1 9 1 — M e t a l l u r g y
Week 16
Corrosion & Course Wrap-up
December 7, 2026 · 5:00 – 7:30 PM · Kai Santos

## Slide 2
Class Agenda
01
Corrosion Fundamentals & Types
The electrochemical cell, uniform, galvanic, pitting, crevice, and stress corrosion cracking — mechanisms and recognition
02
Protection, Material Selection & Inspection
Coatings, cathodic protection, inhibitors, design decisions, and corrosion monitoring methods
03
Course Wrap-up
How the five units connect — from atomic structure to failure analysis — and what it means to be a metallurgy-literate
technician

## Slide 3
Alloy Research Portfolio — Module 15
No Microscope Required
Module 15 · Week 16
Course Capstone & Synthesis
What to do this week:
No new research this week — synthesize your notes from Modules 1–14
into the final capstone questions.
Steps:
1 Research — record data & sources
2 Answer — short-answer questions
3 Apply — critical-thinking & equations
Alloys of Record
· No new alloy — synthesis exercise
How to Complete This Module:
1 Research the alloy(s) using credible sources
2 Record data with a source citation
3 Answer the short-answer questions
4 Answer the critical-thinking questions
5 Keep the module with your portfolio
Portfolio Handout — Module 15

## Slide 4
MECH 191 — Course & Unit Roadmap
Unit 1
Materials Fundamentals
Unit 2
Steel & Alloys
Unit 3
Testing & Quality
Unit 4
Manufacturing
Unit 5
Joining & Failure
Wk 1
Aug 24
Atomic Structure
& Bonding
Wk 4
Sep 14
Carbon &
Alloy Steels
Wk 7
Oct 5
Mechanical
Testing
Wk 10
Oct 26
Casting
Wk 14
Nov 23
Welding
Processes
Wk 2
Aug 31
Mechanical
Properties
Wk 5
Sep 21
Stainless &
Cast Irons
Wk 8
Oct 12
NDT Methods
Wk 11
Nov 2
Forming
Wk 15
Nov 30
Weld Metallurgy
& Failure
Wk 6
Sep 28
Nonferrous &
Phase Diagrams
Wk 9
Oct 19
Quality
Standards
Wk 12
Nov 9
Machining
Wk 16 ← here
Dec 7
Corrosion
& Wrap-up
Wk 13
Nov 16
Powder
Metallurgy
Week 17 · FINAL EXAM · December 16, 2026

## Slide 5
Week 16 — At a Glance
Topics
Electrochemical corrosion — the four-element cell, galvanic series, and
passivation
Corrosion types — uniform, galvanic (area effect), pitting (PREN), crevice, SCC,
intergranular
Coatings — paint systems, surface preparation (Sa 2.5), hot-dip galvanizing,
thermal spray, anodizing
Cathodic protection — sacrificial anodes vs. impressed current, -0.85V criterion
per NACE SP0169
Design for corrosion — eliminate crevices, ensure drainage, isolate dissimilar
metals, control residual stress
Inspection & monitoring — UT thickness, pulsed eddy current for CUI, ER probes,
corrosion coupons
Course wrap-up — connecting the five units into a single integrated framework
Resources
Reference Material
Moniz Ch. 31
Corrosion
Reference Pages
Stainless Steel PREN — Grade Comparison
Corrosion Protection Guide — NACE / ISO 12944
ASM Vol. 13A — Corrosion Fundamentals
Standards
NACE SP0169 — CP Criteria
ISO 8501 — Surface Preparation
NACE MR0175 — H₂S Service
Final Exam · December 16, 2026
5:00 – 7:00 PM · Same location as class

## Slide 6
Core Questions
Try to answer these before we dive in — we'll revisit them with answers at the end of class.
1
What is corrosion and why is it thermodynamically driven?
2
What are the main types of corrosion and how is each recognized?
3
What protection methods are available and how do you choose between them?
4
How does material selection and design influence corrosion risk?

## Slide 7
Electrochemical Corrosion — The Cell & Passivation
The Four-Element Corrosion Cell
All four elements must be present simultaneously for electrochemical
corrosion to occur. Remove any one and the corrosion cell stops — this is
the basis of every protection strategy.
Anode (oxidation)
Metal atoms lose electrons and dissolve as ions: M → M²⁺ + 2e⁻. This is where
material loss occurs. The anode is the more active (less noble) metal or region.
Cathode (reduction)
Electrons arriving from the anode drive reduction. Alkaline/neutral: O₂ + 2H₂O
+ 4e⁻ → 4OH⁻. Acidic: 2H⁺ + 2e⁻ → H₂. No material loss at the cathode.
Electrolyte
Conducting liquid medium — water with dissolved salts, acids, or gases.
Conductivity increases with salt concentration and temperature. Seawater is
highly corrosive because of its high conductivity.
Metallic path
Electrical connection between anode and cathode — can be the metal itself
(different microstructural features or two metals in contact) or an external
conductor.
Galvanic Series & Passivation
Galvanic series
Metals ranked by electrochemical potential in seawater. More active (less
noble) metals are anodic and corrode preferentially when coupled to more
noble metals. Greater separation in the series = more severe galvanic attack.
Active (anodic) end
Magnesium → Zinc → Aluminum → Carbon steel
Mid-range
Cast iron → Lead → Tin → Copper alloys → Bronzes
Noble (cathodic) end
Stainless steel (passive) → Titanium → Gold → Platinum
Passivation
Some metals form a stable, adherent oxide that dramatically slows further
corrosion:
Stainless steel (Cr₂O₃) · Aluminum (Al₂O₃) · Titanium (TiO₂)
Passivity destroyed by: chloride ions, mechanical damage, or reducing conditions.
Once broken, the metal corrodes actively until the passive film can reform — if
ever.

## Slide 8
Corrosion Types — Uniform & Galvanic
Uniform (General) Corrosion
Mechanism
Anodic and cathodic reactions distributed uniformly across the surface — no
localization. The most predictable form of corrosion because the rate is
measurable and stable.
Recognition
Even surface loss, uniform scale or rust layer. Corrosion rate measured in
mm/year or mils per year (MPY) — allows remaining life calculations.
Design approach
Specify a material with a known corrosion rate for the environment, then add
a corrosion allowance to the wall thickness. Monitor with UT thickness
measurement at regular intervals throughout service life.
Examples
Rusting of unprotected carbon steel in atmosphere or soil. Acid attack on steel
in pickling baths. Uniform thinning of tank shells in process environments.
Galvanic Corrosion
Mechanism
Two dissimilar metals in electrical contact in an electrolyte — potential difference
drives current; the less noble metal (anode) corrodes at an accelerated rate while
the more noble metal (cathode) is protected.
Area effect — critical
Large cathode + small anode = severe attack; large anode + small cathode = mild.
Zinc on steel works: Zn is the large anode, exposed steel at scratches is a tiny
cathode. Never coat the anode only — any break creates a concentrated small-
anode attack.
Recognition
Concentrated corrosion on the less noble material, particularly near the junction
between the two metals. The more noble material shows little or no attack.
Prevention & Examples
Electrical isolation (non-conducting gaskets, sleeves); select metals close in
galvanic series; apply protective coating to the cathode. Examples: zinc anodes on
ship hulls; Al fittings on SS pipework; carbon steel fasteners in copper alloy
corroding rapidly.

## Slide 9
Corrosion Types — Pitting, Crevice & Stress Corrosion Cracking
Pitting & Crevice Corrosion
Pitting Corrosion
Local passive film breakdown → small anode surrounded by large passive
cathode → pit becomes self-sustaining. Metal ions accumulate inside the pit,
attracting Cl⁻, dropping pH, preventing repassivation. Recognition: discrete pits
on otherwise intact surface — depth concealed by thin corrosion product.
PREN = %Cr + 3.3×%Mo + 16×%N → higher = better pitting
resistance
304 (PREN ~19) · 316 (PREN ~24) · Duplex 2205 (PREN ~35–40)
Crevice Corrosion
Stagnant electrolyte in a tight gap (0.025–0.1 mm) depletes oxygen → interior
becomes anodic → metal ions accumulate, pH drops, Cl⁻ migrates in →
aggressive chemistry prevents repassivation. Recognition: damage
concentrated under gaskets, lap joints, bolt heads, and deposits.
Prevention: butt joints over lap joints; solid/PTFE-filled gaskets; continuous
rather than intermittent welds; higher PREN alloys; ensure drainage.
Stress Corrosion Cracking (SCC)
Mechanism
Tensile stress (residual or applied) + specific corrosive environment = cracking at
stresses far below yield strength. Involves anodic dissolution at crack tip and
hydrogen embrittlement. Crack propagates stably until the remaining cross-
section fractures by overload.
Critical material-environment pairs
Austenitic SS + chlorides. High-strength steel + H₂S (sulfide stress cracking — NACE
MR0175). Brass + ammonia (season cracking). Aluminum alloys + chlorides.
Titanium + methanol or red fuming nitric acid.
Recognition
Branching, intergranular or transgranular crack network. Minimal plastic
deformation. Brittle fracture surface with no beach marks — this is the key
distinction from fatigue. Branching is the most characteristic macroscopic feature
visible in the field.
Prevention & Detection
Stress relief (PWHT), shot peening for compressive RS. Select resistant alloys
(duplex SS for chlorides, low-alloy steel + PWHT for H₂S). Modify environment
(remove Cl⁻ or O₂; inhibitors; maintain pH >7). Detection: PT, ACFM through
coatings, UT for subsurface.

## Slide 10
Corrosion Protection — Coatings & Cathodic Protection
Protective Coatings
Organic paint systems
Three-coat system: zinc-rich primer (sacrificial — zinc corrodes to protect steel
even when scratched) + intermediate barrier coat + UV/abrasion-resistant
topcoat. Surface preparation is the single most important factor — blasting to
Sa 2.5 per ISO 8501. Holiday testing detects pinholes before commissioning.
Hot-dip galvanizing
Steel immersed in molten zinc at ~450°C — zinc metallurgically bonds through
a series of Fe-Zn alloy layers. Provides both barrier and sacrificial protection.
Zinc corrodes preferentially at scratches and cut edges. Service life 20–50
years in mild environments.
Thermal spray
Zinc or aluminum powder/wire melted and propelled onto the surface —
applied to large structures in situ (bridges, offshore structures). Thicker than
electroplating; can be applied without immersion.
Anodizing & conversion coatings
Anodizing thickens the oxide on aluminum electrochemically — improves
corrosion and wear resistance. Phosphating provides paint-adhesion base for
automotive steel. Chromate conversion being phased out (toxicity); trivalent
alternatives increasingly specified.
Cathodic Protection & Inhibitors
Cathodic protection (CP)
Makes the structure the cathode of an electrochemical cell — corrosion only
occurs at anodes.
Sacrificial anode CP
Zn, Mg, or Al anode connected to the structure — the anode corrodes
preferentially. Passive, no power required, self-regulating. Ship hulls, buried
pipelines, tank floors. Anodes must be inspected and replaced periodically.
Impressed current CP (ICCP)
DC power source drives current from inert anode (graphite, MMO) onto the
structure. Controllable and suitable for large installations. Buried/submerged
pipelines, storage tanks, reinforced concrete. Requires monitoring — power
supply failure leaves structure unprotected.
CP criterion (NACE SP0169): −0.85 V vs. Cu/CuSO₄ reference electrode
Inhibitors
Anodic (form anode film — risk if under-dosed) · Cathodic (reduce cathodic rate —
safer under-dosed) · Mixed (act on both — cooling water, pipelines, preservation
fluids).

## Slide 11
Design, Material Selection & Corrosion Inspection
Design & Material Selection
Material selection is the most permanent defense — an inherently
resistant alloy requires no maintenance and won't fail if the protection
system is damaged.
Joint design
Butt joints preferred over lap joints — lap joints create crevices. Continuous
welds instead of intermittent welds seal gaps. Full-penetration seal welds at
tube-to-tubesheet joints eliminate the crevice between tube OD and bore.
Drainage & surface finish
Slope surfaces so water drains — horizontal surfaces that pool water corrode
faster. Smooth surfaces are more corrosion resistant than rough (rough
surfaces trap moisture and contamination). Smooth machined keyways +
polished fillets reduce both corrosion and fatigue initiation.
Dissimilar metal isolation
Electrically isolate dissimilar metals with non-conducting gaskets, sleeves, and
washers. If isolation is impractical, select metals close together in the galvanic
series or ensure the less noble material has a much larger area than the more
noble.
Residual stress control
Tensile residual stress from welding or machining accelerates SCC. PWHT for
stress relief. Shot peening introduces compressive residual stress at the
surface — a common SCC and fatigue prevention measure for welded joints
and keyways.
Corrosion Inspection & Monitoring
Visual inspection
First step — rust staining, discoloration, paint blistering, pitting, deposits, and
scaling. Requires adequate lighting, access, and mirrors or borescopes for
confined spaces.
UT thickness measurement
Primary method for measuring remaining wall thickness in corroded piping,
vessels, and structural members — from one side without internal access. Results
compared to minimum acceptable thickness (fitness for service).
Corrosion Under Insulation (CUI)
Corrosion hidden beneath insulation — cannot be seen without stripping. Pulsed
eddy current (PEC) and radiographic profile techniques screen through insulation
without removal. A significant inspection challenge in process plant.
Monitoring — rate measurement
ER probes and LPR probes: real-time corrosion rate in process pipelines and
vessels. Corrosion coupons: pre-weighed metal samples exposed for a defined
period — direct weight loss measurement. Used to verify inhibitor programs and
detect changes in process chemistry.

## Slide 12
Course Wrap-Up — How the Five Units Connect
These are not five separate subjects. They form a single chain — each unit explains why the next one matters.
Unit 1 — Materials Fundamentals
Aug 24 – Sep 7
Atomic bonding explains conductivity and electrochemical corrosion. Crystal structure determines slip systems, deformation
behavior, and SCC crack paths. Grain boundaries are sites of sensitization, intergranular corrosion, and hydrogen trapping.
Unit 2 — Steel & Alloys
Sep 14 – Sep 28
Carbon equivalent drives preheat requirement and determines HIC susceptibility. Stainless grade determines pitting (PREN)
and SCC resistance. Heat treatment condition sets HAZ hardenability — the microstructure that either resists or fails in service.
Unit 3 — Testing, Inspection & Quality
Oct 5 – Oct 19
NDT methods detect the defects that Unit 2's microstructure makes and Unit 4's processes create. Hardness testing verifies
heat treatment. Inspection documentation creates the traceability that makes a failure investigation possible.
Unit 4 — Manufacturing Processes
Oct 26 – Nov 16
Casting defects provide corrosion and fatigue initiation sites. Forming introduces residual stress that drives SCC. Machining
quality determines surface finish and residual stress state — the foundation for fatigue life in service.
Unit 5 — Joining, Failure & Corrosion
Nov 23 – Dec 7
The weld HAZ is a microstructure gradient each zone with different corrosion resistance. Residual weld stress drives SCC.
Failure analysis connects all previous units — explaining why a component failed and feeding that knowledge back into design,
material selection, and inspection.

## Slide 13
Technician's Perspective
Corrosion type identification in the field — what the technician sees and what it means.
Red Flag: Leak at 304 SS tube-to-tubesheet joint in seawater heat exchanger — 14 months in service
Inspection reveals three overlapping corrosion mechanisms: (1) Galvanic — carbon steel tubesheet is anodic to stainless tubes; unfavorable area ratio (small
anode/large cathode) drives accelerated attack at the tubesheet. (2) Crevice — the tight gap between tube OD and tubesheet bore in stagnant seawater depletes
O₂, drops pH, concentrates Cl⁻ — classic crevice geometry. (3) Sensitization — if standard 304 (not 304L) was used without interpass temperature control, chromium
carbide precipitation in the HAZ depletes Cr below the passivity threshold. Action: specify 304L or duplex 2205 for seawater; specify full-strength seal welds to
eliminate the crevice; apply sacrificial zinc anodes to the carbon steel tubesheet; add to failure investigation as a multi-mechanism case study.
Caution: Branching cracks at weld toes on austenitic stainless pressure vessel in chloride service
VT finds tight, branching cracks running from weld toes. No beach marks on the fracture surface (distinguishing SCC from fatigue). No plastic deformation.
Metallographic sections show transgranular cracking with fine branching — the textbook appearance of chloride SCC in austenitic stainless. Root cause: tensile weld
residual stress + chloride from insulation + elevated temperature. Action: PWHT for stress relief (not always possible on austenitic SS — sensitization risk); shot peen
weld toes; review insulation specification (chloride-free insulation required per NACE for SS service); consider upgrade to duplex stainless or super-austenitic for
remaining vessels in the same service.
Good Practice: Holiday testing a coating before cathodic protection commissioning — finding the pinhole that prevents a concentrated attack
A newly coated pipeline section is holiday tested before backfilling using a high-voltage spark tester. A pinhole is found at a fitting where the coating was not fully
sealed. The pinhole is repaired and retested. Without the repair, the pinhole under CP would have created a small anode/large cathodically protected cathode
situation — concentrating the full galvanic driving force at a single point and producing rapid localized attack. Action: holiday testing is a mandatory step before
burying or commissioning any cathodically protected coated structure; document all findings and repairs; retest after each repair until the coating is holiday-free.

## Slide 14
Core Question Answers
What is corrosion and why is it thermodynamically driven?
Corrosion is the degradation of a metal through chemical or electrochemical reaction with its environment. It is thermodynamically driven because most metals exist
naturally as ores (lower energy state) — refining requires energy input, and corrosion is the metal releasing that energy and returning toward its natural state.
Electrochemical corrosion requires four elements simultaneously: anode, cathode, electrolyte, and metallic path. Remove any one element and corrosion stops.
What are the main types of corrosion and how is each recognized?
Uniform: even surface loss, predictable rate. Galvanic: concentrated attack on the less noble metal at a dissimilar metal junction. Pitting: discrete pits on otherwise intact
surface — depth concealed by corrosion product; driven by local passive film breakdown and Cl⁻ concentration; PREN quantifies resistance. Crevice: damage under
gaskets, lap joints, deposits — stagnant O₂-depleted chemistry. SCC: branching, intergranular/transgranular cracks with no beach marks, no plastic deformation, driven by
tensile stress + specific environment.
What protection methods are available and how do you choose between them?
Coatings (barrier and sacrificial) + surface prep is #1 factor. Hot-dip galvanizing for structural steel: barrier + sacrificial, 20–50 yr life. Cathodic protection: sacrificial anodes
(passive, ships/pipelines) or ICCP (controllable, large structures). Inhibitors: anodic (risk if under-dosed), cathodic (safer). Material selection: most permanent — match
PREN, CE, and alloy to the specific environment. Design: eliminate crevices, ensure drainage, isolate dissimilar metals, control residual stress. Most effective systems
combine multiple methods.
How does material selection and design influence corrosion risk?
Material selection must match the specific corrosion mechanism — 304 SS resists uniform attack but fails in Cl⁻ pitting; copper is excellent in freshwater but fails in
ammonia. PREN guides stainless selection for chloride service. CE and alloy composition determine weldability and HAZ hardenability. Design decisions: butt joints over lap
joints (no crevice); sloped surfaces for drainage; non-conducting isolation for dissimilar metals; smooth surface finish; PWHT and shot peening to control residual stress
and prevent SCC.

## Slide 15
Key Takeaways — Week 16: Corrosion & Course Wrap-up
1
Corrosion is thermodynamically inevitable — the goal is not to prevent it absolutely but to understand the specific mechanism
operating in a given material-environment combination, slow the rate to an acceptable level, detect it early, and design structures with
enough allowance and protection to achieve the required service life.
2
Every corrosion type has a characteristic appearance that allows a technician to identify it in the field — uniform surface loss, galvanic
concentration at dissimilar metal junctions, discrete pitting, crevice location under gaskets and deposits, SCC branching — recognition is
the first step toward prevention and remediation.
3
The five units of this course are not separate subjects but a single interconnected body of knowledge — atomic structure determines
properties, properties determine material selection, processing determines microstructure, microstructure determines performance,
and inspection and failure analysis close the loop; a technician who understands these connections is not just a procedure-follower but
a problem-solver.

## Slide 16
Resources & Final Exam
Week 16 Resources
Moniz Ch. 31
Corrosion and Its Prevention — primary reading
Stainless Steel PREN — Grade Comparison Table
Service environment guide for stainless alloy selection
Corrosion Protection Guide — NACE / ISO 12944 / ASM 13A
Coating selection, surface preparation, and cathodic protection
NACE SP0169
Standard for cathodic protection of buried pipelines — CP criteria
NACE MR0175 / ISO 15156
Material requirements for H₂S service (sour service)
ASM Vol. 13A — Corrosion Fundamentals
Primary reference for corrosion mechanisms and materials selection
Final Exam
Week 17 · December 16, 2026
5:00 PM – 7:00 PM · Same classroom
Exam covers all 5 units:
Unit 1 — Atomic structure, bonding, mechanical properties
Unit 2 — Steel families, heat treatment, phase diagrams
Unit 3 — NDT methods, mechanical testing, quality standards
Unit 4 — Casting, forming, machining, powder metallurgy
Unit 5 — Welding, weld metallurgy, fracture, corrosion
Exams must be returned by 7:00 PM to be graded.