## Slide 1
M E C H 1 9 1 — M e t a l l u r g y
Week 2
Mechanical Properties & Behavior
August 31, 2026 · 5:00 – 7:30 PM · Kai Santos

## Slide 2
Class Agenda
01
Stress & Strain
The fundamental language for describing how metals respond to force
02
Crystal Defects
Point, line, planar, and volume defects — and why they matter more than you'd expect
03
Grain Boundaries & Diffusion
How boundaries strengthen metal, the Hall-Petch relationship, and how atoms move through solid
metal

## Slide 3
Alloy Research Portfolio — Module 2
No Microscope Required
Module 2 · Week 2
Mechanical Properties
What to do this week:
Research 1018 vs. 1045 steel: composition, published hardness, and
expected pearlite content — then apply the Vickers HV formula.
Steps:
1 Research — record data & sources
2 Answer — short-answer questions
3 Apply — critical-thinking & equations
Alloys of Record
· Alloy A — 1018 steel (normalized)
· Alloy B — 1045 steel (normalized)
How to Complete This Module:
1 Research the alloy(s) using credible sources
2 Record data with a source citation
3 Answer the short-answer questions
4 Answer the critical-thinking questions
5 Keep the module with your portfolio
Portfolio Handout — Module 2

## Slide 4
MECH 191 — Course & Unit Roadmap
Unit 1
Materials Fundamentals
Wk 1
Aug 24
Atomic Structure
& Bonding
Wk 2 ← here
Aug 31
Mechanical
Properties
Unit 2
Steel & Alloys
Wk 4
Sep 14
Carbon &
Alloy Steels
Wk 5
Sep 21
Stainless &
Cast Irons
Wk 6
Sep 28
Nonferrous &
Phase Diagrams
Unit 3
Testing & Quality
Wk 7
Oct 5
Mechanical
Testing
Wk 8
Oct 12
NDT Methods
Wk 9
Oct 19
Quality
Standards
Unit 4
Manufacturing
Wk 10
Oct 26
Casting
Wk 11
Nov 2
Forming
Wk 12
Nov 9
Machining
Wk 13
Nov 16
Powder
Metallurgy
Unit 5
Joining & Failure
Wk 14
Nov 23
Welding
Processes
Wk 15
Nov 30
Weld Metallurgy
& Failure
Wk 16
Dec 7
Corrosion
& Wrap-up
Week 17 · FINAL EXAM

## Slide 5
Week 2 — At a Glance
Topics
•
Stress and strain — the language of mechanical behavior
•
Elastic vs. plastic deformation and the yield point
•
Key properties: strength, hardness, ductility, toughness,
brittleness
•
Crystal defects — point, line, planar, and volume
•
Grain boundaries — formation, energy, and the Hall-Petch
effect
•
Diffusion — how atoms move through solid metal
Resources
Reference Material
Moniz 5th — Ch. 3
Mechanical Properties of Metals
Kalpakjian 6th — Ch. 2
Fundamentals of Mechanical
Behavior of Materials
Visualizers
•
Stress-Strain Curve (Interactive)
•
Hot vs Cold Working & Work
Hardening

## Slide 6
Core Questions
Try to answer these before we dive in — we'll revisit them with answers at the end of class.
1
What is the difference between strength and toughness? Can a material be strong but not tough?
2
At the atomic level, what exactly happens at the yield point when you pull a metal specimen in tension?
3
Cold-working a metal (rolling, drawing) increases its strength but reduces ductility. What microstructural change
explains both effects simultaneously?
4
A fine-grained and a coarse-grained steel have identical composition. Which yields at higher stress — and why?
5
A steel shaft fails well below its yield strength after thousands of rotation cycles. What failure mode is this, and
what property should have been checked?

## Slide 7
Stress and Strain — The Language
When a force is applied to a metal, we need precise language to describe what happens inside it — at the
grain level and at the atomic level.
Stress (σ)
σ = F / A
Internal force per unit area — the pressure the atoms
inside the material experience when an external load is
applied.
Types of stress:
Tensile — pulling apart (positive σ)
Compressive — pushing together (negative σ)
Shear — sliding one plane over another (τ)
Units: Pa, MPa, ksi
Strain (ε)
ε = ΔL / L₀
The amount of deformation relative to original size —
how much the material has stretched or compressed
under load.
Key points:
Dimensionless — or expressed as %
Ductility is reported as % elongation at fracture
Strain rate matters — fast loading vs. slow loading
Dimensionless — expressed as mm/mm, in/in, or %

## Slide 8
Elastic vs. Plastic Deformation
Elastic Zone
The material deforms under load but
returns to its original shape when the
load is removed — like a spring. Atoms
are displaced but not permanently
rearranged. The bonds stretch, then
pull back.
Example:
Spring, tight bolt that can still be
removed, a bent ruler that snaps back
Yield Point
The critical transition stress — above
this, deformation becomes
permanent. Atoms and dislocations
have moved too far to recover. This is
the most important value in material
selection for structural design.
Example:
The 'click' when a bolt is overtightened
— it won't come back to correct preload
Plastic Zone
Permanent deformation — the
material will not spring back.
Dislocations are moving through the
crystal, allowing shape change without
fracture. The material flows,
distributing stress.
Example:
Bent paperclip, cold-formed bracket,
stamped sheet metal door panel
Ultimate Tensile Strength (UTS): the maximum stress the material can handle before fracture — the peak of the stress-strain curve,
past the yield point.

## Slide 9
Key Mechanical Properties
These five properties are how engineers describe and compare materials — you will encounter all of them in
specifications, data sheets, and test reports.
σ
Strength
Maximum stress a
material can handle
before yielding (yield
strength) or fracturing
(UTS). Higher = harder to
permanently deform or
break.
How tested:
Tensile test, compression
test
H
Hardness
Resistance of the surface
to indentation or
scratching. Directly
related to yield strength
— harder materials
resist surface
deformation.
How tested:
Rockwell, Brinell, Vickers
%
Ductility
How much plastic
deformation a material
can tolerate before
fracturing. Reported as
% elongation. Essential
for forming operations.
How tested:
% elongation, % area
reduction
J
Toughness
Energy absorbed before
fracture — the area
under the stress-strain
curve. High toughness =
survives impacts.
Requires both strength
and ductility.
How tested:
Charpy, Izod impact tests
✗
Brittleness
Fractures with little or
no plastic deformation.
Brittle materials can be
very strong but fail
suddenly with no
warning. The opposite of
toughness.
How tested:
Observed at the fracture
surface

## Slide 10
Crystal Defects — Point Defects
No real metal is perfect — defects exist at every scale. Point defects are disruptions at a single lattice site. Every cubic
centimeter of real metal contains millions.
Vacancy
A missing atom — an empty site where
an atom should be. The most common
point defect in all metals. Number
increases exponentially with
temperature.
Why it matters:
Enable atom movement (diffusion).
Essential for heat treatment, annealing,
and solid-state reactions.
One missing atom out of billions — but millions
of them create measurable softening and
diffusion pathways.
Interstitial Defect
An extra atom squeezed into a gap
between host atoms. If the same
element: self-interstitial. If a smaller
foreign element: interstitial alloy.
Why it matters:
Carbon in iron is an interstitial defect —
even tiny amounts dramatically harden
steel by blocking dislocation movement.
This is exactly what we covered in Week 1 — the
mechanism behind carbon steels.
Substitutional Defect
A wrong atom sitting in a lattice site,
replacing a host atom. Works best when
the substitute is within ~15% in size and
has similar valence electrons.
Why it matters:
Cr, Ni, Mo in steel are all substitutional —
this is how stainless steel and alloy steels
are made.
Same mechanism as substitutional solid
solutions from Week 1.

## Slide 11
Crystal Defects — Line Defects (Dislocations)
Core question:
If dislocations make metals easier to deform, why don’t we want to eliminate them? A metal with zero dislocations would
need enormous stress to deform at all, then fracture suddenly with no warning — like glass.
Edge Dislocation
An extra half-plane of atoms inserted into
the lattice — like forcing an extra card
into a deck halfway through. The
distortion runs along the edge of this
extra plane.
Burgers vector (b): perpendicular to the
dislocation line
Like a wrinkle in a rug — slide the wrinkle
across instead of lifting the whole rug at
once
Screw Dislocation
A helical distortion of the lattice —
atomic planes spiral around the
dislocation line like a corkscrew. Can
cross-slip between slip planes, giving
more paths to deform.
Burgers vector (b): parallel to the dislocation
line
Like tearing paper by sliding the two halves
sideways rather than pulling them apart
Mixed Dislocation
In practice, most dislocations are a
mixture of edge and screw character —
the Burgers vector is at an angle. Pure
edge or pure screw are rarely found in
real metals.
Burgers vector: at an angle — has both edge
and screw components
Real metal dislocations wind and curve
through the crystal in complex three-
dimensional paths

## Slide 12
Crystal Defects — Planar Defects
Two-dimensional surfaces where crystal structure or orientation changes — grain boundaries are the most
common and most important.
Grain Boundaries
The most common planar defect. When independently
nucleating crystals grow into each other during solidification,
the orientation mismatch creates a disordered boundary
region.
•
High misorientation (>15°): high disorder, high energy,
more reactive to corrosion and diffusion
•
Low misorientation (<15°): tilt or twist boundary — more
structured, lower energy
Twin Boundaries
A boundary where the crystal on each side is a perfect mirror
image of the other — extremely low energy and very stable.
Two types with different origins:
•
Annealing twins: form during recrystallization of FCC
metals (Cu, Al, austenitic stainless steel)
•
Deformation twins: form under shock loading or low-
temperature plastic deformation — common in HCP and
BCC
Stacking Faults
A disruption in the normal atomic stacking sequence — FCC follows ABCABC… and HCP follows ABAB…; a fault breaks this pattern.
Low Stacking Fault Energy (SFE) → wide stable faults → dislocations can’t cross-slip → the metal work-hardens quickly. High SFE →
narrow faults → easy cross-slip → softer cold-working behavior.

## Slide 13
Crystal Defects — Volume Defects
Three-dimensional imperfections large enough to detect with inspection equipment. These are the defects
that cause failures in service.
Voids & Porosity
Empty spaces trapped during
solidification.
•
Gas porosity: dissolved
gases escape as metal
solidifies — spherical
voids
•
Shrinkage porosity:
metal contracts while
cooling without enough
feed metal — irregular
voids
Stress concentrators that reduce
fatigue life. Detected by
radiography (X-ray, CT scan).
Inclusions
Non-metallic particles (oxides,
sulfides, silicates) trapped
inside the metal during
melting.
•
Disrupt metal continuity
throughout
•
Common initiation sites
for fatigue cracks in
service
Managed by vacuum melting,
good melt practice, and clean
steel processing standards.
Cracks
Planar separations within the
metal — the most dangerous
defect class.
•
Hot cracks: form at grain
boundaries during
solidification
•
Cold cracks: form during
cooling, heat treatment,
or in service (fatigue,
stress corrosion)
Stress concentrators that grow
rapidly under cyclic load.
Detected by dye penetrant,
magnetic particle, UT, or
radiography.
Delaminations &
Segregation
Two structural defect types:
•
Delaminations:
separation between
rolled/forged layers
from elongated
inclusions — detected
by UT
•
Segregation: uneven
distribution of alloying
elements from
solidification — causes
localized hardness and
corrosion resistance
variations
Both require careful process
control and systematic inspection
during manufacturing.

## Slide 14
Grain Boundaries — Strengthening and Growth
Grain boundaries are high-energy regions that actively control strength, toughness, corrosion, and diffusion
— not just where grains meet.
The Hall-Petch Relationship
σᵧ = σ₀ + k / √d
Yield strength increases as grain size (d) decreases — smaller grains
mean more boundaries, and dislocations pile up sooner.
•
When a dislocation reaches a grain boundary, it cannot cross —
orientation mismatch blocks it
•
Dislocations pile up, creating a back-stress that resists further
deformation
•
Smaller grain = shorter distance before hitting a boundary =
more pile-ups = stronger
•
One of the most powerful and practical strengthening tools in
metallurgy
Grain Growth in Annealing
1. Recovery
Internal stresses relieved, no major
microstructure change. Metal softens slightly but
retains deformed grain shape.
2. Recrystallization
New strain-free grains nucleate and replace
deformed grains. Strength drops, ductility fully
recovers.
3. Grain Growth
New grains coarsen as boundaries migrate to
reduce total energy. Control time and
temperature to reach target grain size.

## Slide 15
Diffusion — Atoms in Motion
Even in solid metal, atoms are not perfectly still — they vibrate constantly, and at elevated temperatures
they have enough energy to jump between sites.
Substitutional Diffusion
Larger atoms move by jumping into neighboring vacancies
— hopping from one lattice site to an adjacent empty one.
Requires: a nearby vacancy AND enough thermal energy to
squeeze through the gap between atoms.
Rate: Slow — vacancies are relatively rare and large atoms must
squeeze between others.
Example: Alloying additions spreading through steel: Cr, Ni, Mo
homogenization during annealing
Interstitial Diffusion
Small atoms move through the gaps between host atoms
without displacing them — flowing through the interstitial
network.
No vacancy required — gaps are everywhere, so this is
much faster than substitutional diffusion.
Rate: Fast — gaps are abundant, and small atoms can move
easily even at lower temperatures.
Example: Carbon in iron (carburizing, case hardening),
nitrogen in steel (nitriding)
Temperature Effect:
Diffusion rate increases exponentially with temperature — a small temperature rise causes a
dramatic increase in atom movement. This is why heat treatment temperatures must be
controlled precisely.

## Slide 16
Core Questions — Answers
1
What is the difference between strength and toughness?
Strength is the peak stress before yielding or fracture. Toughness is total energy absorbed — the area under the stress-
strain curve. A material can be strong but brittle (high-carbon steel, glass): high peak stress, negligible plastic zone,
low toughness.
2
What happens at the yield point at the atomic level?
Dislocations overcome their pinning obstacles and begin moving irreversibly through the crystal. Below yield, bonds
stretch elastically and recover. At yield, atomic planes shift permanently — plastic deformation begins and cannot be
undone by removing the load.
3
Why does cold work increase strength AND reduce ductility simultaneously?
Cold work multiplies dislocation density enormously. Dislocations tangle and block each other — work hardening —
requiring more stress to continue deformation (higher strength). But with so many dislocations already present, little
capacity for further plastic flow remains (lower ductility).
4
Fine-grained vs. coarse-grained steel: which is stronger and why?
Fine-grained. Hall-Petch: σ_y = σ_0 + k/√d. More grain boundaries per unit volume block dislocation movement at
each boundary — each crossing requires additional stress. Finer grains = more barriers = higher yield strength.
5
Shaft fails below yield strength under cyclic loading. What is it?
Fatigue failure. Cyclic loading initiates tiny cracks at stress concentrations (surface defects, notches) that grow with
each cycle until catastrophic fracture — often well below the static yield strength. The relevant property is the
endurance limit.

## Slide 17
Key Takeaways
1
Stress and strain are the engineer’s language
Stress (σ = F/A) is internal force per area. Strain (ε = ΔL/L₀) is deformation relative to original size. The yield point — the
elastic-to-plastic transition — is the most important value in structural material selection.
2
Defects are features, not failures
Point, line, planar, and volume defects each affect metal differently. Dislocations enable ductility — eliminate them and the
metal becomes brittle. Real engineering metals are defined by their defect structure.
3
Grain size is the most practical lever
Hall-Petch: σᵧ = σ₀ + k/√d — making grains smaller makes metal stronger. Grain size is controlled through alloy additions and
thermal processing (annealing temperature and time).
4
Diffusion drives heat treatment
Atoms move through solids at rates exponential with temperature. Carburizing, nitriding, and homogenization all rely on
controlled diffusion — this is why heat treatment temperatures are precise.
5
Safety is not optional!
PPE is mandatory in the shop — no exceptions. We work with heat, sharp edges, and hazardous materials every lab session.
Protect yourself and your classmates.

## Slide 18
Resources & What's Next
Week 2 Resources
•
Moniz Ch. 3 — Mechanical Properties of Metals
•
Kalpakjian Ch. 2 — Fundamentals of Mechanical
Behavior of Materials
Visualizers
•
Stress-Strain Curve (Interactive)
•
Hot vs Cold Working & Work Hardening (Interactive)
Coming Up — Week 4
Carbon & Alloy Steels
•
Week 3 is Labor Day — no class
•
Iron vs. steel — what carbon does to the lattice
•
AISI/SAE four-digit classification system
•
Plain carbon vs. alloy steel grades and alloying
elements
Unit 1 Quiz covers Weeks 1 – 2 · Review bonding, crystal structures, and the stress-strain curvees