## Slide 1
M E C H 1 9 1 — M e t a l l u r g y
Week 4
Carbon & Alloy Steels
September 14, 2026 · 5:00 – 7:30 PM · Kai Santos

## Slide 2
Class Agenda
01
Steel Fundamentals
What steel is, why it matters, and how carbon controls everything
02
AISI/SAE Classification
How to read and use the four-digit steel designation code
03
Alloy Steels & Heat Treatment
Alloying elements, alloy steel families, CCT diagrams, and heat treatment processes

## Slide 3
Alloy Research Portfolio — Module 3
No Microscope Required
Module 3 · Week 4
Carbon & Alloy Steels
What to do this week:
Research 1018, 1045, and 1075 steel: composition and published hardness
across the carbon range, then apply the lever rule.
Steps:
1 Research — record data & sources
2 Answer — short-answer questions
3 Apply — critical-thinking & equations
Alloys of Record
· Alloy A — 1018 steel
· Alloy B — 1045 steel
· Alloy C — 1075 steel
How to Complete This Module:
1 Research the alloy(s) using credible sources
2 Record data with a source citation
3 Answer the short-answer questions
4 Answer the critical-thinking questions
5 Keep the module with your portfolio
Portfolio Handout — Module 3

## Slide 4
MECH 191 — Course & Unit Roadmap
Unit 1
Materials Fundamentals
Wk 1
Aug 24
Atomic Structure
& Bonding
Wk 2
Aug 31
Mechanical
Properties
Unit 2
Steel & Alloys
Wk 4 ← here
Sep 14
Carbon &
Alloy Steels
Wk 5
Sep 21
Stainless &
Cast Irons
Wk 6
Sep 28
Nonferrous &
Phase Diagrams
Unit 3
Testing & Quality
Wk 7
Oct 5
Mechanical
Testing
Wk 8
Oct 12
NDT Methods
Wk 9
Oct 19
Quality
Standards
Unit 4
Manufacturing
Wk 10
Oct 26
Casting
Wk 11
Nov 2
Forming
Wk 12
Nov 9
Machining
Wk 13
Nov 16
Powder
Metallurgy
Unit 5
Joining & Failure
Wk 14
Nov 23
Welding
Processes
Wk 15
Nov 30
Weld Metallurgy
& Failure
Wk 16
Dec 7
Corrosion
& Wrap-up
Week 17 · FINAL EXAM

## Slide 5
Week 4 — At a Glance
Topics
•
Iron and steel — the difference carbon makes
•
How carbon content controls strength, ductility, and weldability
•
The carbon content spectrum: pure iron → low → medium →
high carbon → cast iron
•
AISI/SAE four-digit classification system
•
Plain carbon steel grades and their applications
•
Alloying elements (Mn, Cr, Ni, Mo, V, Si) and their effects
•
When and why to specify an alloy steel over plain carbon
Resources
Reference Material
Moniz 5th — Ch. 11, 12 & 14
Iron & Steel / Carbon Steels / Heat Treatment
Kalpakjian 6th — Ch. 5 & 6
Metal Alloys & Ferrous Metals
Visualizer
Iron-Carbon Phase Diagram
(Interactive)
Reference
AISI/SAE Steel Designation Codes

## Slide 6
Core Questions
Try to answer these before we dive in — we'll revisit them with answers at the end of class.
1
Why is low-carbon steel easy to weld while welding high-carbon steel requires preheat and post-weld heat
treatment?
2
An AISI/SAE designation reads 4340. What does each part tell you about the composition and intended use?
3
Nickel, chromium, and molybdenum are all common alloying elements. What specific property does each
primarily contribute?
4
Two steels with the same ultimate tensile strength: one plain carbon, one quenched-and-tempered alloy steel.
Why might you choose the alloy steel?
5
You need steel for a cutting tool that must hold a sharp edge under high contact stress. What carbon content
range and steel category should you specify?

## Slide 7
Iron vs. Steel — What Carbon Does
Pure iron is a soft, weak metal with limited structural use. Steel is what happens when you dissolve carbon
into iron — and control exactly how much.
Fe
Pure Iron
•
BCC crystal structure at room temperature (ferrite
phase)
•
Extremely soft — yield strength ≈ 130 MPa
•
High ductility — almost too easy to deform
•
No carbon = no lattice distortion = no dislocation
blocking
•
Rarely used structurally on its own
Iron is BCC below 912°C (ferrite) and FCC above (austenite). This
allotropy is the foundation of all heat treatment — revisited in detail
in Week 6.
Fe+C
Steel
•
Carbon dissolves interstitially into the iron lattice (like
Week 1 alloys)
•
Carbon atoms distort the lattice → block dislocation
movement → stronger
•
Yield strength ranges from 250 MPa to over 2,000
MPa
•
Properties tunable through carbon content, alloying,
and heat treatment
•
0.02% to 2.14% carbon by weight — a narrow
window covering an enormous property range
Above 2.14% C, excess carbon can no longer stay in solution — it
precipitates as iron carbide. This is cast iron, which behaves very
differently and is covered in Week 5.

## Slide 8
Carbon's Effect — The Central Tradeoff
Carbon is the most powerful and cost-effective strengthening tool in steel — but every increase is a trade-off.
You cannot maximize all properties simultaneously.
Yield
Strength
↑ increases
More carbon → more
lattice distortion →
dislocations blocked
more effectively →
higher force needed to
cause permanent
deformation. Strength
can be doubled or
tripled with heat
treatment.
Hardness
↑ increases
Carbon increases
resistance to surface
indentation. Heat
treatment (hardening)
exploits this — high-
carbon steels can be
hardened to Rockwell C
60+, making excellent
cutting edges and wear
surfaces.
Ductility
↓ decreases
High carbon steels
deform less before
fracture. The distorted
lattice resists dislocation
movement — which
gives strength but
removes the plastic
warning before failure.
High-carbon steels snap,
not bend.
Toughness
↓ decreases
Toughness requires both
strength AND ductility.
High carbon reduces the
area under the stress-
strain curve — less
energy absorbed before
fracture. High-carbon
steels fail without
absorbing significant
impact.
Weld-
ability
↓ decreases
High carbon creates
hard, brittle heat-
affected zones prone to
hydrogen cracking.
Carbon equivalent (CE)
determines preheat
requirements. Above
~0.40% CE, careful
process control is
essential.

## Slide 9
Carbon Content — From Iron to Cast Iron
A narrow range of carbon content spans the entire world of iron-based materials. Each zone has its own
properties, applications, and behavior.
Pure Iron
< 0.02% C
Applications:
Electrical cores,
magnetic applications
Soft, ductile.
Rarely structural.
Low Carbon
Steel
0.02–0.30%
Applications:
Structural steel,
sheet, pipe, fabrication
Excellent weldability.
Most produced steel.
Medium Carbon
Steel
0.30–0.60%
Applications:
Shafts, gears, rails,
automotive parts
Heat-treatable.
Preheat to weld.
High Carbon
Steel
0.60–2.14%
Applications:
Cutting tools,
springs, wire rope
Hard, brittle.
Difficult to weld.
Cast Iron
> 2.14% C
Applications:
Engine blocks,
brake rotors, pipe
Not steel.
Covered in Week 5.

## Slide 10
Steel Classification — AISI/SAE System
AISI and SAE jointly developed the four-digit designation system used throughout industry. Reading a code
fluently is a core technician skill.
The Four-Digit Code:
XX
XX
Steel family &
primary alloying elements
Carbon content
in hundredths of %
Code
Family
Notes / Example Grades
10xx
Plain Carbon Steel
1020 — 0.20% C (low) / 1045 — 0.45% C (medium) / 1095 — 0.95% C
(high)
41xx
Chromium-Molybdenum Steel
4140 — 0.40% C / excellent hardenability, the shop workhorse of alloy
steels
43xx
Nickel-Cr-Molybdenum Steel
4340 — 0.40% C / very high strength, aerospace & defense, landing gear
31xx
Nickel-Chromium Steel
3160 — 0.60% C / improved toughness and hardenability
3xx
Austenitic Stainless (300s)
304, 316 — different naming convention; ≥10.5% Cr — covered in Week 5

## Slide 11
Reading the Code — Worked Examples
Being able to decode a steel designation is a core workplace skill — it tells you composition, expected
properties, preheat needs, and heat treatment response instantly.
1020
Plain Carbon (10xx)
0.20% C
Low carbon steel. Very soft and ductile. Excellent weldability — no
preheat needed for most thicknesses. Used for structural tube,
sheet metal, pipe, and general fabrication. Cannot be significantly
hardened by heat treatment.
1045
Plain Carbon (10xx)
0.45% C
Medium carbon steel. Good balance of strength and toughness.
Can be quenched and tempered to improve strength. Preheat
recommended for thicker sections. Common for shafts, bolts,
gears, and tooling.
4140
Cr-Mo (41xx)
0.40% C
Chromium-molybdenum alloy steel. Same carbon as 1045 but far
superior hardenability — can be hardened through thick sections.
Excellent fatigue and wear resistance. Preheat required for
welding. The workhorse of alloy steel.
4340
Ni-Cr-Mo (43xx)
0.40% C
Nickel-chromium-molybdenum alloy steel. Highest hardenability of
common structural alloy steels. Used in aerospace, landing gear,
and crankshafts. Very demanding preheat and post-weld heat
treatment (PWHT) requirements.

## Slide 12
Plain Carbon Steels — Grades and Applications
Plain carbon steels are the backbone of fabrication and manufacturing — simple, readily available, and well-
understood. The right grade depends on the application.
Low Carbon Steel
< 0.30% C
•
Soft and ductile — deforms
without fracture
•
Excellent weldability — no
preheat required
•
Good formability — bends, draws,
and rolls easily
•
Cannot be significantly hardened
by heat treatment
Applications:
Structural sections (I-beams, angles,
channels), sheet metal, pressure vessels, pipe,
general fabrication, stampings
Typical: A36, A572, 1018, 1020
Medium Carbon Steel
0.30–0.60% C
•
Stronger and harder than low
carbon
•
Can be quenched and tempered
to improve strength
•
Reduced weldability — preheat
often needed
•
Good balance of strength and
toughness after heat treatment
Applications:
Shafts, gears, couplings, rails, automotive
axles, bolts, crankshafts, agricultural
equipment
Typical: 1040, 1045, 1050
High Carbon Steel
0.60–2.14% C
•
Very high hardness and wear
resistance
•
Low ductility — limited
formability
•
Difficult to weld — requires
careful preheat and PWHT
•
Excellent response to hardening
heat treatment
Applications:
Cutting tools, drill bits, springs, wire rope, saw
blades, files, wear plates, knife blades
Typical: 1060, 1080, 1095

## Slide 13
Alloying Elements — What Each One Does
Plain carbon steels cannot meet every requirement. Alloying elements are added to extend performance
beyond what carbon alone can achieve.
Mn
Manganese
Improves hardenability and
strength. Combines with sulfur
to form MnS — trapping sulfur
as harmless inclusions and
preventing hot cracking during
rolling.
Present in virtually all steels. Typical
range: 0.5–2.0%.
Cr
Chromium
Increases hardenability, wear
resistance, and corrosion
resistance. At ≥10.5% by weight,
forms the passive chromium
oxide layer that makes stainless
steel corrosion resistant.
Key element in stainless steels and
tool steels.
Ni
Nickel
Improves toughness, especially
at low temperatures. Increases
hardenability without reducing
ductility significantly. Stabilizes
the austenite phase (FCC) at
room temperature.
Expensive. Used in cryogenic and
austenitic stainless grades.
Mo
Molybdenu
m
Enhances hardenability and
maintains strength at elevated
temperatures. Reduces temper
embrittlement. Improves pitting
corrosion resistance alongside
chromium (as in 316 stainless).
Key in 4140 alloy steel and 316
stainless. Often paired with Cr.
V
Vanadium
Refines grain size through
precipitation hardening — fine
vanadium carbide particles pin
grain boundaries and resist grain
growth. Improves both strength
and toughness simultaneously.
Used in HSLA structural steels and
high-speed tool steels.
Si
Silicon
Acts as a deoxidizer during
steelmaking — scavenges
oxygen from the melt. In higher
quantities improves strength
and electrical resistivity. Raises
hardenability slightly.
Usually 0.1–0.3% in most steels as a
steelmaking residual.

## Slide 14
Alloy Steels — When Plain Carbon Is Not Enough
Plain carbon steels are the default — cheap, available, and well-understood. You specify an alloy steel only when
the application demands something plain carbon cannot deliver.
Limitations of Plain Carbon Steel
•
Cannot be hardened through thick sections —
hardness drops off rapidly with depth (poor
hardenability)
•
Loses strength at elevated temperatures — not
suitable for high-temperature service above
~300°C
•
Corrodes readily in moisture, chemicals, and
aggressive environments
•
Poor toughness at low (sub-zero) temperatures —
risk of brittle fracture
•
Limited wear resistance for sliding or abrasion
without surface treatment or coating
When to Specify Alloy Steel
•
Deep hardening through thick sections — add Cr,
Mo, or Ni to improve hardenability (4140, 4340)
•
High-temperature service — Mo maintains
strength above 400°C (Cr-Mo steels for pressure
vessels)
•
Corrosive environments — Cr ≥10.5% for stainless;
weathering steel for structural outdoor use
•
Cryogenic or impact applications — Ni improves
toughness at sub-zero temperatures
•
Higher strength-to-weight ratio — HSLA grades
with V or Nb for lighter structural designs

## Slide 15
Steel in the Shop — What a Technician Must Know
Reading a material spec is only the start. Every steel grade carries specific implications for cutting, welding,
heat treating, and inspection.
1
Identify the grade
Find the AISI/SAE code on the material certificate or
drawing. First two digits: steel family and alloying
elements. Last two: carbon in hundredths of a percent.
Both matter for everything that follows — treat the spec
as a full description, not just a name.
2
Assess weldability
Carbon equivalent: CE = %C + %Mn/6 + (%Cr+%Mo+%V)/5
+ (%Ni+%Cu)/15. CE above ~0.40% requires preheat.
Above 0.60%, preheat is mandatory and PWHT is very
likely required. The higher the CE, the more precisely heat
input must be controlled.
3
Know heat treatment
Low carbon steels: no significant heat treatment response
— use as-supplied. Medium and high carbon: quench to
harden, temper to reduce brittleness. Alloy steels: same
sequence but require more precise temperature control
and should NOT be welded in the hardened condition
without PWHT.
4
Inspect for the right defects
High carbon and alloy steels are prone to hydrogen (cold)
cracking in the heat-affected zone — especially in thick
sections or high-restraint joints. Understand WHY preheat
and PWHT requirements exist in the procedure, not just
that they do. That understanding is the difference
between technician and craftsman.

## Slide 16
CCT Diagram — What Actually Forms During Real Cooling
What the CCT Diagram Shows
•
CCT = Continuous Cooling Transformation — plots
temperature vs. time (log scale) with cooling curves
overlaid
•
Each steel composition has its own CCT diagram — the
phase diagram is universal; the CCT is alloy-specific
•
Cooling curves that intersect a transformation region
produce that microstructure; faster curves bypass
regions entirely
•
Ms and Mf lines: martensite start and finish
temperatures — steel must cool below Ms to begin
forming martensite
•
Hardenability: alloying elements (Cr, Ni, Mo, Mn) shift
CCT curves right → martensite forms at slower cooling
rates and in thicker sections
Microstructures by Cooling Rate
Pearlite (slow)
Furnace cooling / annealing. Ferrite + cementite lamellae.
Soft, ductile, machinable. Used where formability and
machinability matter.
Bainite (intermediate)
Interrupted quench or alloy steel air-cool. Finer than pearlite
— better strength + toughness combination. Avoids
martensite brittleness.
Martensite (fast)
Water or oil quench. BCT crystal — carbon trapped.
Extremely hard (up to ~65 HRC) but brittle as-quenched.
Must be tempered before use.

## Slide 17
Heat Treatment Processes
Annealing
Goal:
Soften, relieve stress, restore ductility
How:
Heat to austenite region → furnace
cool (very slow)
Result:
Coarse pearlite — soft, ductile,
excellent machinability
Use:
After cold work, before machining, to
restore formability
Normalizing
Goal:
Refine grain size, homogenize
microstructure
How:
Heat to austenite region → still-air cool
Result:
Fine pearlite — slightly harder and
stronger than annealed
Use:
Forgings and castings before further
processing or machining
Quenching
Goal:
Maximize hardness
How:
Heat to austenite → rapid quench
(water, oil, or polymer)
Result:
Martensite — very hard (up to 65 HRC)
but brittle
Use:
First step in quench-and-temper; never
used as-quenched alone
Tempering
Goal:
Restore toughness after quenching
How:
Reheat quenched martensite to 150–
650°C → air cool
Result:
Tempered martensite — lower
hardness, far higher toughness
Use:
After quenching — higher temp = more
toughness, less hardness
Case Hardening
Goal:
Hard surface over tough core
How:
Carburize (add C to surface) or nitride
(add N), then quench
Result:
Hard martensitic case; tough
ferrite/pearlite core
Use:
Gears, cams, shafts needing wear
resistance + impact toughness

## Slide 18
Core Questions — Answers
1
Why is low-carbon steel easy to weld while high-carbon steel requires preheat and PWHT?
Higher carbon increases hardenability — the HAZ cools fast and forms brittle martensite. Without preheat/PWHT
that's a fracture site. CE > 0.4 generally requires preheat.
2
An AISI/SAE designation reads 4340. What does each part tell you?
43 = Ni-Cr-Mo alloy steel family. 40 = 0.40% nominal carbon. Used in high-hardenability applications: aircraft landing
gear, crankshafts, large structural components.
3
Nickel, chromium, and molybdenum are common alloying elements. What does each primarily contribute?
Chromium → hardenability & corrosion resistance. Nickel → toughness & low-temperature impact strength.
Molybdenum → hardenability, creep resistance, prevents temper embrittlement.
4
Same UTS: plain carbon vs. quenched-and-tempered alloy steel. Why choose the alloy steel?
Alloy steel achieves that UTS at lower carbon → better weldability and toughness. Alloying elements give deep
hardenability so full hardness develops through thick sections.
5
Steel for a cutting tool that must hold a sharp edge under high contact stress — what do you specify?
>0.6% C (typically 0.8–1.2%) for hard martensite. Tool steels add Cr, W, V for carbide particles that resist wear and
retain hardness at elevated temperatures.

## Slide 19
Key Takeaways
1
Steel is a family of alloys, not a single material
Carbon content is the single most important variable — controlling hardness, strength, ductility, and weldability. Every carbon
increase trades strength for weldability and toughness.
2
The AISI/SAE code is a practical tool every technician must use
First two digits = steel family and alloying type. Last two = carbon in hundredths of %. Reading 4140 instantly communicates:
Cr-Mo alloy steel, 0.40% carbon — good hardenability, preheat required to weld.
3
Alloying elements solve problems plain carbon steel cannot
Cr improves corrosion resistance and hardenability. Ni improves low-temperature toughness. Mo maintains high-temperature
strength. Each solves a specific limitation — at the cost of price, weldability, and processing complexity.
4
Every grade carries welding and heat treatment implications
Carbon equivalent (CE) determines preheat requirements. Higher CE → higher preheat → more controlled heat input. Alloy
steels may also require PWHT. Read the spec and know what to plan for before striking an arc.
5
Safety is not optional!
PPE is mandatory in the shop — no exceptions. We work with heat, sharp edges, and hazardous materials every lab session.
Protect yourself and your classmates.

## Slide 20
Resources & What's Next
Week 4 Resources
•
Moniz Ch. 11, 12 & 14 — Iron, Carbon Steels & Heat
Treatment
•
Kalpakjian Ch. 5 & 6 — Heat Treatment & Ferrous
Metals
Visualizers
•
Iron-Carbon Phase Diagram (Interactive)
•
CCT Diagram — Cooling Rate vs. Microstructure
(Reference)
Coming Up — Week 5
Stainless Steels & Cast Irons
•
What makes stainless steel corrosion-resistant —
the passive chromium oxide layer
•
The four stainless steel families and how
microstructure defines each one
•
Ferritic, martensitic, austenitic, and duplex —
grades, properties, and selection
•
Cast iron types — gray, white, ductile, and
malleable — microstructure and applications
Unit 2 covers Weeks 4 – 6 · Review AISI/SAE codes and heat treatment before Week 5