## Slide 1
M E C H 1 9 1 — M e t a l l u r g y
Week 7
Mechanical Testing Methods
October 5, 2026 · 5:00 – 7:30 PM · Kai Santos

## Slide 2
Class Agenda
01
Tensile & Hardness Testing
What each test measures, how to read results, and which method fits which material
02
Impact & Fatigue Testing
Charpy impact, the ductile-brittle transition, fatigue mechanisms, and the S-N curve
03
Reading Mill Test Reports
Traceability, acceptance criteria, common flags, and the technician's responsibility

## Slide 3
Alloy Research Portfolio — Module 6
No Microscope Required
Module 6 · Week 7
Mechanical Testing
What to do this week:
Research published ASTM E112 grain size and HV for 1018 and 1045 steel —
record both in your Hardness Log.
Steps:
1 Research — record data & sources
2 Answer — short-answer questions
3 Apply — critical-thinking & equations
Alloys of Record
· Alloy A — 1018 steel (ref. HV)
· Alloy B — 1045 steel (ref. HV)
How to Complete This Module:
1 Research the alloy(s) using credible sources
2 Record data with a source citation
3 Answer the short-answer questions
4 Answer the critical-thinking questions
5 Keep the module with your portfolio
Portfolio Handout — Module 6

## Slide 4
MECH 191 — Course & Unit Roadmap
Unit 1
Materials Fundamentals
Wk 1
Aug 24
Atomic Structure
& Bonding
Wk 2
Aug 31
Mechanical
Properties
Unit 2
Steel & Alloys
Wk 4
Sep 14
Carbon &
Alloy Steels
Wk 5
Sep 21
Stainless &
Cast Irons
Wk 6
Sep 28
Nonferrous &
Phase Diagrams
Unit 3
Testing & Quality
Wk 7 ← here
Oct 5
Mechanical
Testing
Wk 8
Oct 12
NDT Methods
Wk 9
Oct 19
Quality
Standards
Unit 4
Manufacturing
Wk 10
Oct 26
Casting
Wk 11
Nov 2
Forming
Wk 12
Nov 9
Machining
Wk 13
Nov 16
Powder
Metallurgy
Unit 5
Joining & Failure
Wk 14
Nov 23
Welding
Processes
Wk 15
Nov 30
Weld Metallurgy
& Failure
Wk 16
Dec 7
Corrosion
& Wrap-up
Week 17 · FINAL EXAM

## Slide 5
Week 7 — At a Glance
Topics
•
Tensile testing — stress-strain curve, yield strength, UTS,
elongation at fracture
•
The 0.2% offset method for materials without a clear yield point
•
Hardness testing — Rockwell (HRC, HRB), Brinell (HB), and Vickers
(HV): methods and when each is used
•
Charpy impact testing — notched specimens, energy absorption,
and the ductile-brittle transition temperature
•
Fatigue — cyclic loading, crack initiation at stress concentrations,
the S-N curve, and the steel fatigue limit
•
Reading a mill test report (MTR) — heat numbers, composition,
mechanical test results, and traceability
Resources
Reference Material
Moniz Ch. 3
Mechanical Testing
Kalpakjian Ch. 2
Fundamentals of Mechanical Behavior
Visualizers
Stress-Strain Curve (Interactive)
Reference Pages
Hardness Testing Scales
Impact & Fatigue Testing

## Slide 6
Core Questions
Try to answer these before we dive in — we'll revisit them with answers at the end of class.
1
What does a tensile test actually measure and what do the results tell you about a material?
2
What is the difference between Rockwell and Brinell hardness, and when is each used?
3
Why is impact testing important and what is the ductile-brittle transition?
4
What is fatigue and why can a metal fail at stresses well below its yield strength?
5
How do you read a mill test report — and what are the key items a technician must verify?

## Slide 7
Tensile Testing — The Stress-Strain Curve
What the Test Measures
•
Pulls a standardised specimen apart at a controlled
rate while measuring force and extension
•
Force and extension are converted to engineering
stress (σ = F/A₀) and engineering strain (ε = ΔL/L₀)
•
Results are plotted as a stress-strain curve — each
point tells a different story about the material
•
The 0.2% offset method is used when no clear yield
point exists — draw a line parallel to the elastic slope
from 0.2% strain; the intersection with the curve is the
reported yield strength
•
A single tensile test returns yield strength, UTS,
elongation, and reduction in area — more data per test
than any other routine test
Key Values from the Curve
Proportional limit:
Stress up to which σ–ε is linear — the elastic region
Yield strength (Sy):
Stress at onset of permanent plastic deformation — a primary
design parameter
Ultimate tensile strength (UTS):
Maximum stress on the curve; necking begins at this point
Elongation at fracture:
Total permanent strain at fracture (%) — direct measure of ductility
Reduction in area:
% decrease in cross-section at fracture — especially useful for
materials that neck heavily
Curve shape:
Long plastic plateau = tough and ductile; steep then abrupt fracture
= brittle; no clear yield point = typical aluminum

## Slide 8
Hardness Testing — Three Methods, Three Applications
Method Comparison
Method
Indenter
Load & Readout
Best For
Typical Scale
Rockwell
Diamond cone (HRC)
Steel ball (HRB)
Minor + major load;
depth readout instantly
Production inspection;
finished parts
HRC 20–70 (hard steels)
HRB 0–100 (soft metals)
Brinell
Hardened ball
(10 mm, W/C)
High load; measure
indent diameter optically
Castings, forgings,
coarse-grained materials
HB / BHN up to ~650;
approximate UTS from HB
Vickers
Square pyramid
diamond (same for all)
Variable low loads;
measure diagonals optically
Thin sections, coatings,
precision & microhardness
HV 1–3000;
converts across HRC/HB
Conversion Caution
Approximate conversion tables between HRC, HB, and HV exist —
and approximate UTS can be estimated from HB (UTS ≈ 3.45 × HB in
MPa for carbon steels). These are approximations: use with caution
on alloy steels and non-ferrous materials where the relationship
differs.
Technician Rule of Thumb
Use Rockwell on the production floor for quick pass/fail checks. Use
Brinell on rough or coarse-grained material where a small
indentation would land in a soft spot. Use Vickers when measuring
case depth, thin-wall sections, or individual microstructural phases.

## Slide 9
Impact Testing & the Ductile-Brittle Transition
The Charpy Impact Test
•
A notched rectangular specimen is supported at both
ends; a swinging pendulum strikes from behind at the
notch
•
Energy absorbed = mgh₁ − mgh₂ (the difference
between swing height before and after fracture),
reported in Joules or ft-lbf
•
The notch simulates a real stress concentration — a
crack tip, undercut weld, sharp corner, or inclusion
•
Tough materials absorb high energy and show large
lateral expansion and shear fracture surfaces; brittle
materials absorb little energy and show bright, flat,
cleavage fracture surfaces
•
Izod test: specimen clamped vertically and struck at
the top — less common in modern standards than
Charpy
Ductile-Brittle Transition (DBTT)
Upper shelf:
High absorbed energy — fully ductile fracture. Material behaves
toughly above the transition temperature.
Lower shelf:
Low absorbed energy — fully brittle fracture. Even a tough-looking
material becomes dangerous below this temperature.
Transition temperature:
Defined at 50% of upper shelf energy (or 50% brittle fracture
appearance). A material can pass room-temperature testing but be
catastrophically brittle at service temperature.
BCC steels:
Carbon and low-alloy steels show a sharp DBTT — critical for arctic
pipelines, offshore structures, and pressure vessels in cold service.
FCC metals:
Austenitic stainless, aluminum, copper remain tough at cryogenic
temperatures — no DBTT. Essential for LNG and cryogenic
applications.

## Slide 10
Fatigue — Cyclic Loading and the S-N Curve
How Fatigue Works
•
Fatigue is progressive crack initiation and growth
under cyclic loading — even when applied stress is well
below yield strength
•
Each load cycle causes tiny damage at a stress
concentration; damage accumulates invisibly over
thousands or millions of cycles
•
No plastic deformation occurs until final fracture — a
fatigue failure gives NO visible warning beforehand
•
Crack initiation almost always occurs at a stress
concentration: surface scratch, tool mark, sharp
corner, weld toe, porosity, inclusion, or notch
•
Compressive residual stress (e.g. from shot peening)
delays crack initiation and improves fatigue life; tensile
residual stress (e.g. from welding) accelerates it
The S-N Curve (Wöhler Curve)
What it plots:
Stress amplitude (S) vs. number of cycles to failure (N) on a log scale
— a downward-sloping line: lower stress survives more cycles.
Fatigue limit (steel):
Typically 40–50% of UTS for carbon steels. Below this stress
amplitude, a steel can theoretically survive an indefinite number of
cycles — a genuine design limit.
Aluminum alloys:
Have NO true fatigue limit — the S-N curve continues to slope
downward. Fatigue life must be specified for a finite number of
cycles (e.g. 10⁷ cycles).
Fatigue ratio:
Fatigue limit ÷ UTS — useful for comparing materials; typically 0.4–
0.5 for steels, 0.3–0.4 for aluminum alloys.
Design implication:
Surface finish, notches, and residual stresses affect where the S-N
curve sits — a polished surface in compression performs far better
than a notched surface in tension.

## Slide 11
Reading a Mill Test Report (MTR)
The MTR is the chain of traceability between raw material and finished component — without it, there is no way to verify the
material meets the specification.
01
Heat / Lot Number
Must match the number stamped or
stencilled on the physical material.
Without this match, the MTR does not
certify the material in your hand.
02
Material Grade & Specification
Confirm it matches what was ordered —
ASTM A36, API 5L Grade B, etc. A grade
substitution not approved by engineering
is a nonconformance.
03
Chemical Composition
Compare each element against the
specification limits — carbon, manganese,
phosphorus, and sulfur always; alloying
elements as required by the grade.
04
Mechanical Test Results
Yield strength, UTS, and elongation at
minimum; impact values if required.
Compare each against the minimum (or
maximum) acceptance criteria.
05
Test Standard & Certifying
Signature
Tests must be performed to the correct
standard (e.g. ASTM A370). The document
must be signed and traceable to an
accredited testing facility.

## Slide 12
Technician's Perspective — When Results Have Real Consequences
Red Flag: MTR heat number mismatch
The heat number on the MTR does not match the number stencilled on the pipe. Stop — do not use the material. Tag it as
quarantined, issue a nonconformance report, and notify the quality engineer. A material whose identity cannot be confirmed
cannot be installed in a code-governed system.
Caution: Impact values just at minimum
The Charpy values in the MTR meet the specification — but they are at the minimum allowable limit on a project with a low
minimum service temperature. Flag it to the engineer before installation. Minimum-conforming is not always fit-for-purpose when
temperatures drop below the tested range.
Good Practice: Hardness survey after welding
After welding P91 chrome-moly pipe, a Vickers microhardness survey is run across the weld, HAZ, and base metal. Hard spots
above the limit indicate insufficient post-weld heat treatment — the weld must be heat-treated again before pressure testing. The
test caught a problem before the system went into service.

## Slide 13
Core Questions — Answers
What does a tensile test measure and what do the results tell you?
Pulls a specimen apart while recording force and extension → stress-strain curve. Gives yield strength (permanent deformation
onset), UTS (maximum stress), and elongation (ductility). Curve shape reveals whether the material is ductile or brittle.
Rockwell vs. Brinell hardness — what's the difference and when is each used?
Rockwell measures penetration depth directly — fast, suits production inspection of finished parts (HRC for hard steels, HRB
for softer metals). Brinell measures a large indentation optically — averages out microstructural variation, suits castings and
forgings.
Why is impact testing important and what is the ductile-brittle transition?
Tensile tests apply load slowly; service impact is sudden. BCC steels have a DBTT — above it they absorb high energy (ductile);
below it they fracture with little warning (brittle). Charpy tests verify adequate toughness at minimum service temperature.
What is fatigue and why can a metal fail below yield strength?
Cyclic loading initiates a crack at a stress concentration, growing invisibly with each cycle until sudden fracture. No visible
warning because yield is never reached. The S-N curve gives safe design stress; steels have a fatigue limit; aluminum alloys do
not.
How do you read a mill test report?
Check: ① heat number matches material markings; ② grade/spec matches order; ③ chemical composition within spec
limits; ④ mechanical results (yield, UTS, elongation, impact if required) meet minimums; ⑤ test standard and certifying
signature are present.

## Slide 14
Key Takeaways
1
Mechanical testing translates microstructure into numbers — tensile, hardness, impact, and fatigue tests each
capture a different aspect of material behavior, and a technician who can read and interpret the results can make
informed decisions about material acceptance, fitness for service, and failure investigation.
2
Hardness is the fastest and most practical field test, but must be matched to the right scale and method for the
material — Rockwell for production inspection of finished parts, Brinell for castings and forgings where
microstructural variation matters, Vickers for precision work and thin sections.
3
The mill test report is the documentary backbone of material traceability — verifying that the heat number, grade,
composition, and mechanical results all match the specification is a fundamental quality control responsibility that
every technician must take seriously before any material goes into service.

## Slide 15
Resources & What's Next
Week 7 Resources
Moniz Ch. 3
Mechanical Testing — primary reading
Kalpakjian Ch. 2
Fundamentals of Mechanical Behavior of Materials
Stress-Strain Visualizer
Interactive — plot your own material parameters
Hardness Scales Reference
HRC / HRB / HB / HV conversion chart
Impact & Fatigue Reference
Charpy specimen geometry, S-N curve examples
Week 8 — NDT Methods
October 12, 2026
•
Visual testing (VT) — the first step before any other
method
•
Dye penetrant (PT) — finding surface-breaking
defects in any non-porous material
•
Magnetic particle (MT) — near-surface defects in
ferromagnetic materials
•
Ultrasonic (UT) — internal defect detection and wall
thickness measurement
•
Radiographic (RT) — volumetric imaging and the
radiation safety requirements that come with it