## Slide 1
M E C H 1 9 1 — M e t a l l u r g y
Week 8
Non-Destructive Testing Methods
October 12, 2026 · 5:00 – 7:30 PM · Kai Santos

## Slide 2
Class Agenda
01
Surface & Near-Surface Methods
Visual inspection, dye penetrant, and magnetic particle — what each finds and where each falls short
02
Volumetric Methods
Ultrasonic and radiographic testing — detecting internal defects, technique selection, and safety
03
Method Selection & Qualification
Matching the method to the defect, written procedures, and ASNT certification levels

## Slide 3
Alloy Research Portfolio — Module 7
No Microscope Required
Module 7 · Week 8
NDT Methods
What to do this week:
Research 1018 steel, 360 brass, and Ti-6Al-4V: typical inclusions,
intentional particles, and why NDT replaces sectioning here.
Steps:
1 Research — record data & sources
2 Answer — short-answer questions
3 Apply — critical-thinking & equations
Alloys of Record
· Alloy A — 1018 steel
· Alloy L — 360 leaded brass
· Alloy P — Ti-6Al-4V titanium
How to Complete This Module:
1 Research the alloy(s) using credible sources
2 Record data with a source citation
3 Answer the short-answer questions
4 Answer the critical-thinking questions
5 Keep the module with your portfolio
Portfolio Handout — Module 7

## Slide 4
MECH 191 — Course & Unit Roadmap
Unit 1
Materials Fundamentals
Wk 1
Aug 24
Atomic Structure
& Bonding
Wk 2
Aug 31
Mechanical
Properties
Unit 2
Steel & Alloys
Wk 4
Sep 14
Carbon &
Alloy Steels
Wk 5
Sep 21
Stainless &
Cast Irons
Wk 6
Sep 28
Nonferrous &
Phase Diagrams
Unit 3
Testing & Quality
Wk 7
Oct 5
Mechanical
Testing
Wk 8 ← here
Oct 12
NDT Methods
Wk 9
Oct 19
Quality
Standards
Unit 4
Manufacturing
Wk 10
Oct 26
Casting
Wk 11
Nov 2
Forming
Wk 12
Nov 9
Machining
Wk 13
Nov 16
Powder
Metallurgy
Unit 5
Joining & Failure
Wk 14
Nov 23
Welding
Processes
Wk 15
Nov 30
Weld Metallurgy
& Failure
Wk 16
Dec 7
Corrosion
& Wrap-up
Week 17 · FINAL EXAM

## Slide 5
Week 8 — At a Glance
Topics
•
Visual inspection (VT) — the first step in every inspection sequence;
capabilities and limits
•
Dye penetrant testing (PT) — capillary action, color contrast vs.
fluorescent, dwell time, and surface limitations
•
Magnetic particle testing (MT) — ferromagnetic materials only; yoke
vs. prod; field orientation and 2-direction rule
•
Ultrasonic testing (UT) — sound waves, couplant, straight beam vs.
angle beam, A-scan, phased array
•
Radiographic testing (RT) — X-ray vs. gamma sources, what
volumetric defects look like, planar defect limitation
•
Method selection — matching defect type, material, and geometry
to the right method
•
Written procedures and ASNT SNT-TC-1A qualification levels (I, II, III)
Resources
Reference Material
Moniz Ch. 29
Nondestructive Examination
Kalpakjian Ch. 4
Surfaces, Inspection, & Product Quality
Reference Pages
NDT Methods — Physics, Techniques &
Limitations
Defect Recognition
Unit 3 Quiz — Weeks 7–9
Scheduled during Week 9

## Slide 6
Core Questions
Try to answer these before we dive in — we'll revisit them with answers at the end of class.
1
What is the difference between destructive and non-destructive testing, and why does it matter in practice?
2
What are the five main NDT methods and what types of defects can each detect?
3
How do you choose the right NDT method for a given situation — what factors must you consider?
4
What role do written procedures and technician qualification play in NDT — and why are they non-negotiable?

## Slide 7
Visual Inspection (VT) — The Foundation of Every Inspection
What VT Can and Cannot Find
Direct VT:
Naked eye + adequate lighting, mirrors, and magnifying lenses
— the simplest and most universal method. Minimum
illuminance is specified in the procedure.
Remote VT:
Borescopes, videoscopes, and drones reach where direct
access is impossible — internal pipe surfaces, turbine blades,
vessel interiors.
What VT finds:
Surface cracks, corrosion, mechanical damage, weld surface
defects (undercut, overlap, spatter, surface porosity), incorrect
geometry, misalignment, coating condition.
What VT misses:
Anything subsurface — a visually clean surface gives zero
information about what lies beneath. VT is always Step 1; it is
never the only step for critical components.
Weld Inspection by VT
•
Check weld profile against the weld symbol on the
drawing — correct size, length, and location
•
Undercut: a groove at the weld toe that reduces
effective throat thickness — measured with a fillet
gauge
•
Overlap: weld metal rolled over base metal without
fusion — visible as a rolled edge; planar defect, no
acceptable amount
•
Excessive spatter: indicates incorrect parameters; may
also indicate moisture in consumables
•
Surface porosity: visible pores in the weld face —
investigate shielding gas coverage and base metal
cleanliness
•
Cracks: linear indications at the weld surface, HAZ, or
crater — any crack is cause for rejection pending
investigation
•
Key requirement: lighting ≥ 500 lux (or per procedure)
— poor lighting is the most common cause of missed
surface defects

## Slide 8
Dye Penetrant Testing (PT) — How It Works and Where It Fails
Process Steps
1
Pre-cleaning:
Remove all paint, scale, oil, and coatings — any contamination
can seal the defect opening and prevent penetrant entry
2
Penetrant application:
Apply to the cleaned surface; low-viscosity liquid is drawn into
defects by capillary action
3
Dwell time:
Hold time specified in the procedure — too short misses fine
defects; too long may dry the penetrant in the defect before
developer is applied
4
Excess removal:
Remove surface penetrant without flushing the defect — use a
damp cloth (solvent removable) or water rinse (water-
washable)
5
Developer application:
Draws trapped penetrant back out of defects — creates a
visible bleed-out indication against a white background
6
Inspection + post-clean:
Inspect per procedure; document indications; clean the
surface to remove developer and residual penetrant
Color Contrast vs. Fluorescent
Color contrast (visible):
Red penetrant on white developer — inspected under white light.
Standard field method, simpler logistics.
Fluorescent:
Penetrant glows under UV (black) light — significantly more
sensitive; used for critical or fine-defect applications.
Limitations
•
Only detects surface-breaking defects — subsurface
defects are invisible to PT
•
Surface must be clean and free of coatings that seal the
defect opening
•
Porous materials (as-cast surfaces, thermal spray
coatings) cannot be inspected — the whole surface
bleeds back
•
Works on any non-porous material — metals, ceramics,
plastics (unlike MT which needs ferromagnetic material)

## Slide 9
Magnetic Particle Testing (MT) — Principle, Methods & Limitations
Principle & Magnetization Methods
How it works:
The component is magnetised; at a defect, the magnetic field is
forced out of the material creating flux leakage; iron particles (dry
or wet suspension) are attracted to the leakage and form a visible
indication.
Yoke:
Electromagnetic yoke placed on the surface induces a field
between its poles — portable, widely used for weld inspection;
detects defects perpendicular to the field.
Prod:
Electrical contacts pressed onto the surface pass current through
the material — creates a circular field; detects defects running
between the prods; risk of arc burns at contact points.
Coil / central conductor:
Used for magnetising whole components longitudinally or
circularly — common in shop environments for valves, fittings,
and bar stock.
Key Rules & Limitations
Ferromagnetic only:
Carbon steels, low-alloy steels, martensitic and ferritic stainless
steels. Cannot be used on austenitic stainless, aluminum, copper, or
titanium.
Depth capability:
Detects surface and near-surface defects up to approximately 2–3
mm below the surface — superior to PT for near-surface detection
in magnetic materials.
Two-direction rule:
A defect must be at 45–90° to the field to produce a detectable
indication. Inspections must be performed in at least two
perpendicular directions to ensure all orientations are covered.
WFMT:
Wet fluorescent MT: iron particles in liquid carrier viewed under UV
light — the most sensitive MT technique; widely used for critical
weld inspection in pressure vessel and pipeline fabrication.
Demagnetization:
Required after inspection on components where residual
magnetism would interfere with service — near instruments, or
where particles could contaminate a process.

## Slide 10
Ultrasonic Testing (UT) — Detecting Internal Defects with Sound
Principle & Techniques
How it works:
A transducer converts electrical energy to high-frequency sound
waves (1–10 MHz) that travel through the material. Reflections
from defects or the back wall return to the transducer; time of
flight gives depth.
Couplant:
Gel, oil, or water between transducer and surface — air is a poor
transmitter of ultrasound. Couplant must be compatible with the
material and the process.
Straight beam (compression wave):
Transducer perpendicular to the surface — sound travels straight
through. Used for lamination detection and thickness
measurement in corroded pipe.
Angle beam (shear wave):
Transducer angled to direct sound at 45°, 60°, or 70° into the
material — used for weld inspection where the sound must be
directed toward fusion faces and the weld root.
Reading Results & Advanced Techniques
A-scan display:
Time-base trace showing signal amplitude vs. time of flight — the
inspector reads peaks (echoes) to identify defect depth and relative
size. Fundamental UT display.
Phased array UT (PAUT):
Multiple elements steer and focus the beam electronically —
produces S-scans (sectoral cross-sections of the weld). Increasingly
replaces conventional UT and radiography in modern fabrication.
Thickness measurement:
Straight beam UT from one side gives remaining wall thickness —
essential for in-service corrosion monitoring where internal access
is impossible.
Limitations:
Rough surfaces reduce coupling efficiency. Coarse-grained materials
(some austenitic stainless, castings) scatter sound and make
interpretation difficult. Defects parallel to the beam may not reflect
sufficient energy.

## Slide 11
Radiographic Testing (RT) — Volumetric Imaging with X-Ray and Gamma
Principle & Sources
How it works:
Radiation passes through the component onto film or a digital
detector on the opposite side. Denser material absorbs more
radiation and appears lighter on the image; voids absorb less and
appear darker.
X-ray sources:
X-ray tubes generate radiation with adjustable energy — suitable
for a wide range of thicknesses; require electrical power. Used in
shop environments.
Gamma ray sources:
Radioactive isotopes (Ir-192, Co-60, Se-75) — compact, no power
required, fixed energy output. Ideal for field use and confined
spaces where power is unavailable.
Film RT vs. digital:
Film provides a permanent archival image processed in a
darkroom. Digital radiography (DR) and computed radiography
(CR) use digital detectors or phosphor plates — faster, no
chemicals, images can be enhanced.
What RT Finds, Misses, and Safety
Detects well:
Volumetric defects — porosity, slag inclusions, tungsten inclusions,
burn-through, lack of fill. The rounded or irregular shape creates a
clear density difference on film.
Detects poorly:
Tight planar defects (cracks, lack of fusion) oriented at a small angle
to the beam may be completely invisible on a radiograph. UT is
superior for planar defect detection.
Permanent record:
RT produces an image record that can be stored, reviewed, and
compared over time — valuable for in-service monitoring and
fitness-for-service assessments.
Radiation safety:
RT involves ionising radiation subject to strict regulatory controls —
designated radiation areas, dosimetry monitoring, and licensing. A
technician working near RT must understand exclusion zone
requirements and never enter a restricted area during an exposure.

## Slide 12
Method Selection — Matching the Method to the Problem
Ask five questions in sequence — the answers eliminate unsuitable methods and point to the correct choice.
Factor
VT
PT
MT
UT
RT
Defect location
Surface only
Surface-breaking
only
Surface &
near-surface
Surface &
deep internal
Surface &
deep internal
Material type
Any
Non-porous
any material
Ferromagnetic
only
Most metals
& composites
Most solid
materials
Detects planar
cracks well?
Depends
(surface)
Yes (if
surface-breaking)
Yes (near-
surface)
Yes
(preferred)
Poor (if parallel
to beam)
Access required
One side
(direct view)
One side
One side
One side
Both sides
(source + film)
Produces permanent
image record?
No
No
No
A-scan /
S-scan digital
Yes
(film or digital)
ASNT SNT-TC-1A — Level I: perform under supervision · Level II: perform, interpret & accept/reject · Level III: write procedures & certify

## Slide 13
Core Questions — Answers
What is the difference between destructive and non-destructive testing, and why does it matter?
Destructive testing (tensile, hardness, Charpy) consumes or damages the specimen — accurate but the tested piece cannot go into
service. NDT inspects the actual component without altering it, enabling 100% inspection and in-service monitoring of critical
components.
What are the five main NDT methods and what does each detect?
VT: visible surface defects. PT: surface-breaking defects in any non-porous material. MT: surface and near-surface defects in
ferromagnetic materials. UT: surface and deep internal defects via sound waves. RT: volumetric defects (porosity, inclusions) via
radiation imaging.
How do you choose the right NDT method?
Consider: (1) defect type and expected location (surface, near-surface, volumetric); (2) material (ferromagnetic or not, porous or
not); (3) geometry and access available; (4) required sensitivity; (5) applicable code or standard specifying the method.
What role do written procedures and technician qualification play — and why are they non-negotiable?
Every method must be performed per a qualified written procedure specifying equipment, materials, technique, and acceptance
criteria. Technicians must hold ASNT Level I, II, or III certification for the method. An uncertified person cannot accept or reject an
indication, and deviating from the procedure invalidates the inspection regardless of the result.

## Slide 14
Key Takeaways
1
Each NDT method operates on a different physical principle and detects a different subset of defects — no single
method finds everything, and method selection must be matched to the defect type, material, geometry, and
applicable code requirement.
2
Written procedures and technician qualification are not bureaucratic formalities — they are what makes NDT results
legally and technically defensible. An inspection performed outside its qualified procedure is not a valid inspection
regardless of what the technician found.
3
Understanding the limitations of each method is just as important as understanding its capabilities — knowing what
a method cannot detect is what prevents a false sense of security after an inspection passes.

## Slide 15
Resources & What's Next
Week 8 Resources
Moniz Ch. 29
Nondestructive Examination — primary reading
Kalpakjian Ch. 4
Surfaces, Inspection, and Product Quality Assurance
NDT Methods Reference
Physics, techniques, and limitations for all 5 methods
Defect Recognition Guide
Visual identification of common weld and material defects
Week 9 — Quality Standards
October 19, 2026
•
What quality standards are and why they exist —
ASTM, AWS, ASME, ISO, and API
•
Common weld defects and how to recognize them —
porosity, LOF, cracks, undercut
•
Indication vs. discontinuity vs. defect vs. reject —
precise language that matters
•
What good inspection documentation looks like and
why it is a legal document