## Slide 1
M E C H 1 9 1 — M e t a l l u r g y
Week 9
Quality Standards & Inspection
October 19, 2026 · 5:00 – 7:30 PM · Kai Santos

## Slide 2
Class Agenda
01
Standards, Codes & Defect Recognition
ASTM, AWS, ASME, ISO, and API — what each governs; manufacturing and service defects and how
each is identified
02
Indication → Defect → Reject
Precise definitions and the evaluation sequence from detection to final disposition
03
Inspection Documentation
What a valid inspection report must contain, traceability, record retention, and non-conformance
reports

## Slide 3
Alloy Research Portfolio — Module 8
No Microscope Required
Module 8 · Week 9
Quality Standards
What to do this week:
Research published ASTM E112 grain size and E45 inclusion ratings
typical for normalized 1018 steel.
Steps:
1 Research — record data & sources
2 Answer — short-answer questions
3 Apply — critical-thinking & equations
Alloys of Record
· Alloy A — 1018 steel (normalized)
How to Complete This Module:
1 Research the alloy(s) using credible sources
2 Record data with a source citation
3 Answer the short-answer questions
4 Answer the critical-thinking questions
5 Keep the module with your portfolio
Portfolio Handout — Module 8

## Slide 4
MECH 191 — Course & Unit Roadmap
Unit 1
Materials Fundamentals
Wk 1
Aug 24
Atomic Structure
& Bonding
Wk 2
Aug 31
Mechanical
Properties
Unit 2
Steel & Alloys
Wk 4
Sep 14
Carbon &
Alloy Steels
Wk 5
Sep 21
Stainless &
Cast Irons
Wk 6
Sep 28
Nonferrous &
Phase Diagrams
Unit 3
Testing & Quality
Wk 7
Oct 5
Mechanical
Testing
Wk 8
Oct 12
NDT Methods
Wk 9 ← here
Oct 19
Quality
Standards
Unit 4
Manufacturing
Wk 10
Oct 26
Casting
Wk 11
Nov 2
Forming
Wk 12
Nov 9
Machining
Wk 13
Nov 16
Powder
Metallurgy
Unit 5
Joining & Failure
Wk 14
Nov 23
Welding
Processes
Wk 15
Nov 30
Weld Metallurgy
& Failure
Wk 16
Dec 7
Corrosion
& Wrap-up
Week 17 · FINAL EXAM

## Slide 5
Week 9 — At a Glance
Topics
•
Quality standards — ASTM, AWS, ASME, ISO, and API: what each
organization governs and why using the wrong standard is a serious
error
•
Manufacturing weld defects — porosity, slag inclusions, lack of
fusion, lack of penetration, cracks, undercut, and overlap
•
Service defects — fatigue cracks, stress corrosion cracking, and
creep damage
•
Precise terminology: indication vs. discontinuity vs. defect vs. reject
•
The evaluation sequence: detection → characterization →
evaluation → disposition
•
Inspection documentation — minimum report content, traceability,
record retention, and non-conformance reports
Resources
Reference Material
Moniz Ch. 10
Materials Standards
Reference Pages
Quality Standards & Codes
Reading Inspection Documentation
Defect Recognition
Unit 3 Quiz
Covers Weeks 7–9
Scheduled this session
Next: Unit 4 — Manufacturing

## Slide 6
Core Questions
Try to answer these before we dive in — we'll revisit them with answers at the end of class.
1
What is a quality standard and why does it exist — what problem does it solve for a technician in the field?
2
What are the most common defects a technician will encounter and how is each one recognized during
inspection?
3
What is the difference between an indication, a discontinuity, a defect, and a reject — and why does the
distinction matter?
4
What does good inspection documentation look like, and why is an incomplete inspection report a serious
problem?

## Slide 7
Quality Standards & Codes — Knowing Which Rules Apply
Major Standards Bodies
Body
Governs
Key Standard(s)
Technician Relevance
ASTM
Material specs & test methods
A36, A370, E165
Acceptance criteria for base metals; test
procedures for mechanical and NDT
AWS
Welding codes & inspection
D1.1 Structural Steel
Weld acceptance criteria, inspection
requirements, welder qualification
ASME
Pressure vessels, boilers & piping
BPVC Sec. V (NDT), Sec. IX
NDT methods and procedures; welding
qualification for pressure equipment
ISO
International standards (global use)
9606, 17636, 17640
Welder qualification, RT and UT of welds —
used on international projects
API
Oil & gas industry
1104, 570, 650
Pipeline welding, piping inspection, storage
tank fabrication and repair
Using the wrong standard is as serious an error as missing a defect.
Acceptance criteria differ between codes — a weld accepted under AWS D1.1 may be rejectable under ASME Section VIII, or vice versa.
Know your governing document before you inspect.

## Slide 8
Common Weld Defects — Manufacturing Discontinuities
Porosity
Cause: Gas trapped in weld pool — moisture in consumables,
contaminated base metal, inadequate shielding gas, or excessive travel
speed.
Appears: Rounded voids — dark circular spots on RT; round bleed-out on
PT; discrete point reflectors on UT A-scan.
Risk: Reduces cross-sectional area; acts as stress concentrator.
Acceptance criteria limit size, number, and spacing.
Slag Inclusions
Cause: Flux or slag from SMAW/FCAW not fully removed between passes,
or trapped by poor bead geometry.
Appears: Irregular elongated dark indications on RT; irregular linear
bleed-out on PT if surface-breaking; elongated UT reflectors.
Risk: Reduces cross-section; can initiate fatigue cracks. Planar slag
inclusions are more serious than rounded ones.
Lack of Fusion (LOF)
Cause: Insufficient heat input, incorrect travel speed, or poor technique
— weld metal does not fuse with base metal or previous pass.
Appears: Linear indication parallel to fusion face on RT (may be missed if
beam isn't parallel); strong planar reflector on UT. Not detectable by
PT/MT unless surface-breaking.
Risk: Pre-existing planar crack with a sharp tip — most standards have
zero tolerance for LOF.
Lack of Penetration (LOP)
Cause: Insufficient heat or incorrect joint preparation — incomplete
fusion at the weld root.
Appears: Continuous or intermittent linear indication at weld root
centerline on RT; detectable by UT; visible to VT on root side if accessible.
Risk: Reduces effective throat and creates a sharp root notch — serious in
cyclically loaded structures.

## Slide 9
Weld Defects — Cracks, Undercut & Overlap; and Service Defects
Fabrication Defects (cont.)
Cracks — always rejectable:
Hot cracks (solidification), cold/hydrogen-induced cracks (HAZ,
<300°C), lamellar tearing, crater cracks. Appear as fine linear
indications on RT, linear bleed-out on PT/MT, strong planar
reflectors on UT. A crack is rejectable in virtually all standards
regardless of size — no minimum applies.
Undercut:
Groove at the weld toe caused by excessive current or incorrect
technique. Visible to VT; detectable by PT. Creates a stress
concentration especially dangerous in fatigue-loaded structures.
Acceptance criteria limit depth and length.
Overlap:
Weld metal rolled over base metal without fusing — low current
or slow travel. Visible to VT as a lip at the toe; detectable by PT.
Creates a sharp notch similar to undercut. No acceptance criteria
— no overlap is acceptable.
Service-Induced Defects
Fatigue cracks:
Initiate at stress concentrations (notches, weld toes, holes,
surface scratches) and propagate perpendicular to the applied
cyclic stress. Often invisible to VT until large — PT, MT, or UT
required for early detection.
Stress corrosion cracking (SCC):
Branching crack networks forming in susceptible alloys under the
simultaneous presence of stress and a corrosive environment.
Common in austenitic stainless (chlorides) and high-strength
steels. Appears as branching linear PT indications.
Creep damage:
Occurs at elevated temperature under sustained stress — grain
boundary cavitation progresses to cracking over time. Visible
metallographically in cross-section; later-stage damage may be
detectable by UT or RT.
Corrosion pitting:
Localised material loss — pits act as stress concentrations and
can initiate fatigue or SCC cracks. VT reveals visible pits; UT
thickness surveys map remaining wall. Severity assessed by pit
depth and density.

## Slide 10
Indication → Discontinuity → Defect → Reject — Precise Definitions
1
Indication
Definition:
Any response or evidence of a
discontinuity detected by an
NDT method. Simply means
something was found — no
judgment about significance.
Key point:
Non-relevant indications
(caused by geometry — weld
caps, threads, edges) must be
distinguished from real
discontinuities.
2
Discontinuity
Definition:
A physical interruption in the
material — a void, crack,
inclusion, or boundary — that
may or may not be harmful.
Key point:
Every defect is a discontinuity,
but not every discontinuity is a
defect. Evaluation against
criteria is required.
3
Defect
Definition:
A discontinuity that has been
evaluated against the
acceptance criteria of the
applicable standard and found
to exceed the allowable limits.
Key point:
The word 'defect' has a legal
meaning — it implies a finding
of non-conformance. Do not use
it casually before evaluation is
complete.
4
Reject / Disposition
Definition:
The disposition applied to a
component containing one or
more defects — repair, rework,
scrap, or use-as-is with
engineering approval (fitness for
service).
Key point:
Finding an indication does not
equal rejection. Every indication
must be evaluated against
acceptance criteria before a
disposition is made.
›
›
›

## Slide 11
Inspection Documentation — The Legal Record of Every Inspection
Minimum Report Content
•
Component ID: drawing number, heat/lot number, weld ID or location
reference
•
Applicable standard and revision
•
NDT method and written procedure reference number
•
Equipment used: make, model, serial number, calibration due date
•
Inspector name, certification level, and certification scheme
•
Date, time, and location of inspection
•
Environmental conditions (temperature, lighting for VT, surface
condition)
•
Description of any indications: location, orientation, size/length,
detection method
•
Acceptance criteria applied and evaluation result for each indication
•
Final disposition: accept or reject, with repair or re-inspection
requirements
•
Inspector signature and date
Traceability & Retention
Every record must link to the physical component
through unique identifiers — without traceability the
record is useless in an audit or failure investigation.
In most regulated industries records must be retained
for the design life of the equipment. Electronic
records must be backed up and protected against
alteration.
Non-Conformance Reports (NCR)
When a component is rejected, a formal NCR is raised
documenting:
• Nature of the non-conformance
• Disposition: repair, rework, scrap, or use-as-is with
engineering approval
• Re-inspection requirements after repair
Verbal assurances are worthless in a quality audit — if
it isn't documented, it didn't happen.

## Slide 12
Technician's Perspective — Documentation and Disposition in Practice
Red Flag: Report missing procedure reference and inspector certification
An inspection report arrives describing a linear PT indication within acceptance limits — but no procedure number, no equipment
calibration record, and no inspector certification level are listed. Do not accept the component. Return the report, require complete
documentation, and arrange re-inspection if procedural compliance cannot be demonstrated. The finding is meaningless if the
inspection cannot be shown to have been performed correctly.
Caution: Indication evaluated against the wrong standard
A weld in a pressure vessel is evaluated against AWS D1.1 (structural steel) acceptance criteria. The applicable code is actually
ASME Section VIII. Acceptance criteria differ between codes — a finding that passes AWS D1.1 may exceed ASME limits. This is as
serious as missing a defect: confirm the governing standard before evaluating any indication.
Good Practice: Complete NCR triggers correct disposition
A root crack is found in a pipeline girth weld by UT. A Non-Conformance Report is raised immediately, the weld is marked and
quarantined, and re-inspection after repair is scheduled with the same qualified procedure and inspector level. The NCR provides a
traceable record of the finding, the repair, and the re-test — essential documentation if the line ever fails in service.

## Slide 13
Core Questions — Answers
What is a quality standard and why does it exist?
A standard is a document published by a recognized body (ASTM, AWS, ASME, ISO, API) defining minimum acceptable requirements
for materials, processes, and inspection. Standards exist to ensure consistent quality, prevent disputes, and provide legal protection
— the governing standard is the technician's rulebook for acceptance criteria, methods, and documentation.
What are the most common defects a technician will encounter?
Manufacturing: porosity (rounded voids), slag inclusions (elongated voids), lack of fusion (planar — most serious), lack of
penetration (root), cracks (always rejectable), undercut, and overlap. Service: fatigue cracks, stress corrosion cracking, creep
damage, and corrosion pitting. Each defect has characteristic appearance in each NDT method.
Indication vs. discontinuity vs. defect vs. reject?
Indication: something was found — no judgment yet. Discontinuity: a physical interruption — may or may not be harmful. Defect: a
discontinuity that exceeds the acceptance criteria of the applicable standard. Reject: the disposition applied to a component
containing a defect. Finding an indication does NOT automatically mean rejection.
What does good inspection documentation look like — and why does an incomplete report matter?
A valid report records: component ID, applicable standard, NDT procedure, equipment & calibration, inspector name & certification
level, date/location, all indications with evaluation, final disposition, and signature. Missing any of these means the inspection
cannot be verified — an uncertifiable inspection is no inspection at all.

## Slide 14
Key Takeaways
1
Standards define the rules — a technician must know which standard governs their work and apply its acceptance
criteria consistently. Using the wrong standard or misapplying acceptance criteria is as serious an error as missing a
defect.
2
Indication, discontinuity, defect, and reject are precise technical terms with distinct meanings — confusing them
leads to incorrect dispositions and potentially unsafe components entering service.
3
Inspection documentation is not paperwork — it is the legal and technical record that proves the work was done
correctly. Incomplete, inaccurate, or untraceable records undermine the entire value of the inspection process.

## Slide 15
Resources & What's Next
Week 9 Resources
Moniz Ch. 10
Materials Standards — primary reading
Quality Standards & Codes
ASTM, AWS, ASME, ISO, API reference summary
Reading Inspection Documentation
Sample MTR, inspection report walkthrough
Defect Recognition Guide
Visual identification of all common weld defects
Unit 3 Quiz
Covers Weeks 7–9 — Mechanical Testing, NDT, Standards
Week 10 — Casting
October 26, 2026 · Unit 4: Manufacturing begins
•
Sand casting, investment casting, and die casting —
how each process works and what it produces
•
How solidification microstructure differs from
wrought microstructure — and why it matters for
properties
•
Common casting defects — porosity, shrinkage, hot
tears — and how to identify them
•
Why castings require Brinell hardness testing and
often need heat treatment before machining