## Slide 1
M E C H 1 9 1 — M e t a l l u r g y
Week 10
Casting Processes & Defect Recognition
October 26, 2026 · 5:00 – 7:30 PM · Kai Santos

## Slide 2
Class Agenda
01
Solidification & Sand Casting
How metal solidifies — shrinkage, gas, segregation, risers, chills, dendrites — and the sand casting
process from pattern to shakeout
02
Die Casting & Investment Casting
High-pressure die casting, hot vs. cold chamber, lost-wax investment casting, and other casting
processes
03
Casting Defects & Process Selection
Recognizing shrinkage porosity, gas porosity, hot tears, cold shuts, misruns, and inclusions — and how
to choose the right process

## Slide 3
Metallography Lab — Module 9
EXAMET-5-R-600-HD · 50–500×
Module 9 · Week 10
Wrought Aluminum Alloys
What to do this week:
Compare constituent particle size/density between 6061-T6 and 2024-T3 at
500×. This week's lab no longer uses a cast specimen — casting
fundamentals remain in today's lecture.
Steps:
1 Observe — complete feature table
2 Sketch — label magnification & specimen
3 Answer — 4 short questions
Specimens to Check Out
· Specimens G, J — 6061-T6 & 2024-T3 aluminum
How to check out the kit:
1 See instructor after class today
2 Sign out the specimen tray
3 Use the EXAMET-5 at your convenience
4 Return kit before leaving class
5 Submit completed module with your portfolio
Portfolio Handout — Module 9

## Slide 4
MECH 191 — Course & Unit Roadmap
Unit 1
Materials Fundamentals
Wk 1
Aug 24
Atomic Structure
& Bonding
Wk 2
Aug 31
Mechanical
Properties
Unit 2
Steel & Alloys
Wk 4
Sep 14
Carbon &
Alloy Steels
Wk 5
Sep 21
Stainless &
Cast Irons
Wk 6
Sep 28
Nonferrous &
Phase Diagrams
Unit 3
Testing & Quality
Wk 7
Oct 5
Mechanical
Testing
Wk 8
Oct 12
NDT Methods
Wk 9
Oct 19
Quality
Standards
Unit 4
Manufacturing
Wk 10 ← here
Oct 26
Casting
Wk 11
Nov 2
Forming
Wk 12
Nov 9
Machining
Wk 13
Nov 16
Powder
Metallurgy
Unit 5
Joining & Failure
Wk 14
Nov 23
Welding
Processes
Wk 15
Nov 30
Weld Metallurgy
& Failure
Wk 16
Dec 7
Corrosion
& Wrap-up
Week 17 · FINAL EXAM

## Slide 5
Week 10 — At a Glance
Topics
•
Solidification mechanics — shrinkage, gas porosity, segregation,
dendrite arm spacing, and how riser and chill design controls them
•
Sand casting — pattern, mold, gating system, cores, green sand vs.
chemically bonded sand, advantages and limitations
•
Die casting — hot chamber vs. cold chamber, high-pressure injection,
surface finish and tolerance advantages, alloy limitations
•
Investment (lost-wax) casting — ceramic shell process, best surface
finish and accuracy of any casting process, applications
•
Seven common casting defects — shrinkage porosity, gas porosity, hot
tears, cold shuts, misruns, inclusions, and warping
•
Process selection — alloy, part size, production volume, required
tolerance, and cost as the five deciding factors
Resources
Reference Material
Kalpakjian Ch. 10 & 11
Fundamentals & Processes of Metal Casting
Visualizers
Solidification & Dendrite Growth
Sand Casting — Process & Defects
Die Casting — NADCA Process
Investment Casting — ICI Process
Reference
Casting Defects — TWI Defect Library
Next: Week 11 — Metal Forming

## Slide 6
Core Questions
Try to answer these before we dive in — we'll revisit them with answers at the end of class.
1
What happens during solidification and why does it matter for casting quality?
2
What are the main casting processes and what are the trade-offs between them?
3
What defects are most common in castings and how is each one recognized?
4
How do you choose the right casting process for a given application?

## Slide 7
Solidification & Shrinkage — What Happens When Metal Freezes
Solidification Zones
Chill Zone
Fine equiaxed grains nucleate at mold wall — fastest cooling
Columnar Zone
Dendrites grow inward toward thermal center — directional
heat flow
Equiaxed Zone
Last region to solidify — equiaxed grains; site of shrinkage &
segregation
Key Mechanisms
Shrinkage
Metal contracts 2–8% vol. during solidification. Risers (feeders)
supply liquid metal to compensate — without a riser, internal voids or
surface sink marks form in the last section to solidify.
Gas Porosity
Dissolved gases (especially H₂) become insoluble as metal solidifies
and are expelled. If they cannot escape, smooth spherical voids form
— distributed through the casting or clustered near the surface.
Segregation
Alloying elements partition between solid and liquid — low-melting
elements concentrate in the last liquid, creating compositional
gradients. Homogenization heat treatment reduces microsegregation.
Dendrites & DAS
Solidification begins as tree-like dendrites growing from the mold
wall. Dendrite arm spacing (DAS) decreases with faster cooling —
finer DAS means better mechanical properties.

## Slide 8
Sand Casting — The Most Flexible Casting Process
1
Pattern Making
Replica of part in wood, plastic, or
metal — includes shrinkage,
machining, and draft allowances
2
Mold Prep
Sand (green or chemically bonded)
packed around pattern in a flask;
pattern withdrawn leaving the
cavity
3
Core Making
Separate sand shapes inserted to
create internal cavities or
undercuts the pattern cannot form
4
Mold Assembly
Cope (top) and drag (bottom)
halves assembled; gating system —
sprue, runner, gates — channels
metal in
5
Pouring
Molten metal poured into pouring
cup; controlled pour rate prevents
turbulence and oxide entrapment
6
Cooling
Metal solidifies; risers feed
shrinking sections; chills can
accelerate cooling in thick sections
7
Shakeout
Sand mold is broken away; casting
removed; sand reclaimed for reuse
8
Cleaning & Finish
Gates and risers removed; surface
cleaned by shot blasting;
dimensional and visual inspection
Advantages
Low tooling cost · Any metal and almost any size · Complex internal
geometry with cores · Short lead time at low volume
Limitations
Rough surface finish (Ra 6–25 μm) · Loose dimensional tolerances · Labor
intensive · Each mold destroyed after shakeout

## Slide 9
Die Casting — High Pressure, High Volume, Tight Tolerances
Hot Chamber Die Casting
•
Injection mechanism submerged in molten metal bath
•
Fast cycle times — mechanism always ready with liquid
metal
•
Limited to low-melting-point alloys: zinc, tin, lead
•
Cannot use for aluminum — molten Al attacks the steel
mechanism
Cold Chamber Die Casting
•
Metal ladled into separate shot chamber before each
injection
•
Slower cycle than hot chamber but handles higher-melting
alloys
•
Used for aluminum, magnesium, copper — the important
structural alloys
•
Injection pressure: 7–700 MPa; high velocity fills complex die
cavities
Advantages
Excellent surface finish (Ra 0.8–3.2 μm) ·
Tight tolerances · Fast cycle times · Thin
walls possible
Limitations
High tooling cost · Limited to lower-melting
alloys · No sand cores — limited internal
geometry
Die Casting Porosity
High velocity traps air — gas porosity is
inherent in die castings. Limits pressure-tight
and heat-treat applications. Vacuum die
casting significantly reduces this.

## Slide 10
Investment Casting — Lost Wax, Best Accuracy
1
Wax Pattern
Inject wax into a metal die — produces an exact wax replica of the
finished part
2
Tree Assembly
Multiple wax patterns attached to a central wax sprue forming a 'tree'
3
Shell Building
Tree dipped in ceramic slurry, stuccoed with refractory sand — repeated
5–15 times
4
Dewaxing
Steam autoclave melts and removes the wax — leaving a hollow ceramic
shell
5
Shell Firing
Kiln burns residual wax, sinters ceramic — shell is now rigid and ready for
pouring
6
Pouring
Molten metal poured into pre-heated shell — ceramic conforms exactly
to wax surface
7
Shell Removal
Ceramic shell broken away; parts cut from tree, finished, inspected
Why Investment Casting?
•
Best surface finish of any casting process — Ra 1.6–3.2 μm
•
Tightest tolerances — ±0.1–0.25mm on small features
•
Almost any alloy, including superalloys and reactive metals
•
Complex geometry, thin walls, undercuts — often without cores
•
Applications: turbine blades, medical implants, firearm parts,
jewelry
Other Casting Processes
Permanent Mold: Gravity pour into reusable metal mold — better
finish than sand, limited alloys
Centrifugal: Rotating mold distributes metal outward — used for pipes,
rings, tubes; dense outer surface
Continuous Casting: Molten steel/aluminum solidified continuously
into slabs and billets — dominant process for structural steel

## Slide 11
Common Casting Defects — Recognition and Detection
Defect
Cause
Appearance
Likely Location
Detection
Shrinkage Porosity
Insufficient feed metal; poor riser
design or placement
Irregular, rough-surfaced spongy
voids
Thick sections; last to solidify
RT, UT
Gas Porosity
Dissolved hydrogen expelled during
solidification; moisture in mold
Smooth, spherical voids —
distributed or clustered
Throughout casting or near
surface
RT, UT
Hot Tears
Mold restrains contracting casting
during solidification
Irregular branching cracks with
oxidized surfaces
Section changes, sharp corners
VT, PT, MT
Cold Shuts
Two metal streams meet but too
cold to fuse; low pouring temp
Linear seam with smooth
oxidized surface
Mid-section; opposite ingate
VT, PT
Misrun
Metal solidifies before filling mold;
thin section or low temp
Incomplete casting — smooth
rounded edges at termination
Thin sections; far from ingate
VT
Inclusions
Sand, slag, or oxide entrained
during pouring
Irregular hard spots; dark
irregular RT indications
Near gates; upper mold
surfaces
RT, UT
Warping
Non-uniform cooling; residual
thermal stress
Dimensional distortion — not
visible as a crack or void
Long flat sections
Dimensional

## Slide 12
Casting Process Selection — Five Factors, One Right Answer
Factor
Sand Casting
Die Casting
Investment Casting
Alloy
Any metal — steel, cast iron,
aluminum, copper, superalloys
Lower-melting only — Al, Zn, Mg,
Cu; NOT steel or cast iron
Almost any — including superalloys and reactive
metals
Part Size
Virtually unlimited — from grams
to hundreds of tonnes
Limited by machine capacity —
typically under 25 kg
Typically under 50 kg; best for small to medium
precision parts
Production Volume
Low to medium — tooling cost
low; each mold is single-use
High volume only — die cost (tens
of $K) must be amortized
Low to medium — ceramic shell is single-use but
patterns are reusable
Tolerance & Finish
Rough — Ra 6–25 μm; tolerances
±1–3 mm on large parts
Good — Ra 0.8–3.2 μm;
tolerances ±0.1–0.3 mm
Best — Ra 1.6–3.2 μm; tolerances ±0.1–0.25 mm
on small features
Internal Geometry
Excellent — sand cores create
complex internal passages
Limited — no sand cores; some
complexity with die slides
Good — many undercuts possible without cores;
shell broken away

## Slide 13
Technician's Perspective
Reading the defect — what it tells you about how the casting was made.
Red Flag: Die casting ordered for a 304 stainless steel bracket
A job order specifies die casting for a 304 stainless steel structural bracket. Do not proceed — die casting cannot be used for stainless steel. The
steel die cannot withstand the pouring temperature of stainless (above 1400°C), and the metal would freeze before filling the die. Die casting is
limited to aluminum, zinc, magnesium, and copper alloys. Correct the process specification: investment casting or sand casting are the appropriate
processes for this part.
Caution: Specifying RT on a die casting to find internal defects
A die cast aluminum housing is being evaluated for a pressure-tight application. RT reveals no defects — do not accept this as proof of soundness.
Die castings inherently contain gas porosity from air trapped during high-velocity injection; this porosity is often fine, distributed, and below RT
detection sensitivity. UT is more sensitive to this type of defect. Additionally, confirm the application: die cast parts with this porosity may blister if
subsequently heat treated. Consult the applicable specification before accepting.
Good Practice: Identifying hot tears vs. cold cracks by oxidation
A cracking indication is found on a sand casting at a thick-to-thin section change. To distinguish a hot tear from a cold crack: hot tears form during
solidification when the metal is still partly liquid — the fracture surfaces are oxidized (dark, discolored) because they were exposed to atmosphere
at high temperature. Cold cracks form after solidification — the surfaces are clean and metallic. An oxidized crack surface at a stress-concentration
point is a hot tear and indicates a casting design or mold restraint issue that must be corrected before re-casting.

## Slide 14
Core Question Answers
What happens during solidification and why does it matter for casting quality?
Solidification starts at the mold wall (chill zone), progresses inward as columnar dendrites, and finishes in the equiaxed center — the last zone to solidify
is where shrinkage voids, gas porosity, and segregation concentrate. Riser design, chill placement, and pouring temperature control where and when
solidification occurs, and therefore where defects form.
What are the main casting processes and what are the trade-offs between them?
Sand casting: any alloy and size, low tooling cost, rough surface. Die casting: high pressure, excellent finish, limited to lower-melting alloys, high tooling
cost, gas porosity inherent. Investment casting: ceramic shell over wax pattern, best surface finish and accuracy, any alloy, expensive per part, limited to
smaller components.
What defects are most common in castings and how is each one recognized?
Shrinkage porosity: irregular rough voids in thick sections (RT, UT). Gas porosity: smooth spherical voids (RT, UT). Hot tears: branching oxidized cracks at
section changes (VT, PT, MT). Cold shuts: smooth linear seam where metal streams didn't fuse (VT, PT). Misrun: incomplete casting with rounded smooth
edge (VT). Inclusions: hard spots with irregular RT indications (RT, UT).
How do you choose the right casting process for a given application?
Five factors together: alloy (die casting cannot handle steel; investment casting handles superalloys), part size (sand for large, die for small), production
volume (die only justified at high volume), required surface finish and tolerance (investment for precision), and internal geometry complexity (sand with
cores for complex passages).

## Slide 15
Key Takeaways — Week 10: Casting Processes & Defect Recognition
1
Solidification is not instantaneous or uniform — shrinkage, gas evolution, segregation, and dendrite growth occur
simultaneously, and controlling them through riser design, chilling, and pouring practice is what separates a sound casting
from a defective one.
2
Sand casting, die casting, and investment casting each occupy a distinct niche defined by alloy, size, volume, tolerance,
and cost — selecting the wrong process for an application leads to either excessive cost or unacceptable quality, and a
technician who understands why a process was chosen can anticipate where defects are most likely.
3
Casting defects are predictable from the process — shrinkage porosity in thick sections, gas porosity in die castings, hot
tears at section changes, cold shuts at ingate-remote locations. A technician who understands how a casting was made
focuses inspection effort accordingly and interprets indications in the context of the manufacturing process.

## Slide 16
Resources & What's Next
Week 10 Resources
Kalpakjian Ch. 10 & 11
Fundamentals of Metal Casting & Metal Casting Processes — primary
reading
Casting Defects — TWI
Defect library with photographs and NDT detection guidance for each defect
type
Solidification Visualizer
Dendrite growth, riser design, and solidification sequence — interactive
Sand Casting Visualizer
Process animation, design guidelines, and common defects — interactive
Die & Investment Casting
NADCA and ICI process animations with design and defect coverage —
interactive
Week 11 — Metal Forming
November 2, 2026 · Unit 4: Manufacturing continues
•
Hot working vs. cold working — the recrystallization
temperature and why it defines the boundary
between the two
•
Work hardening — how dislocations accumulate
during cold working and how annealing restores
ductility
•
Rolling, forging, extrusion, and drawing — what each
process produces and where it is used
•
Grain flow in forgings — why a forged part
outperforms a casting or a machined bar in critical
applications
•
Forming defects — laps, seams, bursts, pipe defects,
and delamination and how each is detected