## Slide 1
M E C H 1 9 1 — M e t a l l u r g y
Week 11
Metal Forming Processes
November 2, 2026 · 5:00 – 7:30 PM · Kai Santos

## Slide 2
Class Agenda
01
Hot & Cold Working + Work Hardening
Recrystallization temperature as the boundary between hot and cold working; how dislocations
accumulate, strengthen, and are removed by annealing
02
Rolling, Forging, Extrusion & Drawing
The four major forming processes — what each produces, where each is used, and what makes forgings
the highest-integrity formed part
03
Grain Flow & Forming Defects
Why grain flow gives forgings superior fatigue performance, and the characteristic defects of each
forming process and how to detect them

## Slide 3
Metallography Lab — Module 10
EXAMET-5-R-600-HD · 50–500×
Module 10 · Week 11
Aluminum Alloys for Forming
What to do this week:
Compare precipitate presence (G, heat-treatable) vs. absence (I, solid-
solution only) at 500×.
Steps:
1 Observe — complete feature table
2 Sketch — label magnification & specimen
3 Answer — 4 short questions
Specimens to Check Out
· Specimen G — 6061-T6 aluminum (revisit)
· Specimen I — 5086 aluminum
How to check out the kit:
1 See instructor after class today
2 Sign out the specimen tray
3 Use the EXAMET-5 at your convenience
4 Return kit before leaving class
5 Submit completed module with your portfolio
Portfolio Handout — Module 10

## Slide 4
MECH 191 — Course & Unit Roadmap
Unit 1
Materials Fundamentals
Wk 1
Aug 24
Atomic Structure
& Bonding
Wk 2
Aug 31
Mechanical
Properties
Unit 2
Steel & Alloys
Wk 4
Sep 14
Carbon &
Alloy Steels
Wk 5
Sep 21
Stainless &
Cast Irons
Wk 6
Sep 28
Nonferrous &
Phase Diagrams
Unit 3
Testing & Quality
Wk 7
Oct 5
Mechanical
Testing
Wk 8
Oct 12
NDT Methods
Wk 9
Oct 19
Quality
Standards
Unit 4
Manufacturing
Wk 10
Oct 26
Casting
Wk 11 ← here
Nov 2
Forming
Wk 12
Nov 9
Machining
Wk 13
Nov 16
Powder
Metallurgy
Unit 5
Joining & Failure
Wk 14
Nov 23
Welding
Processes
Wk 15
Nov 30
Weld Metallurgy
& Failure
Wk 16
Dec 7
Corrosion
& Wrap-up
Week 17 · FINAL EXAM

## Slide 5
Week 11 — At a Glance
Topics
•
Hot working vs. cold working — recrystallization temperature as the
boundary; why hot working prevents work hardening and cold working
enables it
•
Work hardening — dislocation accumulation, anisotropy, strain aging,
and the three stages of annealing: recovery, recrystallization, grain
growth
•
Rolling — flat rolling, shape rolling, hot vs. cold rolling, and
characteristic rolling defects
•
Forging — open die vs. closed die, flash, grain flow, and why forgings
outperform castings and machined bar in fatigue and impact
•
Extrusion & drawing — direct vs. indirect extrusion, wire and tube
drawing, deep drawing, and the characteristic defects of each
•
Forming defects — laps, seams, bursts, pipe defects, delamination,
chevron cracking, and NDT detection methods for each
Resources
Reference Material
Kalpakjian Ch. 13, 14 & 15
Rolling · Forging · Extrusion & Drawing
Visualizers
Hot vs Cold Working & Work Hardening
Forging — FIA Design & Grain Flow
Extrusion — AEC Design & Animation
Forming Defects & Process Comparison
Forming Limit Diagrams
Also Covers
Tube & Pipe Drawing — TPA Manufacturing
Next: Week 12 — Machining

## Slide 6
Core Questions
Try to answer these before we dive in — we'll revisit them with answers at the end of class.
1
What is the difference between hot working and cold working, and why does it matter?
2
What is work hardening and how does it affect the strength, ductility, and residual stress of a formed part?
3
What are the main forming processes and what does each one produce?
4
What is grain flow and why does it give a forged part superior performance compared to a casting or machined
bar?
5
What defects are unique to forming processes and how is each one detected?

## Slide 7
Hot vs. Cold Working — Recrystallization Temperature is the Boundary
Trex
≈ 0.4Tm
Hot Working (above Trex)
No work hardening
Continuous recrystallization annihilates dislocations as fast as they
form — large reductions in a single pass without cracking
Lower flow stress
Less force required — enables shaping of large cross-sections
(structural plate, rail, ship plate)
Recrystallized grain structure
Final grain size controlled by finishing temperature and reduction;
finer finishing = finer grains
Scale formation
Oxidation at high temperature produces mill scale — must be
removed (pickling) before cold finishing
Inferior tolerance & finish
Thermal expansion variation and scale give rough surface; ±1–3
mm typical for hot rolled plate
Cold Working (below Trex)
Work hardening
Dislocations accumulate — strength and hardness increase,
ductility decreases with each pass; eventually must anneal
Better surface finish
No scale, less thermal distortion — achieves Ra 0.8–3.2 μm and
±0.1 mm dimensional tolerances
Residual stress
Compressive stress at surface (beneficial for fatigue resistance);
tensile stress in the interior
Annealing required
When ductility is exhausted, intermediate annealing restores
formability through recrystallization
Warm working
Between room temp and Trex — partial recovery without full
recrystallization; compromise for Al and some steels

## Slide 8
Work Hardening — Dislocations as Both Problem and Tool
Cold Work
Dislocations
accumulate
at
grain boundaries — strength ↑,
ductility ↓
Taylor hardening: σ √ρ
∝
Metal becomes too brittle for
further forming
Recovery
Low-temperature
anneal:
residual
stress
reduced,
dislocation tangles reorganize
Strength largely retained
Exploited
in
stress-relief
annealing
Recrystallization
New strain-free grains nucleate
at high-dislocation sites
Strength returns to annealed
level — ductility restored
Grain size depends on degree
of cold work and annealing
temperature
Grain Growth
At higher temperatures or
longer times: grains grow to
reduce boundary area
Excessive grain growth reduces
strength and toughness
Controlled
by
annealing
temperature and time
›
›
›
Anisotropy
Cold working creates crystallographic texture —
grains rotate to align with working direction; part is
stronger and less ductile in the working direction
than perpendicular to it
Strain Aging
In low-carbon steels: interstitial C and N atoms
diffuse to dislocations after cold working, pinning
them — raises yield strength but causes Lüders
bands (stretcher strains) on deep-drawn sheet
steel
Deliberate Strengthening
Controlled cold work is used to strengthen wire,
spring, and structural members without alloying or
heat treatment — specifying the % reduction in
area controls the final strength level

## Slide 9
Rolling — The Highest-Volume Forming Process
Hot Rolling
•
Continuously cast slab reheated above Trex → successive rolling
stands reduce thickness progressively
•
Finishing temperature controls final grain size — lower finish
temp = finer grains = better properties
•
Blue-gray mill scale surface; rough tolerance ±1–3 mm; used for
structural plate, beam, rail, pipe
•
Shape rolling: specially shaped rolls produce I-beams, channels,
angles in a single pass sequence
Cold Rolling
•
Hot rolled strip pickled (acid cleaned to remove scale) → cold
rolled to final gauge
•
Bright, smooth surface; tight thickness tolerance ±0.05 mm;
strong in rolling direction
•
Final batch or continuous anneal restores ductility for deep
drawing (automotive panels, cans)
•
Ring rolling: thick-walled ring reduced in cross-section and
expanded in diameter — seamless bearing rings, flanges with
circumferential grain flow
Rolling Defects
Edge Cracking
Edges cool faster in hot rolling → tensile stress at roll exit → edge cracks;
insufficient ductility at cooler edges. Detected: VT
Alligatoring
Severe internal cracking during hot rolling of billets with poor ductility —
top and bottom surfaces separate like a mouth opening. Detected: VT
Wavy Edges / Center Buckle
Non-uniform thickness across width from roll bending — one edge or the
center is thicker, causing flatness defects in sheet. Detected: dimensional
Laps & Seams
Metal folds back on itself at the edges during rolling — linear surface
indications parallel to rolling direction; fatigue crack initiation sites.
Detected: MT, PT
Pipe (Lamellar Defect)
Ingot shrinkage void drawn out into a central planar defect during primary
rolling — dangerous under through-thickness load in welded connections.
Detected: UT

## Slide 10
Forging & Grain Flow — Highest-Integrity Forming Process
Open Die Forging
Metal compressed between flat or simple shaped dies — flows freely
laterally. Used for very large components (shafts up to 100 tonnes,
discs, rings) and for breaking down ingot structure. Requires skilled
operator to control shape progression. Produces a worked, refined
microstructure throughout the cross-section.
Closed Die (Impression Die) Forging
Metal compressed in a die cavity machined to the part shape — metal
fills the cavity and excess escapes as flash at the parting line. Flash
builds back-pressure to completely fill the die before escaping; trimmed
after forging. Produces near-net-shape with excellent grain flow and
dimensional consistency.
Flash: the thin fin squeezed out at the die parting line — a functional
feature, not a defect. Its resistance to flow forces complete die fill.
Grain Flow — Why Forgings Win
What grain flow is
Grains elongate and align in the direction of metal flow during forging — a
fiber-like structure analogous to wood grain. Revealed by etching a cross-
section with acid.
Why it matters
A well-designed die orients grain flow to follow the part contour and
resist primary service loads. Grain flow aligned with load path = maximum
fatigue and impact resistance.
vs. machined bar
A part machined from bar stock has grain flow running straight through —
the grain cuts across the critical geometry. A forging wraps the grain
around the shape.
vs. casting
Castings have no grain flow — random, equiaxed grains with no preferred
orientation. Forgings outperform equivalent castings in fatigue life by
factors of 2–5×.
Laps: the failure mode
If the die causes metal to fold back on itself, the grain flow creates a plane
of weakness — a lap. A folded grain flow is always rejectable in fatigue-
loaded components.

## Slide 11
Extrusion & Drawing — Continuous and Pulled Product
Direct (Forward) Extrusion
Ram pushes heated billet through die — extrude exits in direction of
ram travel. High container friction; most common type. Extrusion ratio
10:1 to 100:1 for aluminum. Produces rods, tubes, angles, and complex
constant-cross-section profiles. Al at 400–500°C; steel at 1100–1250°C
with glass or graphite lubricant.
Indirect (Backward) Extrusion
Die moves into the stationary billet — no relative movement between
billet and container wall. Lower friction, more uniform deformation.
Used for precise profiles and difficult alloys (superalloys, titanium). Cold
impact extrusion: aluminum, copper, soft steels at room temperature
— produces thin-walled tubes and cups.
Wire, Tube & Deep Drawing
•
Wire drawing: rod pulled through progressively smaller dies —
15–25% reduction per die; intermediate annealing for large total
reductions
•
Tube drawing: mandrel controls internal diameter — tight-
tolerance seamless tubing for hydraulic and medical applications
•
Deep drawing: sheet blank drawn into cup by punch —
automotive panels, beverage cans; requires good ductility and
appropriate crystallographic texture
•
Drawing is compressive die + tensile pull — distinguished from
extrusion (compressive only)
Extrusion & Drawing Defects
Pipe (Extrusion): Oxide from billet surface drawn into extrude center
near billet end — every extrusion back-end is cropped. UT detects.
Fir Tree Cracking: Periodic transverse surface cracks at die exit —
excessive extrusion speed or temperature. VT detects.
Chevron / Center Burst: Internal cracks along centerline — excessive
hydrostatic tension in drawing or extrusion deformation zone. UT, RT
detects.

## Slide 12
Forming Defects — Process, Cause, and Detection
Defect
Process
Cause
Location
Detection
Laps
Rolling, Forging
Metal folds back on itself at surface
Surface, parallel to working
direction
MT, PT
Seams
Rolling
Surface cracks from ingot closed but
not welded
Surface, parallel to rolling
direction
MT, PT
Bursts
Forging, Extrusion
Tensile stress in deformation zone
exceeds ductility
Internal, linear
UT, RT
Pipe
Rolling, Extrusion
Ingot shrinkage void drawn to
center
Central, linear or planar
UT
Delamination
Rolling
Pipe or inclusions separate under
through-thickness load
Internal, planar
UT
Chevron Cracking
Drawing, Extrusion
Hydrostatic tension at centerline
Centerline, internal
UT, RT
Orange Peel
Cold Working
Coarse grain deforms non-uniformly
Surface
VT

## Slide 13
Technician's Perspective
Knowing the process tells you where to look and what you're looking for.
Red Flag: Rolled plate accepted for a welded T-joint without UT
Plate passes VT and MT — no rejectable indications. It is welded into a T-joint with through-thickness tensile stress. The plate later delaminates at
the weld. MT and PT cannot see lamellar pipe defects lying parallel to the plate surface. All rolled plate used in through-thickness-loaded
connections must be UT-tested for lamellar defects before fabrication. This is a code requirement, not optional.
Caution: Linear MT indication on a forged crankshaft — orientation matters
MT reveals a linear indication in the crankpin fillet. Before disposition: determine orientation relative to grain flow. Parallel to grain flow = less
critical than transverse — a cross-grain crack cuts across fibers rather than following them. Read the etch pattern to establish grain flow direction,
then evaluate. Orientation does not eliminate the need to evaluate against acceptance criteria, but it determines urgency and disposition.
Good Practice: Linear PT indications on drawn hydraulic tube — reject, don't size
PT on drawn hydraulic tubing reveals linear indications parallel to the tube axis. Could be seams (ingot surface defects) or laps (metal folding during
drawing) — both are rejectable in pressure-rated tubing. The technician does not size them against acceptance limits. Any linear surface indication
parallel to the axis concentrates hoop stress from internal pressure and is a fatigue initiation site. Surface quality is part of the process release
criteria — not an afterthought.

## Slide 14
Core Question Answers
What is the difference between hot working and cold working, and why does it matter?
The boundary is the recrystallization temperature (~0.4Tm). Hot working: continuous recrystallization prevents work hardening — large reductions without
cracking, recrystallized equiaxed grain structure, inferior surface finish. Cold working: dislocations accumulate — strength increases, ductility decreases, better
surface finish, annealing required when ductility is exhausted.
What is work hardening and how does it affect a formed part?
Plastic deformation accumulates dislocations; as they tangle and pile up, further movement becomes harder — strength and hardness increase, ductility
decreases. The part has anisotropic properties (stronger in working direction), residual compressive surface stress (good for fatigue), and loses its work-
hardened strength if heated above the recrystallization temperature.
What are the main forming processes and what does each produce?
Rolling: passes slab between rolls — plate, sheet, strip, structural sections. Forging: compressive force through dies — highest-integrity parts (crankshafts,
flanges, aircraft structure). Extrusion: forces through die opening — constant cross-section profiles (Al extrusions). Drawing: tensile pull through die — wire,
tube, bar at tight tolerances.
What is grain flow and why does it give a forged part superior performance?
Forging elongates and aligns grains in the direction of metal flow — a fiber-like structure. A well-designed die orients grain flow to follow the part contour and
resist service loads. This gives forgings 2–5× better fatigue life than equivalent castings (no grain flow) or machined bar (grain flow cuts across the geometry).
What defects are unique to forming processes and how is each detected?
Laps and seams: surface linear defects parallel to working direction — MT, PT. Bursts: internal cracks from excessive tensile stress in forging or extrusion — UT,
RT. Pipe: ingot shrinkage void drawn to center of rolled or extruded product — UT. Delamination: pipe or inclusions separating under through-thickness load in
rolled plate — UT. Chevron cracking: centerline cracks in drawing/extrusion — UT, RT.

## Slide 15
Key Takeaways — Week 11: Metal Forming Processes
1
Hot working and cold working produce fundamentally different microstructures and properties — hot working refines grain
structure through recrystallization while cold working strengthens through dislocation accumulation; the choice between them
determines final mechanical properties as much as the alloy composition does. The boundary is recrystallization temperature,
not whether the metal feels hot.
2
Grain flow in forgings is a deliberate microstructural feature that gives forged components superior fatigue and impact
resistance compared to castings or machined bar — grain flow should follow the part contour and resist the primary service
loads. A technician who can read a grain flow etch pattern can assess whether a forging die was designed correctly, and can
recognize a lap as a plane of weakness rather than just a surface mark.
3
Every forming process produces its own characteristic defects — laps and seams in rolling and forging, pipe defects in rolled
plate and extrusion, center bursts in drawing, delamination in welded rolled plate connections — and a technician who
understands the process can anticipate where to look, what the defect looks like, and which NDT method will find it.

## Slide 16
Resources & What's Next
Week 11 Resources
Kalpakjian Ch. 13, 14 & 15
Rolling of Metals · Forging · Extrusion & Drawing — primary reading
Hot vs Cold Working Visualizer
Work hardening curve, recrystallization stages, annealing effects —
interactive
Forging Visualizer
FIA design guidelines, grain flow animation, open vs. closed die —
interactive
Extrusion Visualizer
AEC design guidelines, direct vs. indirect extrusion animation — interactive
Forming Defects Visualizer
Process comparison and defect recognition for each forming process —
interactive
Week 12 — Machining
November 9, 2026 · Unit 4: Manufacturing continues
•
What happens at the cutting zone — shear plane,
chip formation, heat generation, and surface integrity
•
Turning, milling, drilling, and grinding — what each
produces and what surface finish each achieves
•
Cutting tool materials — HSS, cemented carbide,
coatings, ceramics, CBN, and PCD
•
Surface finish parameters — Ra, Rz, and why surface
roughness affects fatigue, sealing, and wear
•
Machining defects — built-up edge marks, chatter,
grinding burn, and recast layer in EDM