## Slide 1
M E C H 1 9 1 — M e t a l l u r g y
Week 12
Machining
November 9, 2026 · 5:00 – 7:30 PM · Kai Santos

## Slide 2
Class Agenda
01
The Cutting Zone & Machining Processes
Shear plane, chip types, heat generation, and surface integrity — then turning, milling, drilling, and
grinding
02
Cutting Tool Materials
HSS to CBN — hardness, heat resistance, toughness, coatings, and how to choose the right tool for the
job
03
Surface Finish, Integrity & Machining Defects
Ra, Rz, residual stress, grinding burn, machining cracks, chatter — and how to detect each one

## Slide 3
Metallography Lab — Module 11
EXAMET-5-R-600-HD · 50–500×
Module 11 · Week 12
Machining
What to do this week:
Examine near-surface grain condition at 500×. Identify any subsurface
deformation from sectioning.
Steps:
1 Observe — complete feature table
2 Sketch — label magnification & specimen
3 Answer — 4 short questions
Specimens to Check Out
· Specimen A — 1018 steel
· Specimen B — 1045 steel
· Specimen G — 6061-T6 aluminum
How to check out the kit:
1 See instructor after class today
2 Sign out the specimen tray
3 Use the EXAMET-5 at your convenience
4 Return kit before leaving class
5 Submit completed module with your portfolio
Portfolio Handout — Module 11

## Slide 4
MECH 191 — Course & Unit Roadmap
Unit 1
Materials Fundamentals
Wk 1
Aug 24
Atomic Structure
& Bonding
Wk 2
Aug 31
Mechanical
Properties
Unit 2
Steel & Alloys
Wk 4
Sep 14
Carbon &
Alloy Steels
Wk 5
Sep 21
Stainless &
Cast Irons
Wk 6
Sep 28
Nonferrous &
Phase Diagrams
Unit 3
Testing & Quality
Wk 7
Oct 5
Mechanical
Testing
Wk 8
Oct 12
NDT Methods
Wk 9
Oct 19
Quality
Standards
Unit 4
Manufacturing
Wk 10
Oct 26
Casting
Wk 11
Nov 2
Forming
Wk 12 ← here
Nov 9
Machining
Wk 13
Nov 16
Powder
Metallurgy
Unit 5
Joining & Failure
Wk 14
Nov 23
Welding
Processes
Wk 15
Nov 30
Weld Metallurgy
& Failure
Wk 16
Dec 7
Corrosion
& Wrap-up
Week 17 · FINAL EXAM

## Slide 5
Week 12 — At a Glance
Topics
•
The cutting zone — shear plane, primary and secondary deformation
zones, chip types, heat distribution, and surface integrity
•
Turning and milling — single-point vs. multi-tooth cutting, operations
produced, surface finish formula, up vs. down milling
•
Drilling and grinding — twist drill geometry, hole tolerance, grinding
wheel types, grinding burn, and dressing
•
Cutting tool materials — HSS, cemented carbide, coatings (TiN, TiAlN),
ceramics, CBN, PCD, and selection criteria
•
Surface finish — Ra and Rz parameters, typical values by process,
connection to fatigue and sealing performance
•
Machining defects — built-up edge, chatter, grinding burn (re-temper
and re-hardening), machining cracks, and recast layer in EDM
Resources
Reference Material
Kalpakjian Ch. 21, 22 & 23
Fundamentals of Cutting · Tool Materials ·
Machining Processes
Visualizers
Cutting & Chip Formation
Turning & Milling — Sandvik Coromant
Calculators
Surface Finish
Ra = f² / (8r) · feed & nose radius control
roughness in turning
Next: Week 13 — Powder Metallurgy

## Slide 6
Core Questions
Try to answer these before we dive in — we'll revisit them with answers at the end of class.
1
What happens at the cutting zone during machining and why does it matter for part quality?
2
What are the main machining processes and what does each one produce?
3
What are the main cutting tool materials and how do you choose between them?
4
How is surface finish measured and why does it matter for performance?
5
What machining-related defects should a technician know how to recognize and detect?

## Slide 7
The Cutting Zone — Where Dimensions and Surface Integrity Are Made
Three Deformation Zones
1
Primary Shear Zone
Chip forms along the shear plane ahead of the tool tip — most
of the cutting energy consumed here. Severe plastic
deformation; temperatures to 400–700°C.
2
Secondary Deformation Zone
Tool-chip interface — friction between chip and tool rake face
generates significant heat. Drives tool wear and built-up edge
formation at low speeds.
3
Tertiary Zone
Tool flank rubbing the new machined surface — contributes to
work hardening and residual stress. Source of white layer
damage if tool is worn.
Heat distribution: chip carries ~75–80% of cutting heat away from the
part — which is why good chip control and coolant matter for surface
integrity.
Chip Types & Cutting Parameters
Continuous Chip
Ductile materials at high speed with sharp tools — smooth ribbon; best
surface finish. Chip control is a safety concern; chip breakers used.
Discontinuous Chip
Brittle materials (cast iron) or low speed — segments break off easily.
Easier to control but may produce rougher surface.
Built-Up Edge (BUE)
Workpiece material welds to tool rake face at low speed — BUE fractures
and adheres to machined surface; torn, rough finish. Prevented by
increasing speed or improving lubrication.
Cutting Parameters
Cutting speed (Vc): Velocity of workpiece surface vs. tool (m/min) — higher
speed → more heat, better finish above threshold
Feed (f): Tool advance per revolution or per tooth — controls chip thickness and
surface roughness directly
Depth of cut (ap): Radial/axial depth per pass — controls material removal rate
and cutting force

## Slide 8
Turning & Milling — Single Point and Multi-Tooth Cutting
Turning
How it works
Workpiece rotates; single-point tool traverses — each revolution
removes a helical chip strip
Operations
External turning (reducing diameter), facing (flat end face), boring
(enlarging bore), threading, grooving, parting
Surface finish
Theoretical Ra = f² / (8r) — finer feed and larger nose radius give
smoother surface; finish turning achieves Ra 0.8–3.2 μm
Typical Ra values
Rough turning: 6.3–25 μm · Finish turning: 0.8–3.2 μm · Precision
turning: 0.2–0.8 μm
CNC turning centers
Combine turning, milling, drilling in one setup — reduces handling,
improves dimensional consistency for complex rotational parts
Milling
How it works
Rotating multi-tooth cutter removes material — each tooth takes a
small chip per revolution; workpiece feeds past the cutter
Face milling
Large diameter cutter with inserts facing workpiece — generates
flat surfaces on large areas; highly productive
End milling
Smaller cutter for slots, pockets, contours, and complex 3D
surfaces — the workhorse of CNC machining centers
Up vs. Down milling
Up (conventional): chip starts thin, increases — less sensitive to
backlash. Down (climb): chip starts thick, decreases — better finish,
compressive surface residual stress, preferred on CNC
Surface finish
Finish milling: Ra 0.8–3.2 μm · Down milling produces
compressive residual stress — beneficial for fatigue life

## Slide 9
Drilling & Grinding — Holes and Finest Finishes
Drilling
•
Two helical flutes carry chips out; two cutting edges at 118° point
angle (135° for harder materials and stainless)
•
Drilled hole: Ra 1.6–6.3 μm; tolerance H12–H13 — rough; follow
with reaming (sizing) or boring (single-point) for precision bores
•
Peck drilling: drill withdrawn periodically to break chips — used for
deep holes to prevent chip packing and overheating
•
Common errors: drill wandering at entry (use center drill first); work
hardening at hole entrance in stainless (use sharp tools, adequate
feed, no rubbing); BUE in aluminum (sharp HSS or uncoated carbide
with cutting oil)
Grinding Types
Surface: Flat reference surfaces on
precision components
Cylindrical: External diameters —
shafts, bearing journals
Internal: Precision bores — hydraulic
cylinders, bearing housings
Centerless: High-volume bar and
tube — no centers required
Grinding Burn — The Most Serious Grinding Defect
Occurs when heat at the grinding zone exceeds the material's capacity to
dissipate it — surface temperature rises above the tempering temperature
of hardened steel.
Re-tempering Burn
Surface heated above tempering temperature — locally softened.
Appears as dark band on Nital etch. Tensile residual stress introduced.
Reduces fatigue life.
Re-hardening Burn
Surface heated above austenitising temperature then quenched by the
bulk — untempered martensite white layer forms. Very brittle, high
tensile residual stress. Most damaging type.
Detection
Grinding cracks: MT or PT — always reject in critical components. Burn: Nital
etch (acid reveals re-tempered/re-hardened zones) or Barkhausen noise
analysis. Wheel dressing restores sharpness and prevents burn from glazed
wheels.

## Slide 10
Cutting Tool Materials — From HSS to CBN
High Speed Steel (HSS)
Tough · Resharpened · 600°C
max
Most versatile tool material
— excellent toughness
handles interrupted cuts.
Suitable for complex
geometries (drills, taps, form
tools). Softens above ~600°C
— limited to moderate
cutting speeds. Used where
toughness matters more
than speed.
Cemented Carbide
Hard · Fast · Indexed inserts
Most widely used for
production machining —
significantly harder and
more heat-resistant than
HSS; allows much higher
cutting speeds. Used as
indexable inserts that are
replaced rather than
resharpened. Grades tailored
to specific workpiece
materials (P for steel, M for
stainless, K for cast iron).
Coatings (TiN, TiAlN, Al₂O₃)
CVD/PVD · Wear resistant · Low
friction
Deposited on carbide inserts
— extend tool life 3–10× by
reducing wear and friction.
TiN (gold) is general
purpose; TiAlN is superior at
high temperatures; Al₂O₃ for
high-speed steel machining.
The familiar gold color of
coated drills and inserts. Do
not confuse coating type
with base material.
Ceramics (Al₂O₃, Si₃N₄)
Very hard · High-speed
finishing
Used for high-speed finishing
of hardened steels and cast
irons where carbide wear is
excessive. Extremely hard
and heat-resistant but brittle
— sensitive to interrupted
cuts and vibration. Not
suitable for general
machining; specialist
finishing tool.
CBN & PCD
Hardest tools · Precision
finishing
CBN (cubic boron nitride) for
hardened steels and
superalloys — machines
materials carbide cannot.
PCD (polycrystalline
diamond) for non-ferrous
metals and composites —
extreme hardness and tool
life but cannot machine
ferrous materials (carbon
diffusion at cutting
temperature). Both are used
for high-precision finishing.

## Slide 11
Surface Finish & Surface Integrity — More Than Just Ra
Roughness Parameters & Typical Values by Process
Ra (arithmetic mean roughness) — average deviation of profile from mean line;
most widely specified parameter; lower Ra = smoother surface.
Rz (mean roughness depth) — average peak-to-valley height over several
sampling lengths; more sensitive to deep valleys; more relevant for fatigue and
sealing applications.
Process
Ra Range
Sand casting
6.3 – 25 μm
Hot rolling
12.5 – 50 μm
Rough turning/milling
3.2 – 12.5 μm
Finish turning/milling
0.8 – 3.2 μm
Grinding
0.025 – 0.8 μm
Lapping / Honing
0.012 – 0.4 μm
Surface Integrity
Surface integrity is broader than surface finish — it
encompasses roughness, residual stress state, work
hardening depth, and microstructural alteration. Specified
for fatigue-critical aerospace, power generation, and
medical components.
Compressive Residual Stress
Sharp tools, adequate coolant, down milling —
compressive surface stress; beneficial for fatigue life. Shot
peening deliberately introduces deep compressive stress
after machining.
Tensile Residual Stress
Worn tools, excessive heat, aggressive grinding — tensile
surface stress; dramatically reduces fatigue life. The
primary damage mechanism in grinding burn.
Why Surface Finish Matters
Ra on a drawing is an engineering requirement, not an
aesthetic — stress concentrations at surface peaks reduce
fatigue life; rough bores leak; rough bearing surfaces wear
rapidly.

## Slide 12
Machining Defects — Recognition and Detection
Defect
Cause
Appearance
Location
Detection
Action
Built-Up Edge
Marks
Workpiece material welds onto tool
rake face at low speed — BUE
fractures and adheres to machined
surface
Torn, rough patches on machined
surface; inconsistent surface
finish
All over machined
surface
VT
Increase cutting speed; use appropriate
lubricant; replace dull tool
Chatter Marks
Vibration between tool and
workpiece — tool overhang, fixture
rigidity, or cutting parameter issue
Regular wave-like pattern on
machined surface; audible during
machining
Machined surface,
oriented perpendicular
to cutting direction
VT, profilometer
Reduce tool overhang; improve fixturing;
adjust cutting parameters
Grinding Burn /
Cracks
Insufficient coolant or aggressive
grinding parameters — surface
temperature exceeds tempering
point
Discoloration (burn); network of
fine cracks perpendicular or
cross-hatch pattern
Machined surface —
often invisible without
etching
MT, PT; Nital etch
(dark/white zones);
Barkhausen noise
Reduce grinding depth/speed; improve
coolant; dress wheel
Chatter Cracks /
Machining
Cracks
Severe thermal or mechanical
conditions — most common in
hardened steels during grinding
Fine cracks perpendicular to
grinding direction or in a cross-
hatch pattern
Ground surface of
hardened components
MT or PT — always a
reject condition in
critical components
Reduce aggressiveness; correct coolant
delivery; use softer wheel grade
Recast Layer
(EDM)
EDM melts and re-solidifies thin
surface layer — contains tensile
residual stress and untempered
martensite
White layer on cross-section
metallography; no surface VT
indication
All EDM-machined
surfaces
Metallography (cross-
section); Nital etch
Finish grind or polish to remove white
layer in fatigue-critical applications

## Slide 13
Technician's Perspective
Cutting parameters are quality parameters — not just productivity parameters.
Red Flag: Ground hardened shaft passes VT — but Nital etch reveals dark bands
A hardened steel shaft is ground to final diameter and passes visual and dimensional inspection. Nital acid etch reveals dark bands at regular
intervals along the ground surface — re-tempered (softened) zones from grinding burn. The dark bands are locally softened martensite with tensile
residual stress. This shaft must be rejected — the fatigue life has been compromised regardless of the dimensional compliance. Root cause: glazed
grinding wheel or insufficient coolant. Do not accept any ground fatigue-critical component without specifying etch inspection.
Caution: Chatter marks on a milled bore evaluated as within Ra tolerance
A milled bore shows a wave-like surface pattern characteristic of chatter. Profilometer measurement shows Ra = 1.6 μm — within the specified
limit. Do not accept on Ra alone. Chatter marks introduce cyclic residual stresses whose period matches the wave pattern — under pressure cycling
they can nucleate fatigue cracks at a much lower stress than a uniformly rough surface. Flag the chatter pattern, identify the root cause (tool
overhang, fixture rigidity, cutting parameters), correct it, and re-inspect.
Good Practice: Specifying NDT method on the machining drawing note
A bearing journal on a hardened shaft includes a drawing note: 'MT after final grind; Nital etch acceptance per AMS 2759/9.' The technician
performs MT — no indications. Then applies Nital etch per the procedure — no re-tempered or re-hardened zones. Both steps are required; MT
alone cannot detect grinding burn. The complete inspection record is signed off as the final release document. This is the correct sequence for any
ground fatigue-critical surface.

## Slide 14
Core Question Answers
What happens at the cutting zone and why does it matter for part quality?
Three deformation zones: primary shear zone (chip forms, most energy), secondary zone (tool-chip friction, heat), tertiary zone (flank rubbing, surface work
hardening). Heat goes 75–80% into the chip, rest into tool and workpiece. Cutting parameters and tool condition determine surface integrity — residual stress,
microstructural damage, and work hardening affect fatigue life and corrosion resistance.
What are the main machining processes and what does each produce?
Turning: workpiece rotates, single-point tool traverses — cylindrical surfaces, bores, threads. Milling: rotating multi-tooth cutter — flat surfaces, slots, pockets,
complex 3D geometry. Drilling: twist drill — holes (rough, Ra 1.6–6.3 μm; ream or bore for precision). Grinding: abrasive wheel — finest finish (Ra 0.025–0.8
μm), hardened materials, finishing operation after turning or milling.
What are the main cutting tool materials and how do you choose between them?
HSS: toughest, resharpened, <600°C — for drills, taps, interrupted cuts at moderate speed. Carbide: hardest practical, indexed inserts, high-speed production —
the default for most CNC work. Coatings (TiN, TiAlN): extend carbide life 3–10×. Ceramics: high-speed finishing of hard/cast iron, brittle. CBN: hardened steels
and superalloys. PCD: non-ferrous, composites — cannot machine steel.
How is surface finish measured and why does it matter?
Ra = arithmetic mean roughness (μm); Rz = peak-to-valley depth. Ra on a drawing is a legal requirement — stress concentrations at surface peaks reduce fatigue
life; rough bores leak and wear faster. Theoretical Ra for turning = f²/8r (feed² / 8 × nose radius). Surface integrity also encompasses residual stress, work
hardening depth, and microstructural alteration — all affect fatigue performance.
What machining defects should a technician recognize and know how to detect?
Built-up edge marks (torn surface — increase speed/lubrication); chatter marks (wave pattern — fix vibration); grinding burn/re-tempering (dark Nital etch
bands — tensile residual stress, reduced fatigue life — MT + etch); grinding cracks (network cracks — MT or PT, always reject); recast layer in EDM (white layer,
tensile stress — remove by grinding in fatigue-critical parts).

## Slide 15
Key Takeaways — Week 12: Machining
1
What happens at the cutting zone — shear deformation, heat generation, and tool-workpiece interaction — determines not
just the dimensions of the machined part but its surface integrity, residual stress state, and fatigue performance. Cutting
parameters and tool condition are quality parameters, not just productivity parameters.
2
Surface finish is a specified engineering requirement, not an aesthetic preference — Ra values on drawings must be verified.
The connection between surface roughness, stress concentration, and fatigue life means that a surface that looks acceptable
to the eye may still fail the specification and compromise service life.
3
Grinding burn and machining cracks are among the most serious manufacturing defects because they are often invisible to
visual inspection and introduce tensile residual stresses and microstructural damage that dramatically reduce fatigue life.
Recognizing the conditions that cause them and specifying MT, PT, or Nital etch inspection is essential knowledge for any
quality technician.

## Slide 16
Resources & What's Next
Week 12 Resources
Kalpakjian Ch. 21, 22 & 23
Fundamentals of Cutting · Tool Materials · Machining Processes — primary
reading
Cutting & Chip Formation Visualizer
Shear plane, chip types, heat zones, BUE — interactive
Sandvik Coromant Calculators
Turning and milling cutting speed, feed, and Ra calculators — interactive
Nital Etch Acceptance (AMS 2759)
Standard for inspecting ground hardened steel surfaces for burn —
reference
Barkhausen Noise Analysis
Non-contact grinding burn detection for production line use — reference
Week 13 — Powder Metallurgy
November 16, 2026 · Unit 4: Manufacturing continues
•
What powder metallurgy is and why it enables
materials impossible by any other route
•
Powder production — water and gas atomisation,
reduction, electrolytic deposition
•
Compaction and sintering — green compact, neck
formation, densification, HIP
•
PM limitations and defects — density gradients,
lamination cracks, blistering
•
Process selection — how to choose between casting,
forming, machining, and PM