## Slide 1
M E C H 1 9 1 — M e t a l l u r g y
Week 5
Stainless Steels & Cast Irons
September 21, 2026 · 5:00 – 7:30 PM · Kai Santos

## Slide 2
Class Agenda
01
Stainless Steels
What makes it stainless, and why the grade matters as much as the material family
02
Stainless Families
Austenitic, ferritic, martensitic, duplex, and PH — microstructure drives every property difference
03
Cast Irons
Why cast iron is not steel, and how the form of excess carbon determines the type

## Slide 3
Metallography Lab — Module 4
EXAMET-5-R-600-HD · 50–500×
Module 4 · Week 5
Stainless Steel Families
What to do this week:
Compare austenitic twins in D & E. Find the martensitic, precipitate-
hardened structure in F.
Steps:
1 Observe — complete feature table
2 Sketch — label magnification & specimen
3 Answer — 4 short questions
Specimens to Check Out
· Specimen D — 304 stainless steel
· Specimen E — 316 stainless steel
· Specimen F — 17-4PH stainless steel
How to check out the kit:
1 See instructor after class today
2 Sign out the specimen tray
3 Use the EXAMET-5 at your convenience
4 Return kit before leaving class
5 Submit completed module with your portfolio
Portfolio Handout — Module 4

## Slide 4
MECH 191 — Course & Unit Roadmap
Unit 1
Materials Fundamentals
Wk 1
Aug 24
Atomic Structure
& Bonding
Wk 2
Aug 31
Mechanical
Properties
Unit 2
Steel & Alloys
Wk 4
Sep 14
Carbon &
Alloy Steels
Wk 5 ← here
Sep 21
Stainless &
Cast Irons
Wk 6
Sep 28
Nonferrous &
Phase Diagrams
Unit 3
Testing & Quality
Wk 7
Oct 5
Mechanical
Testing
Wk 8
Oct 12
NDT Methods
Wk 9
Oct 19
Quality
Standards
Unit 4
Manufacturing
Wk 10
Oct 26
Casting
Wk 11
Nov 2
Forming
Wk 12
Nov 9
Machining
Wk 13
Nov 16
Powder
Metallurgy
Unit 5
Joining & Failure
Wk 14
Nov 23
Welding
Processes
Wk 15
Nov 30
Weld Metallurgy
& Failure
Wk 16
Dec 7
Corrosion
& Wrap-up
Week 17 · FINAL EXAM

## Slide 5
Week 5 — At a Glance
Topics
•
What makes stainless steel corrosion-resistant — the passive
chromium oxide layer
•
The four stainless steel families and how microstructure defines
each one
•
Austenitic (300s): FCC, Ni-stabilized, non-magnetic, best corrosion
resistance
•
Ferritic & martensitic (400s): BCC/BCT, magnetic, hardenable
grades
•
Cast iron as a distinct iron-carbon family — not a low-quality steel
•
Gray, white, ductile, and malleable cast iron — how carbon form
drives properties
•
When and why to choose cast iron over steel
Resources
Reference Material
Moniz 5th — Ch. 16 & 17
Cast Irons / Stainless Steels
Kalpakjian 6th — Ch. 6
Ferrous Metals and Alloys
Visualizer
Iron-Carbon Phase Diagram
(Interactive)
Reference
AISI/SAE Steel Designation Codes

## Slide 6
Core Questions
Try to answer these before we dive in — we'll revisit them with answers at the end of class.
1
What single threshold separates stainless steel from ordinary alloy steel — and why does that exact percentage
matter?
2
A coastal facility needs a tank for chloride brine: 304 or 316? What is the deciding factor?
3
Two castings from the same iron-carbon melt: one becomes gray iron, one white iron. What determined which
was which?
4
Why is gray cast iron standard for engine blocks and machine bases, despite having low tensile strength?
5
A martensitic stainless weld cracks in the heat-affected zone. What most likely went wrong, and how do you
prevent it?

## Slide 7
What Makes Stainless Steel 'Stainless'?
All stainless steels share one feature: a minimum of 10.5% chromium by weight. That single threshold is
what separates stainless from ordinary alloy steel.
The Passive Chromium Oxide Layer
•
Chromium reacts with atmospheric oxygen to form a thin, stable
Cr₂O₃ layer on the surface — invisible, only a few nanometers
thick
•
This passive layer acts as a barrier, preventing oxygen and
moisture from reaching the steel beneath
•
Self-repairing: if scratched or abraded, the layer reforms
spontaneously in the presence of oxygen
•
Destroy the passive layer (with chlorides, oxygen-poor
environments, or mechanical damage in an aggressive medium)
and corrosion can proceed rapidly
•
10.5% Cr is the threshold — below this, not enough Cr₂O₃ forms
to maintain a complete, stable passive layer
Key Alloying Thresholds
≥ 10.5% Cr
Stainless threshold
Passive layer forms. Now classified as stainless steel.
+ Nickel
Austenite stabilizer
Keeps FCC structure at room temp → non-magnetic,
ductile, tough.
+ Molybdenum
Pitting resistance
Improves resistance to chloride pitting (e.g., 316 vs.
304).
+ Carbon
Hardenability
Enables hardening by heat treatment → martensitic
grades.

## Slide 8
Stainless Steel Families — Microstructure Is Everything
Same passive chromium oxide layer — very different microstructures. The balance of alloying elements
determines which phase is stable at room temperature, and that phase determines everything.
Austenitic
300 series
FCC
Non-magnetic · Cold work only
Cr: 18–20% / Ni: 8–12%
Nickel stabilizes the FCC
austenite phase all the way to
room temperature. Most
widely used family — best
combination of corrosion
resistance, formability, and
weldability. Cannot be
hardened by heat treatment.
304 (general purpose) · 316 (+
Mo for chloride resistance)
Food equipment, chemical vessels,
marine hardware, kitchen
appliances, medical devices
Ferritic
400 series
BCC
Magnetic · Not hardenable
Cr: 10.5–30% / Ni: No Ni
High chromium content
stabilizes the BCC ferrite
structure. No nickel makes
these grades less expensive.
Moderate corrosion resistance,
lower toughness in thick
sections and at low
temperatures.
430 (most common) · 439 · 446
Automotive trim and exhausts,
kitchen appliances, architectural
panels, dishwasher liners
Martensitic
400 series
BCC/BCT
Magnetic · Quench & temper
Cr: 10.5–18% / Ni: Low or none
Higher carbon content allows
martensite to form on
quenching. Can be hardened to
high strength — but at the cost
of lower corrosion resistance
and toughness compared to
austenitic grades. Requires
preheat and PWHT to weld.
410 · 420 · 440C
Cutlery, surgical instruments, valve
stems, pump shafts, turbine blades
Duplex
Various
Austenite
+ Ferrite
Semi-magnetic · Not by HT
Cr: 21–26% / Ni: 4–8%
Mixed austenite/ferrite
microstructure — higher
strength than austenitic, better
resistance to stress corrosion
cracking (SCC). Increasingly
common in oil & gas, chemical
processing, and marine
environments.
2205 · 2507
Subsea pipework, chemical plant,
heat exchangers, desalination
equipment

## Slide 9
Austenitic Stainless — The Workhorse Family (300 Series)
Austenitic grades account for over 70% of all stainless steel produced. 304 and 316 are the two grades a
technician will encounter most often.
304
General-Purpose Austenitic
18% Cr / 8% Ni — the most widely used stainless steel in
the world
•
Excellent corrosion resistance in most atmospheric,
food, and chemical environments
•
FCC structure — very ductile and tough, excellent
formability
•
Non-magnetic in annealed condition (can become
slightly magnetic after cold work)
•
Good weldability — low carbon 304L grade available
for thicker weld sections to prevent sensitization
•
Cannot be hardened by heat treatment — only by
cold work
•
Susceptible to chloride pitting and stress corrosion
cracking (SCC) in chloride environments
Uses: sinks, countertops, food processing, chemical tanks, medical
trays, architectural panels
316
Marine & Chemical Grade
18% Cr / 10% Ni / 2–3% Mo — the upgrade for chloride
environments
•
Molybdenum addition dramatically improves resistance
to chloride pitting and crevice corrosion
•
The grade of choice for marine environments, seawater,
and halide-containing process streams
•
Same FCC structure and non-magnetic behavior as 304
•
316L (low carbon) is preferred for welded assemblies to
prevent sensitization
•
Higher cost than 304 — specify it when 304 has failed in
service or chlorides are known to be present
•
Used in pharmaceutical and food processing where
frequent washdowns with chlorine-based cleaners occur
Uses: marine fittings, chemical plant, pharmaceutical vessels,
coastal architecture, lab equipment

## Slide 10
Ferritic & Martensitic Stainless — The 400 Series
Both are magnetic BCC-based grades. Ferritic cannot be hardened; martensitic can — but both trade
corrosion resistance for other performance priorities.
Ferritic (e.g. 430)
BCC structure · Magnetic · No nickel · NOT hardenable by
heat treatment
•
BCC ferrite phase at all temperatures — high chromium
(10.5–30%) stabilizes BCC and prevents transformation to
austenite
•
No nickel = lower cost than austenitic grades
•
Moderate corrosion resistance — good for mild
environments, not suitable for chloride-rich or highly
aggressive conditions
•
Limited toughness, especially at low temperatures and in
thick sections
•
Good oxidation resistance at elevated temperatures —
useful in exhaust systems
•
Magnetic — can be detected and separated with
magnets (useful in recycling/fabrication)
Martensitic (e.g. 410, 420)
BCC/BCT structure · Magnetic · Hardenable · Higher carbon
than ferritic
•
Higher carbon content allows martensite to form when
austenite is quenched — the same mechanism as tool
steels, applied to a stainless grade
•
Can be hardened to high strength and hardness by
quench and temper — the only stainless family with
significant heat treatment response
•
Lower corrosion resistance than austenitic or ferritic
grades (less Cr, more C)
•
Magnetic in all conditions
•
Requires preheat (typically 200–300°C) and post-weld
heat treatment when welding — failure to do so causes
hard, brittle heat-affected zones prone to cracking
•
410 (general purpose) · 420 (higher C, cutlery) · 440C
(maximum hardness)
Welding Note:
Ferritic: limited weldability in thick sections — grain growth reduces toughness. Martensitic: MUST
preheat; PWHT strongly recommended. Never weld martensitic in the hardened condition.

## Slide 11
Cast Iron — A Distinct Family, Not a Low-Quality Steel
Cast iron is NOT steel that didn't make it. It is a separate family of iron-carbon alloys with its own unique
microstructures, properties, and engineering roles.
What Defines Cast Iron
•
Carbon content above 2.14% — typically 2.5–4%
plus significant silicon (1–3%)
•
At these carbon levels, the excess carbon cannot
stay in solid solution — it must precipitate out
during solidification
•
The FORM the carbon takes when it precipitates
determines everything about the cast iron type
•
Silicon content affects how carbon precipitates:
more Si → graphite forms; less Si → iron carbide
(cementite) forms
•
Cast iron is poured into complex shapes — generally
not wrought, rolled, or drawn into structural
sections
•
Melting point lower than steel (~1150–1200°C vs.
~1500°C) — easier to pour into complex molds
•
Generally more brittle than steel — most grades
cannot absorb significant impact loading
Steel vs. Cast Iron — Key Differences
Property
Steel
Cast Iron
Carbon
0.02–2.14%
> 2.14% (typ. 2.5–4%)
Structure
Wrought (rolled,
forged, drawn)
Cast (poured into
molds)
Ductility
Good to excellent
Poor (most grades)
Toughness
Good — absorbs
impact
Poor — brittle fracture
Machinability
Moderate
Excellent (gray iron esp.)
Damping
Low
Excellent (gray iron)
Weldability
Fair to good
Poor — very difficult
Cost/shape
Higher for complex
shapes
Cheap for complex
shapes

## Slide 12
Gray & White Cast Iron — Two Extremes
The same iron-carbon composition can produce dramatically different materials depending on cooling rate
and silicon content — which determines the form carbon takes.
Gray Cast Iron
Carbon precipitates as GRAPHITE FLAKES — slow cooling,
higher silicon
•
Graphite flakes act as internal stress concentrators —
crack initiation sites that limit tensile strength
•
Poor tensile strength but excellent compressive strength
— used where loads are compressive
•
Graphite provides self-lubrication and acts as a chip
breaker — reduces wear and aids machining
•
Outstanding vibration damping — graphite absorbs
energy; ideal for machine bases and engine blocks
•
Fracture surface appears gray (hence the name) —
identified visually
•
Inexpensive and easy to cast into complex shapes —
most widely produced cast iron
Engine blocks, machine tool bases, brake rotors, pipe, manhole
covers, cookware
White Cast Iron
Carbon locked as IRON CARBIDE (Fe₃C / cementite) — rapid
cooling, lower silicon
•
Rapid cooling (or low Si content) prevents graphite from
forming — carbon stays as cementite (Fe₃C)
•
Cementite is extremely hard and brittle — Rockwell C
65–70+ in some compositions
•
Very high wear resistance — resists abrasive wear
exceptionally well
•
Not machinable by conventional cutting tools — must be
ground
•
Very brittle — fractures with little or no warning, cannot
absorb impact
•
Fracture surface appears white or light-colored
(cementite is pale)
•
Starting material for malleable cast iron — white iron is
annealed to convert cementite to carbon rosettes
Mill liners, crusher plates, grinding media, pump wear parts,
starting stock for malleable iron

## Slide 13
Ductile & Malleable Cast Iron — Engineering-Grade Cast Irons
Both achieve improved ductility by changing the shape of the carbon phase — eliminating the sharp flakes
that make gray iron brittle.
Ductile (Nodular) Iron
Magnesium or cerium added to the melt just before casting
— graphite forms as SPHEROIDS, not flakes
•
Spheroidal graphite shape eliminates the notch
effect of flakes — no internal stress concentrators
•
Dramatically improved ductility, toughness, and
tensile strength compared to gray iron
•
Tensile strength 400–900 MPa — approaching
medium-carbon steel performance
•
Can be heat treated to further adjust properties
•
Good castability — complex shapes achievable at
lower cost than steel castings
•
The most widely used cast iron for structural and
load-bearing applications
Crankshafts, gears, heavy-duty pipe, automotive suspension, wind
turbine housings, pump bodies
Malleable Cast Iron
White cast iron annealed at high temperature — cementite
converts to rounded TEMPER CARBON rosettes
•
Two-step process: cast as white iron (rapid cooling), then
anneal for many hours at ~900°C to convert cementite
•
Temper carbon rosettes have rounded edges — much
less severe stress concentration than graphite flakes
•
Good ductility and machinability — significantly better
than white or gray iron
•
Slower, more expensive process than producing ductile
iron — largely being replaced in modern applications
•
Still used for thin-section castings where ductile iron has
difficulty (small fittings, hand tools)
Pipe fittings, hand tools, brackets, agricultural equipment,
automotive parts (legacy)

## Slide 14
Cast Iron — Choosing the Right Grade
Cast iron is chosen when its specific characteristics are an advantage, not a limitation. Understanding which
property each type excels at is the key to correct grade selection.
Gray Iron
Graphite
Flakes
Strength: Low tensile
high compressive
Damping: Excellent
Machin.: Excellent
Toughness: Poor
Choose when:
Best vibration damping of any
common engineering metal.
Choose for machine bases,
engine blocks, brake rotors, and
anything where vibration
absorption matters.
Avoid when:
Any application with significant
impact or tensile loading. Avoid
where fracture toughness is
needed.
White Iron
Iron Carbide
(Fe₃C)
Strength: Very high comp.
no tension
Damping: Poor
Machin.: Not machinable
Toughness: Very poor
Choose when:
Maximum wear resistance is the
priority and brittleness can be
tolerated. Ideal for mill liners,
crusher plates, and grinding
equipment.
Avoid when:
Structural applications. Any impact
loading. Cannot be welded or
machined conventionally.
Ductile Iron
Graphite
Spheroids
Strength: High — up to
900 MPa
Damping: Moderate
Machin.: Good
Toughness: Good
Choose when:
Need good mechanical
properties at lower cost than
steel castings. Crankshafts, gears,
heavy pipe, and structural
castings where ductile iron
replaces steel forgings.
Avoid when:
Extreme impact or shock loading
— still less tough than steel. Not
suitable where welding is required.
Malleable Iron
Temper Carbon
Rosettes
Strength: Moderate
Damping: Moderate
Machin.: Excellent
Toughness: Moderate
Choose when:
Thin-section castings requiring
ductility and machinability where
ductile iron is difficult to cast.
Fittings, hand tools, and small
hardware.
Avoid when:
Thick sections — process
economics make ductile iron more
attractive. Being phased out for
most new applications.

## Slide 15
Stainless & Cast Iron — Fabrication Considerations
Stainless steels and cast irons each present specific challenges in the shop. Understanding why these
requirements exist is more valuable than just following a checklist.
1
Sensitization in Austenitic Stainless
When austenitic stainless is held at 425–815°C (during
welding), chromium carbides precipitate at grain boundaries
— depleting nearby zones of Cr below 10.5%. This
'sensitized' zone is no longer corrosion-resistant. Solution:
use low-carbon grades (304L, 316L) or stabilized grades (321,
347 with Ti/Nb). Always specify L-grade for welded
fabrication in corrosive service.
2
Martensitic Stainless — Preheat & PWHT
Martensitic stainless must be preheated (typically 200–
300°C) before welding to slow cooling and prevent
martensite formation in the heat-affected zone before
hydrogen can escape. PWHT (temper at 650–750°C) restores
toughness. Welding in the hardened condition without these
steps causes cracking — the HAZ becomes a brittle fracture
initiation site.
3
Cast Iron Welding — Why It's Difficult
High carbon content means high carbon equivalent —
virtually all cast irons have CE > 1.0, requiring extreme
preheat (400–600°C for gray iron) or cold welding with
nickel-based filler. The primary risk is white iron formation in
the HAZ as carbon migrates and cementite forms during
rapid cooling. Pre-heat slow-cool and stress relief are
mandatory for structural welds in gray and ductile iron.
4
Stainless Contamination Control
Stainless steel passive layers are destroyed by contact with
carbon steel particles (rust transfer), chloride-containing
cleaners, and abrasive contamination. In fabrication: use
dedicated stainless tools, discs, and wire brushes. Never use
carbon steel wire brushes on stainless. Pickle and passivate
welds and heat-affected zones on austenitic stainless after
fabrication to restore full corrosion resistance.

## Slide 16
Core Questions — Answers
1
What threshold makes stainless 'stainless,' and why that exact value?
≥ 10.5% Cr. Below this, not enough Cr₂O₃ forms to maintain a complete passive layer. Above this, the layer forms
spontaneously and self-repairs when scratched.
2
304 or 316 for a chloride-brine tank — and why?
316. The 2–3% Mo addition dramatically improves resistance to chloride pitting and crevice corrosion — exactly the
failure mode seawater causes in 304.
3
Same melt, two castings: one gray iron, one white iron. What determined which?
Cooling rate and silicon content. Slow cooling + higher Si → graphite flakes form (gray iron). Rapid cooling + lower Si →
carbon stays as cementite/Fe₃C (white iron).
4
Why gray cast iron for engine blocks despite low tensile strength?
Graphite flakes provide outstanding vibration damping and excellent compressive strength — the loads are
compressive. Graphite also self-lubricates and aids machining.
5
Martensitic stainless HAZ cracks after welding. What went wrong?
Missing preheat (200–300°C) and/or PWHT. Without preheat, hydrogen is trapped in brittle martensite. Without
PWHT (temper 650–750°C), the HAZ remains hard and fractures.

## Slide 17
Key Takeaways
1
Stainless steel is a family — the grade determines the microstructure
Specifying 'stainless' without a grade is insufficient. The microstructure (FCC austenite, BCC ferrite, BCT martensite)
determines magnetic behavior, hardness response, toughness, and corrosion resistance in each service environment.
2
10.5% chromium creates the passive layer — everything else is fine-tuning
Ni stabilizes austenite. Mo improves chloride resistance. C enables hardening. Si and Cr content determine which phase is
stable. Every grade decision traces back to what the passive layer needs to survive in the intended environment.
3
Cast iron's properties are determined by the form its excess carbon takes
Graphite flakes (gray) → damping and machinability but brittle. Spheroids (ductile) → strength and toughness. Carbides
(white) → extreme hardness but very brittle. Temper carbon (malleable) → improved ductility after annealing.
4
Cast iron is not failed steel — it is a deliberate engineering choice
When damping, castability, or wear resistance is the priority, cast iron outperforms steel. The engineer chooses the material
based on service requirements — a technician who understands why helps avoid misapplication.
5
Safety is not optional!
PPE is mandatory in the shop — no exceptions. We work with heat, sharp edges, and hazardous materials every lab session.
Protect yourself and your classmates.

## Slide 18
Resources & What's Next
Week 5 Resources
•
Moniz Ch. 16 & 17 — Cast Irons & Stainless Steels
•
Kalpakjian Ch. 6 — Ferrous Metals and Alloys
Visualizers
•
Iron-Carbon Phase Diagram (Interactive)
•
AISI/SAE Steel Designation Codes (Reference)
Coming Up — Week 6
Nonferrous Metals & Phase
Diagrams
•
Aluminum, copper, and titanium — why each family
exists alongside steel
•
Reading the iron-carbon phase diagram — phases,
regions, and key transformation points
•
From equilibrium to real-world cooling — how CCT
diagrams show what actually forms
•
Unit 2 Quiz covers Weeks 4–6 — review steel
grades, heat treatment, and nonferrous metals
Unit 2 covers Weeks 4 – 6 · Review cast irons, stainless steels, and ferrous metals before Week 6