## Slide 1
M E C H 1 9 1 — M e t a l l u r g y
Week 6
Nonferrous Metals & Phase Diagrams
September 28, 2026 · 5:00 – 7:30 PM · Kai Santos

## Slide 2
Class Agenda
01
Nonferrous Metals
Aluminum, copper, and titanium — what each family offers that steel cannot
02
Iron-Carbon Phase Diagram
Reading the map of steel microstructures — phases, regions, and key transformation points
03
Putting It Together
Technician's perspective on phase diagrams — and Unit 2 Quiz

## Slide 3
Metallography Lab — Module 5
EXAMET-5-R-600-HD · 50–500×
Module 5 · Week 6
Nonferrous Metals & Phase Diagrams
What to do this week:
Observe twin density in brass vs. stainless steel. Look for fine Mg₂Si
precipitates in Al at 500×.
Steps:
1 Observe — complete feature table
2 Sketch — label magnification & specimen
3 Answer — 4 short questions
Specimens to Check Out
· Specimen G — 6061-T6 aluminum
· Specimen K — 70/30 brass
How to check out the kit:
1 See instructor after class today
2 Sign out the specimen tray
3 Use the EXAMET-5 at your convenience
4 Return kit before leaving class
5 Submit completed module with your portfolio
Portfolio Handout — Module 5

## Slide 4
MECH 191 — Course & Unit Roadmap
Unit 1
Materials Fundamentals
Wk 1
Aug 24
Atomic Structure
& Bonding
Wk 2
Aug 31
Mechanical
Properties
Unit 2
Steel & Alloys
Wk 4
Sep 14
Carbon &
Alloy Steels
Wk 5
Sep 21
Stainless &
Cast Irons
Wk 6 ← here
Sep 28
Nonferrous &
Phase Diagrams
Unit 3
Testing & Quality
Wk 7
Oct 5
Mechanical
Testing
Wk 8
Oct 12
NDT Methods
Wk 9
Oct 19
Quality
Standards
Unit 4
Manufacturing
Wk 10
Oct 26
Casting
Wk 11
Nov 2
Forming
Wk 12
Nov 9
Machining
Wk 13
Nov 16
Powder
Metallurgy
Unit 5
Joining & Failure
Wk 14
Nov 23
Welding
Processes
Wk 15
Nov 30
Weld Metallurgy
& Failure
Wk 16
Dec 7
Corrosion
& Wrap-up
Week 17 · FINAL EXAM

## Slide 5
Week 6 — At a Glance
Topics
•
Aluminum, copper, and titanium — why each family exists
alongside steel
•
Aluminum alloy designation (1xxx–7xxx) and heat-treatable vs.
work-hardened series
•
Brass and bronze — how copper alloys balance conductivity,
strength, and corrosion resistance
•
Titanium's alpha/beta microstructure and why Ti-6Al-4V
dominates aerospace
•
The iron-carbon phase diagram: ferrite, austenite, cementite,
pearlite, and eutectoid
•
CCT diagram — what actually forms during real cooling vs.
equilibrium predictions
•
Annealing, normalizing, quenching, tempering, and case
hardening
Resources
Reference Material
Moniz Ch. 6 — Phase Diagrams
Kalpakjian Ch. 7
Nonferrous Metals and Alloys
Visualizers
Iron-Carbon Phase Diagram (Interactive)
Solidification & Dendrite Growth
Unit 2 Quiz
Covers Weeks 4–6

## Slide 6
Core Questions
Try to answer these before we dive in — we'll revisit them with answers at the end of class.
1
What are the three major nonferrous metal families and what unique advantage does each offer that steel cannot
match?
2
What does the iron-carbon phase diagram tell you — and what critical information does it NOT give you?
3
What is the difference between an iron-carbon phase diagram and a CCT diagram, and when do you need each
one?
4
How does cooling rate determine the microstructure — and therefore the mechanical properties — of steel?
5
Quenched martensite is extremely hard but is almost never used in that condition. What does tempering do, and
what trade-off does it involve?

## Slide 7
Nonferrous Metals — Why They Exist Alongside Steel
Aluminum
1/3 the density of steel
•
~2.7 g/cm³ — dominant in
aerospace, automotive, and
structural applications where weight
matters
•
Naturally corrosion-resistant —
stable Al₂O₃ passive layer (similar to
stainless)
•
1xxx–7xxx designation system; heat-
treatable (2xxx, 6xxx, 7xxx) and
work-hardened (1xxx, 3xxx, 5xxx)
series
•
Melts at ~660°C — much lower than
steel; weldable but requires
different process (GTAW/GMAW)
Copper
Best electrical conductivity
•
Standard for electrical wiring,
busbars, and heat exchangers — no
common structural metal matches it
•
Brass (Cu-Zn): good strength,
machinability, corrosion resistance
— fittings, valves, decorative
•
Bronze (Cu-Sn or Cu-Al/Si): higher
strength and wear resistance —
bearings, bushings, marine
hardware
•
High thermal conductivity demands
greater heat input when welding
compared to steel
Titanium
Best strength-to-weight ratio
•
~60% the density of steel, with
comparable or superior strength —
used in aerospace, medical implants
•
Corrosion resistance exceeds even
the best stainless in most
environments
•
Alpha (HCP), beta (BCC), and alpha-
beta alloys — Ti-6Al-4V (Grade 5) is
the workhorse alloy
•
Extremely reactive at elevated
temps — must weld in inert
shielding or vacuum to prevent
embrittlement

## Slide 8
Aluminum Alloys — Designation and Selection
4-Digit Designation System
Series
Alloying Element
Strengthening
Common Use
1xxx
Pure Al (≥99%)
Work-hardened
only
Electrical conductors, foil
2xxx
Cu alloying
Heat-treatable
Aerospace structures (7075
rival)
3xxx
Mn alloying
Work-hardened
only
Beverage cans, roofing
5xxx
Mg alloying
Work-hardened
only
Marine, structural,
pressure vessels
6xxx
Mg + Si alloying
Heat-treatable
Most widely used —
extrusions, frames
7xxx
Zn alloying
Heat-treatable
Highest-strength Al —
aircraft skins
Technician Notes
Melting point
~660°C — far lower than steel. High heat
input in welding can cause burn-through or
hot cracking without proper technique.
Weld process
GTAW (TIG) or GMAW (MIG) with inert
shielding. AC polarity for GTAW to break up
the tenacious Al₂O₃ surface oxide.
Heat treatment
T6 temper (solution treat + age) is the most
common condition for 6061 and 7075 —
provides near-peak strength.
Galvanic risk
Aluminum is anodic relative to steel and
copper. Avoid direct contact in wet
environments; use isolation gaskets.

## Slide 9
Copper & Titanium — Key Properties and Alloy Families
Copper Alloys
Best electrical & thermal conductivity of structural metals
•
Pure copper (C10000–C18000): highest conductivity —
standard for wiring, busbars, heat exchangers
•
Brass (Cu-Zn): improved strength and machinability over
pure Cu — fittings, valves, fasteners, decorative parts
•
Bronze (Cu-Sn): better wear resistance than brass —
bearings, bushings, gear blanks, marine hardware
•
Cu-Al / Cu-Si / Cu-Be bronzes: specialist alloys for
springs, corrosion-resistant bolts, non-sparking tools
•
Welding: high thermal conductivity demands greater
heat input than steel; most grades weld with GTAW or
GMAW; oxygen-free grades preferred to prevent porosity
Titanium Alloys
Best strength-to-weight ratio · exceptional corrosion resistance
•
Density ~4.5 g/cm³ (60% of steel) with comparable or
superior strength — indispensable in aerospace
•
Alpha alloys (HCP): best creep resistance at high
temperature; weldable; CP titanium used in chemical
processing
•
Beta alloys (BCC): highest strength, heat-treatable; used
for fasteners and springs
•
Alpha-beta: Ti-6Al-4V (Grade 5) — accounts for ~50% of
all titanium used; dominant in aircraft frames, jet engine
fan blades, medical implants
•
Welding: extremely reactive above 600°C — must use
inert gas trailing shield or weld in a purge box/vacuum;
any oxygen or nitrogen pickup causes brittle
embrittlement

## Slide 10
The Iron-Carbon Phase Diagram
What It Tells You
•
Maps the stable phases in the iron-carbon system from
pure iron (0% C) to iron carbide (6.67% C = Fe₃C)
•
Horizontal axis: carbon content (%). Vertical axis:
temperature (°C). Any point = equilibrium microstructure
at that T and composition
•
Crossing a phase boundary during heating or cooling
triggers a phase transformation
•
The diagram assumes equilibrium — it shows what
should form if you hold temperature long enough for the
microstructure to fully stabilize
•
It does NOT account for cooling rate — that is what the
CCT diagram is for
Key Regions & Points
Ferrite (α):
BCC, max 0.022% C at 727°C — soft and ductile; stable phase in
low-carbon steels at room temperature
Austenite (γ):
FCC, dissolves up to 2.14% C at 1147°C — the phase steel must be
in for most heat treatment to work
Cementite (Fe₃C):
6.67% C — extremely hard, brittle iron carbide; forms when
carbon exceeds solubility limit
Pearlite:
Not a phase — a microstructural constituent: lamellar ferrite +
cementite formed at eutectoid (0.77% C, 727°C)
Eutectoid point:
0.77% C at 727°C — austenite transforms simultaneously to ferrite
+ cementite; boundary between hypo- and hypereutectoid
Steel vs. Cast Iron:
2.14% C = boundary — above this, carbon can no longer fully
dissolve in austenite

## Slide 11
Reading the Phase Diagram — Steel Classification
Hypoeutectoid Steel
< 0.77% C
•
On slow cooling from austenite,
proeutectoid ferrite forms first at
grain boundaries
•
Remaining austenite then
transforms to pearlite at 727°C
•
Room-temperature microstructure:
ferrite + pearlite
•
More carbon → more pearlite →
higher strength, lower ductility
•
Examples: 1020 (0.20% C), 1040
(0.40% C) — most structural steels
fall here
Eutectoid Steel
= 0.77% C
•
Austenite transforms entirely to
pearlite at exactly 727°C — no
proeutectoid phase
•
Finest microstructure achievable by
slow cooling alone
•
Maximum hardness from slow
cooling, but martensite gives far
higher hardness when quenched
•
Example: 1080 (0.80% C) — wire
rope, rail steel
Hypereutectoid Steel
> 0.77% C
•
On slow cooling, proeutectoid
cementite forms at prior austenite
grain boundaries before pearlite
•
Cementite network can cause
brittleness — often spheroidize
annealed to break up the network
•
Room-temperature microstructure:
cementite + pearlite
•
Examples: 1095 (0.95% C), 52100
bearing steel (1.0% C) — tools,
springs, bearings

## Slide 12
The Technician's Perspective — Putting It Together
Material Selection
•
Use aluminum (6061-T6) where weight matters and strength is moderate — most structural
fabrication, frames, enclosures
•
Specify copper alloy based on function: pure Cu for conductivity; brass for fittings/machinability;
bronze for bearings/wear
•
Titanium when steel is too heavy AND stainless isn't corrosion-resistant enough — budget for
specialized welding procedures
Reading a WPS / Material
Cert
•
Phase diagram knowledge lets you interpret weld heat-affected zone behavior — why HAZ can
soften (Al) or harden (medium-C steel)
•
CCT diagram reasoning: if you see 'preheat to 200°C,' that's slowing the cooling rate to avoid
martensite in the HAZ
•
Temper color on stainless or Ti welds tells you the surface temperature reached — purple =
~300°C, straw = ~200°C
Heat Treatment
Specifications
•
'Normalize and temper' on a drawing means two separate heating cycles — not one
•
Tempering temperature is critical: 150°C gives a different hardness than 450°C; verify with
hardness test after
•
Case depth on carburized parts is specified on drawing — confirm by sectioning a coupon and
etching with nital

## Slide 13
Core Questions — Answers
1
What are the three major nonferrous families and what unique advantage does each offer?
Aluminum (one-third the density of steel — weight-critical apps), Copper (best electrical/thermal conductivity —
wiring & heat exchangers), Titanium (best strength-to-weight ratio + exceptional corrosion resistance — aerospace &
medical).
2
What does the iron-carbon phase diagram tell you — and what does it NOT tell you?
It maps which phases are stable at equilibrium for any temperature and carbon %. It does NOT show what forms
during real industrial cooling — that requires the CCT diagram, which accounts for cooling rate.
3
What is the difference between the iron-carbon phase diagram and a CCT diagram?
Phase diagram = thermodynamic equilibrium — what forms if you hold temperature long enough. CCT = continuous
cooling — what actually forms at different cooling rates. CCT is steel-specific; phase diagram covers the whole Fe-C
system.
4
How does cooling rate determine the microstructure — and properties — of steel?
Slow → carbon diffuses fully → soft pearlite. Intermediate → bainite (stronger, tougher). Fast quench → carbon
trapped → hard brittle martensite. CCT diagram shows exactly which cooling curve produces which result.
5
What does tempering do to as-quenched martensite, and what trade-off does it involve?
Tempering reheats martensite below the austenite region, letting some carbon diffuse and relieving internal stress.
Trade-off: higher tempering temperature = more toughness but lower hardness. Required because as-quenched
martensite is too brittle for service.

## Slide 14
Key Takeaways — Week 6
01
The three major nonferrous families solve problems steel cannot: aluminum for weight, copper for conductivity,
and titanium for corrosion resistance combined with high strength-to-weight. Knowing when to reach for a
nonferrous alloy — and which one — is as important as knowing the steel families.
02
The iron-carbon phase diagram and the CCT diagram work together — the phase diagram shows what is
thermodynamically possible at equilibrium; the CCT diagram shows what actually forms under real cooling
conditions. You need both to reason about heat treatment.
03
Cooling rate is the most powerful processing variable in steel heat treatment: slow cooling gives soft pearlite,
fast quenching gives hard martensite, and tempering after quenching trades some hardness back for toughness.
This gives a technician the ability to reason about why a heat-treated part performs the way it does — and what
went wrong when it doesn't.

## Slide 15
Resources & What's Next
Reference Material
•
Moniz 5th Edition — Ch. 6: Phase Diagrams
•
Kalpakjian 6th Edition — Ch. 7: Nonferrous Metals
and Alloys
Visualizers
•
Iron-Carbon Phase Diagram (Interactive)
•
Solidification & Dendrite Growth (Interactive)
Coming Up — Week 7
Mechanical Testing
•
Tensile testing and the stress-strain curve — yield
strength, UTS, elongation
•
Hardness testing: Rockwell, Brinell, Vickers — when
to use each
•
Charpy impact testing — measuring toughness and
ductile-to-brittle transition
•
How testing results connect back to the
microstructures we mapped this week
Unit 2 Quiz covers Weeks 4 – 6 · Review the Fe-C diagram and CCT microstructures