MECH 191 — Unit Quizzes

Applied, scenario-based short-answer quiz — each question requires using a formula, chart, or diagram from the course reference materials to reach an answer

MECH 191 — Metallurgy

Leeward Community College · Math and Science Division · Mechatronics Program

Name: _______________________________________        Date: _______________        Unit: 3

Student Handout — write your answers in the space provided

Unit 3 — Testing, Inspection & Quality

1. A Brinell hardness test uses a 10 mm diameter ball under a 3000 kgf load, producing a 4.2 mm diameter indentation. Using HB = 2F / [πD(D − √(D²−d²))], calculate the Brinell hardness number, then use UTS(MPa) ≈ 3.45 × HB to estimate this steel's ultimate tensile strength.

________________________________________________________________________________________

________________________________________________________________________________________

________________________________________________________________________________________

________________________________________________________________________________________

________________________________________________________________________________________

2. An S-N curve for a steel alloy shows: at 400 MPa stress amplitude the part survives about 10⁴ cycles, at 300 MPa about 10⁶ cycles, and the curve flattens at 250 MPa (the endurance limit). A component in service sees a cyclic stress amplitude of 240 MPa. Based on this curve, would you expect the component to eventually fail from fatigue? Explain.

________________________________________________________________________________________

________________________________________________________________________________________

________________________________________________________________________________________

________________________________________________________________________________________

________________________________________________________________________________________

3. An impact-energy-vs-temperature curve for a pressure vessel steel shows 15 J absorbed at -40°C (lower shelf), 60 J at 0°C (transition region), and 120 J at 40°C (upper shelf). This vessel will operate in an environment that regularly reaches -30°C. What concern does this raise, and what does the curve tell you about the material's suitability at that temperature?

________________________________________________________________________________________

________________________________________________________________________________________

________________________________________________________________________________________

________________________________________________________________________________________

________________________________________________________________________________________

4. A weld inspector needs to detect a suspected lack-of-fusion defect located 15 mm below the surface of a 25 mm thick steel plate. Referencing the capabilities of VT, PT, MT, UT, and RT, which method(s) could actually detect this defect, and which should be ruled out immediately, and why?

________________________________________________________________________________________

________________________________________________________________________________________

________________________________________________________________________________________

________________________________________________________________________________________

________________________________________________________________________________________

5. A magnetic particle test reveals a linear indication 3 mm long at the toe of a fillet weld. The governing code states that linear indications longer than 1.5 mm in this location are unacceptable. Walk through how this finding moves through the indication → discontinuity → defect → reject sequence, and state the final disposition of the weld.

________________________________________________________________________________________

________________________________________________________________________________________

________________________________________________________________________________________

________________________________________________________________________________________

________________________________________________________________________________________