## Slide 1
M E C H 1 9 1 — M e t a l l u r g y
Week 1
Atomic Structure & Bonding
August 24, 2026 · 5:00 – 7:30 PM · Kai Santos

## Slide 2
Week 1 — At a Glance
Topics
•
What is metallurgy — and why does it matter?
•
The atom: protons, neutrons, electrons, valence shells
•
The Periodic Table — groups, periods, and metals
•
Atomic bonding — metallic, ionic, covalent
•
Alloys and solid solutions
•
Crystal structures — SC, BCC, FCC, HCP
•
Grains and grain boundaries
Resources
Reference Material
Moniz 5th — Ch. 4
Structure of Metals
Kalpakjian 6th — Ch. 3
Structure and Manufacturing
Properties of Metals
Visualizers
•
Crystal Structures Visualization
•
Periodic Table of Elements
•
Grain Boundaries and Types

## Slide 3
Alloy Research Portfolio — Module 1
No Microscope Required
Module 1 · Week 1
Atomic Structure & Bonding
What to do this week:
Research 1018 low-carbon steel (normalized): composition, mechanical
properties, and how normalizing produces its grain structure.
Steps:
1 Research — record data & sources
2 Answer — short-answer questions
3 Apply — critical-thinking & equations
Alloys of Record
· Alloy A — 1018 low-carbon steel (normalized)
How to Complete This Module:
1 Research the alloy(s) using credible sources
2 Record data with a source citation
3 Answer the short-answer questions
4 Answer the critical-thinking questions
5 Keep the module with your portfolio
Portfolio Handout — Module 1

## Slide 4
What is Metallurgy?
The science of metals — understanding structure, properties, and behavior so we can choose, test,
treat, and work with them effectively.
The Bronze Example — The First Alloy
Copper: abundant, conductive — but weak. Adding ~10–20% Tin disrupts copper's crystal lattice, creating
Bronze: significantly harder and stronger than either metal alone, while keeping copper's workability and
corrosion resistance. The first alloy in human history.
Why use alloys?
Pure metals rarely provide the
properties we need. Alloys let us
engineer the material for the job.
How do alloys work?
Adding a second element disrupts the
crystal structure, blocking deformation
and changing properties.
What comes next?
Carbon in iron → steel. Chromium in
steel → stainless. Every unit in this
course builds on this idea.

## Slide 5
The Atom
Three key components:
Protons
Positive charge — inside the nucleus — defines the element (atomic
number)
Neutrons
No charge — inside the nucleus — defines mass. Isotopes vary in
neutron count.
Electrons
Negative charge — orbit in energy bands/shells around the nucleus
Valence Electrons — The Bonding Shell
The outermost electrons — the only ones involved in bonding.
Carbon has 4 valence electrons, bonding in 4 directions
simultaneously. This is why adding carbon to iron creates steel —
carbon atoms sit between iron atoms and block deformation.
p⁺ n
valence e⁻

## Slide 6
The Periodic Table
Periods (Rows)
Organized by electron shells. Moving
down adds shells — each period is a
new shell level.
Groups (Columns)
Organized by valence electrons. Same
group = similar bonding behavior and
chemical properties.
Our Focus: Groups 3–12
Transition metals — Fe, Cu, Ni, Cr, Ti,
Mo, and all engineering metals live
here.
Classification by the staircase line:
Metals
Left of the staircase
•
Electrically & thermally
conductive
•
Malleable and ductile
•
Lustrous (shiny surface)
•
Solid at room temp (except Hg)
Metalloids
The staircase itself
•
Properties depend on conditions
•
Semiconducting — critical for
electronics
•
Behavior: part metal, part non-
metal
•
Si, Ge, As, Sb, Te, Po, At
Non-metals
Right of the staircase
•
Poor electrical conductors
•
Brittle (if solid) or gaseous
•
Non-lustrous
•
Tend to gain electrons

## Slide 7
Atomic Bonding
The Octet Rule: Atoms are most stable with 8 valence electrons — they bond (lose, gain, or share electrons)
to reach that stable state.
Metallic Bond
Metal + Metal
Electrons leave individual atoms and
form a shared 'electron sea' —
flowing freely through the structure.
Effect on material:
Conducts heat & electricity · Bends
without fracturing · Atoms slide past
each other
← Our primary focus
Ionic Bond
Metal + Non-metal
One atom gives away electrons; the
other takes them. Creates oppositely
charged ions that attract strongly.
Effect on material:
High melting point · Hard but brittle ·
Conducts only when molten or
dissolved
Covalent Bond
Non-metal + Non-metal
Neither atom gives up electrons —
they share them instead, forming
strong directional bonds.
Effect on material:
Extremely strong · Poor conductors ·
Can be very hard (diamond = covalent
network)

## Slide 8
Alloys and Solid Solutions
An alloy is an intentional mixture of two or more elements engineered for desired properties — most
engineering metals are alloys.
Substitutional Solid Solution
Works when atoms are within ~15% of each other in size
Added atoms swap into lattice positions of the host — like
replacing similarly sized bricks. The crystal structure
remains but is strained.
Example:
Copper-Nickel (Cu-Ni)
Brass (Cu + Zn)
Many stainless steel alloying additions
Interstitial Solid Solution
Added atoms are much smaller than the host atoms
Small atoms fit into gaps between host atoms — no host
atom is displaced. Even tiny amounts dramatically change
properties.
Example:
Carbon in Iron → Steel
Carbon atoms sit in gaps between Fe atoms, stiffening the
lattice and blocking slip

## Slide 9
Crystal Structures — Unit Cells
When metals solidify, atoms arrange into repeating 3D patterns. The unit cell is the smallest repeating
building block — like a tile in a tiled floor.
SC
Simple Cubic
Packing: 52%
Ductility: —
Atoms at 8 corners only.
Teaching example — not
found in real engineering
metals.
BCC
Body-Centered
Cubic
Packing: 68%
Ductility: Low
Corners + 1 center atom.
Stronger, less ductile.
Fe (room temp), W, Cr, Mo, V
FCC
Face-Centered
Cubic
Packing: 74%
Ductility: High
Corners + center + face atoms.
Most ductile — most slip
planes.
Al, Cu, Ni, Fe (>912°C), Au, Ag
HCP
Hexagonal
Close-Packed
Packing: 74%
Ductility: Med
Same packing as FCC, fewer
slip planes → less ductile.
Ti, Mg, Zn, Co

## Slide 10
Grains and Grain Boundaries
From unit cell to bulk metal:
Unit Cell
Single repeating building block (~0.3 nm). All atoms perfectly aligned.
Crystal / Grain
Millions of unit cells — all with the same orientation. One crystal
domain.
Polycrystalline Metal
Countless grains packed together, each pointing a different direction.
Why Grain Size Matters
Grain boundaries block dislocation movement — the mechanism by
which deformation spreads through metal. More boundaries =
stronger barriers to deformation.
Smaller grains → more boundaries → stronger, tougher material
Grain boundaries = white lines between regions

## Slide 11
Key Takeaways
1
Metallic bonding explains metals
Shared electron sea → electrical and thermal conductivity. Non-directional bonding → ductility. This is what
separates metals.
2
Navigate the periodic table
Transition metals (Groups 3–12) are the focus. Elements in the same column share behavior — useful for predicting
alloy effects.
3
Structure exists at every scale
Atoms arrange into unit cells → unit cells form grains → grains make bulk metal. Each level determines performance.
4
Know BCC, FCC, and HCP
FCC is most ductile (74%, many slip planes). BCC is stronger but less ductile. HCP has 74% packing but fewer slip
planes — less ductile than FCC.

## Slide 12
Resources & What's Next
Week 1 Resources
•
Moniz Ch. 4 — Structure of Metals
•
Kalpakjian Ch. 3 — Structure and Manufacturing
Properties of Metals
Visualizers
•
Crystal Structures Visualization
•
Periodic Table of Elements
Coming Up — Week 2
Mechanical Properties & Behavior
•
Stress and strain — the language of mechanical
behavior
•
Elastic vs. plastic deformation and the yield point
•
Crystal defects — point, line, planar, and volume
types
•
Grain boundaries, Hall-Petch, and diffusion through
solid metal
Unit 1 covers Weeks 1 – 2 · Review atomic bonding and crystal structures before Week 2